### Adsorption isotherm kinetics of copper, lead and cadmium onto Mukurweini’s raw kaolinite and alkali modified Kaolinite

### ABSTRACT

It is essential to remove heavy metal ions from industrial or domestic waste before they are released into water sources, as their presence in water, even in small concentrations, is a significant environmental concern. Industrial, domestic, and agricultural activities are the primary sources of heavy metal ion contamination in water sources. This study used Mukurweini Kaolinite and alkali-modified Kaolinite for lead, copper, and cadmium adsorption from an aqueous solution using a batch adsorption process. Of the three isotherm models investigated (Langmuir, Freundlich, and Temkin), the Freundlich model gave the best fit to the experimental data. The result of kinetic studies indicated that the adsorption process followed a pseudo-second-order, spontaneous physical progression.

Keywords: Adsorption, kinetics, kaolinite, modified kaolinite, Langmuir, Temkin, Freundlich

INTRODUCTION

It is of utmost importance to take action to reduce environmental heavy metal pollution, as it poses a serious health risk[1]. Lead, copper, and cadmium are some of the most common heavy metals that may be hazardous to human health[2]. Lead is a neurotoxin that can damage the neurological system and brain[3], while copper can be poisonous and harm the liver and kidneys when consumed in large doses. Additionally, cadmium, a known carcinogen, can cause cancer when present in high amounts[4]. Furthermore, environmental heavy metal pollution can also contaminate food and water supplies, thus increasing the danger of health issues[5]. Therefore, it is essential to take steps to reduce environmental heavy metal pollution in order to protect human health.

Adsorption studies are carried in order to gain a better understanding of the interactions between molecules and surfaces. Adsorption is the process in which molecules of a material are attracted to and remain on the surface of a solid or liquid [6]. Through these studies, the ability to analyze the surface properties of materials, such as surface area, pore size, and porosity, which can be used to create new materials and improve existing ones, as well as to develop more efficient separation and purification processes.  Determining the adsorption isotherm, kinetics, and thermodynamics of heavy metals in water can be immensely helpful in removing these metals from water [7]. The adsorption isotherm describes the connection between the heavy metal concentration in water and the quantity of metal adsorbed onto the surface of the adsorbent material [8]. Adsorption kinetics explains how quickly a heavy metal is adsorbed onto the surface of an adsorbent material [9].

The adsorption isotherm is one of the best ways to study adsorption while representing the relationship between the adsorbent, the adsorbate and the different external factors[10]. Adsorption isotherms represent these relationships using graphs. From the adsorption isotherms graph, one can know in which conditions the adsorption capacity is great and how to enhance the adsorption capacity. They are different models of adsorption isotherms, which are Langmuir, Freundlich, Temkin, isotherms models among[11].

Langmuir isotherm model assumes that adsorption occurs at a precise spot on the adsorbent's homogeneous site. This method is effective in adsorption processes containing molecular monolayer. This model assumes the Following factor ;

- adsorbent has an active site and only one adsorbate can interact with one adsorbent active site,

- All adsorbed molecule has the same energy therefore, there is no interaction between neighboring molecules.

- the adsorption frequency is proportional to the solution concentration and

- The adsorbate occupies the active site on the adsorbent fully [12]

Freundlich isotherm model deals with adsorption processes on heterogeneous site of the adsorbent with molecular multilayer. This model has the following advantages:

It enables the adequate description of non-linear adsorption in a well-defined way of the adsorbate concentration. It has a simplified mathematical equation that is easy to use and describes adsorption site with different energy level unlike the Langmuir isotherm model [13]. However, Freundlich isotherm model is not able to predict the maximum adsorption occurrence [14].

Temkin isotherm model focuses on the adsorbate-adsorbent interaction regardless of the external factors. Therefore, it is often used in adsorption heat with the non-uniform distribution. This model assumes that the decrease in temperature affects the adsorption linearly rather than how the Freundlich model suggested, logarithmically [15].

Adsorption kinetics is the measurement of the speed of adsorption versus time. It describes the adsorption mechanism and aids in the assessment of the adsorbent. Several kinetics models have been developed in the determination of the rates of adsorption. The most frequently applied adsorption kinetic models in the removal of water pollutants are Pseudo-first-order and Pseudo-second-order kinetic models.

Pseudo-first-order kinetic model is the first kinetic model has ever been used in the determination of the adsorption rate. In order to determine the adsorption rate, this model uses the adsorption capacity [16].

The pseudo-second-order- kinetic model, unlike the Pseudo-first-order kinetic model, is based on the adsorbent concentration in the determination of the adsorption rate[16].

Adsorption thermodynamics is an important parameter in the adsorption process because provides information on the spontaneity of adsorption process. This is determined from Gibb’s free energy (∆G0) that is calculated from the change in both the entropy (∆S0) and enthalpy (∆H0) of the system[17].

METHODS AND MATERIALS

The materials were collected from Nyeri County in Mukurweini, then dried in an oven at 80°C for 18 hours and finely ground using a motor and pestle. A part of this sample was then taken to a muffle furnace, where it was heated at 700°C for two hours. After this, it was hydrothermally treated with 8M of NaOH in a pressure cooker at 120°C for three hours. Finally, it was put back into the muffle furnace for two hours at 650°C. A batch adsorption study was conducted using two adsorbents, kaolinite and alkali-modified kaolinite, in order to determine the adsorption isotherm, adsorption kinetics, and adsorption thermodynamics.

The batch adsorption study was carried out and the sample solutions analyzed alongside standard solutions using an AA-6300 SHIMADZU Atomic Absorption Spectrophotometer and the following procedure: The computer connected to the AAS was first turned on, as different parameters were set. The ASS lamp was setting based on the metal being analyzed (copper, lead and cadmium).  After that, the compressed air and acetylene cylinders valves were opened and the flame was ignited. Using the University of Nairobi laboratory standards, the calibration curve was set. Different prepared samples were then injected into the flame and their absorbances were recorded.

RESULTS AND DISCUSSION

- ADSORPTION ISOTHERM

This study focused on three different adsorption isotherms: Langmuir, Freundlich and Temkin adsorption isotherms. The adsorption isotherms were studied at room temperature, pH 7 and 30 min contact time where Ce is the concentration at equilibrium and qe is the adsorption capacity at equilibrium.

- Langmuir adsorption isotherm

Using the Langmuir linear equation

Ceqe=1b1Kl+1bCe                                                                               (1)

Ce/qe vs. Ce were plotted and from the slope and intercept, the Langmuir constant KL and the maximum monolayer capacity qmax were calculated.  The maximum monolayer capacity qmax was calculated using the following equation:

qmax =1slope.                                                                                               (2)

Figure 1 illustrates, Langmuir adsorption isotherm for lead

Figure  1 Langmuir adsorption isotherm for lead

Figure 2 shows Langmuir adsorption isotherm for copper

Figure 2 Langmuir adsorption isotherm for copper

Figure 3 illustrates Langmuir adsorption isotherm for cadmium

Figure 3 Langmuir adsorption isotherm for cadmium

Langmuir isotherm is a model, which assumes that all the adsorption process takes place at a monolayer level and that the process is lateral. This means that one surface site can only be occupied by one molecule[18]. The Langmuir parameters obtained from plotting Ce/qe vs. Ce in table 4:5 can indicate three things: one, the adsorption was favorable, which means that the dimensionless equilibrium parameter, RL is between 0 and 1[19].

For this study, the RL values were 0.2485, 0.2695 and 0.5577 respectively lead, copper and cadmium. Two, the qmax, the maximum adsorption capacity, is very crucial in the determination of the adsorbent performance. The highest qmax in this study was obtained while using lead with 61.208g/g followed by copper 47.7502g/g, and cadmium with lowest maximum adsorption capacity of 23.5164g/g. Three, the KL, the Langmuir equilibrium constant, describes the adsorption/ desorption equilibrium of every adsorbate in contact with the adsorbents. This means that one particular portion of the adsorbent occupied by the one adsorbate at a very specific temperature and pressure[18]. Therefore, the highest KL of this study was 0.302L/g while using lead as an adsorbate followed by, 0.271 L/g, and 0.079 L/g respectively for copper and Cadmium. From the figure 1 to 3 a linear progression adsorption process of the adsorbate per adsorbent in unit mass is represented. This adsorption process fits the Langmuir adsorption isotherm model as their correlation coefficient R2 is above 0.95 (table 1). Therefore, it can be concluded that this is a monolayer adsorption.

Table 1 Langmuir adsorption isotherm constants

|  | CONSTANTS | Lead | Copper | Cadmium |
| --- | --- | --- | --- | --- |
| M-Kaolinite | KL(L/g) | 0.302365 | 0.271048 | 0.079307 |
|  | qmax(g/g) | 61.20896 | 47.75029 | 23.5164 |
|  | RL | 0.24853 | 0.2695 | 0.5577 |
|  | R2 | 0.966697 | 0.996844 | 0.953959 |
| Kaolinite | KL(L/g) | 1.429442 | 0.856043 | 3.301867 |
|  | qmax(g/g) | 30.20675 | 39.12857 | 28.6401 |
|  | RL | 0.24853 | 0.2695 | 0.5577 |
|  | R2 | 0.929424 | 0.898283 | 0.925385 |

- Freundlich adsorption isotherm

From the Freundlich linear equation

lnqe=lnKf+1nlnCe                                                                         (3)

The Freundlich constant Kf   and n, which is the index, representing the free energy associated with the multilayer adsorbents were determined after plotting lnqe vs. lnCe.

Figure  4 shows Freundlich adsorption isotherm for lead

Figure  4 Freundlich adsorption isotherm for lead

Figure 5 shows Freundlich adsorption isotherm for copper

Figure 5 Freundlich adsorption isotherm for copper

Figure 6 shows Freundlich adsorption isotherm for Cadmium

Figure 6 Freundlich adsorption isotherm for Cadmium

The Freundlich adsorption isotherm parameters give more insight on the multilayer coverage. KF represents the adsorption capacity and n is the index representing the free energy associated with the multilayer adsorbents. If 1/n=0, the adsorption isotherm is linear. If 1/n<1, the adsorption is non-linear. For this model to be applicable, 1\n has to be between 1 and 0 (n >0)[20]. KF represents the adsorption capacity but not at saturation like the qmax in Langmuir adsorption isotherm. In table 2, the values of n are between 1 and 3. This means that, 1/n is less than 1. Implying that, the Freundlich model is applicable for this study.

The adsorption capacity ranking KF was similar to the Langmuir adsorption isotherm. However, their values differed. The highest adsorption capacity in (mg/g)(L/mg)(1/n) was lead with a value equals to 13.9861, followed by, 10.1812and 2.1407 respectively for copper and cadmium. The coefficient of correlation of this study were respectively 0.995, 0.997 and 0.9889 respectively for lead, copper and cadmium. Therefore, this adsorption process fits best the Freundlich adsorption isotherm. Implying it is a multilayer adsorption.

Table 2 Freundlich adsorption isotherm constants

|  | CONSTANTS | Lead | Copper | Cadmium |
| --- | --- | --- | --- | --- |
| M-Kaolinite | n(L/mg) | 1.324247 | 1.415708 | 1.419274 |
|  | KF((mg/g)(L/mg)(1/n)) | 13.9861 | 10.18126 | 2.140731 |
|  | R2 | 0.995076 | 0.997383 | 0.989909 |
| Kaolinite | n(L/mg) | 2.295767 | 1.750613 | 2.621857 |
|  | KF((mg/g)(L/mg)(1/n)) | 16.92915 | 17.48657 | 21.7668 |
|  | R2 | 0.958092 | 0.970116 | 0.952525 |

c. Temkin adsorption isotherm

From this equation,

qe=RTb×lnA+RTb×lnCe                                                             (4)

The Temkin constants were determined after plotting qe vs. lnCe.

Figure 7 shows Temkin adsorption isotherm for lead

Figure 7 Temkin adsorption isotherm for lead

Figure 8 shows Temkin adsorption isotherm for copper

Figure 8 Temkin adsorption isotherm for copper

Figure 9 shows Temkin adsorption isotherm for Cadmium

Figure 9 Temkin adsorption isotherm for Cadmium

Temkin adsorption isotherm model emphasizes on even distribution of binding energy up to maximum binding energy. Even distribution as uniformity of the energy binding plays an important role in the interaction between the adsorbent and the adsorbate [21]. The main parameters of Temkin isotherm are KT ,the equilibrium binding constant, which is also the maximum binding energy; and B, the heat of adsorption. From figure 6 to figure 9 Lnqe and LnCe were plotted, and the two parameters were deduced. The heat of adsorption B was positive and adsorption energy was less than 20 J/mol throughout the adsorption process.

It means that this was an exothermic physical adsorption. The KT values from table 3 indicates that lead had the highest equilibrium binding constant 4.142 L/mg, implying that the interaction between the adsorbent and the adsorbate was high.  After lead, copper had the highest equilibrium binding followed by cadmium. The coefficient of correlation from this study was above 0.92. Therefore, this adsorption study fit the Temkin isotherm model, meaning there is an evenly distributed energy between the adsorbent and the adsorbate throughout the adsorption process.

Table 3 Temkin adsorption isotherm constants

|  | CONSTANTS | Lead | Copper | Cadmium |
| --- | --- | --- | --- | --- |
| M-Kaolinite | KT(L/mg) | 4.142331 | 2.855076 | 0.782683 |
|  | B(J/mol) | 8.118019 | 9.730484 | 4.918514 |
|  | R2 | 0.929582 | 0.9963 | 0.99149 |
| Kaolinite | KT(L/mg) | 15.15285 | 8.257104 | 39.53823 |
|  | B(J/mol) | 6.452853 | 8.578505 | 5.881098 |
|  | R2 | 0.915121 | 0.937422 | 0.888923 |

- ADSORPTION KINETICS

The adsorption kinetics was determined at room temperature, pH7, with an initial dosage and concentration 0.050 g and 10 ppm respectively, where Ce is the concentration at equilibrium, Ct the concentration at time t,  qe the adsorption capacity at equilibrium and qt the adsorption capacity at time t.

For the pseudo first model using this linear equation;

lnqe-qt=lnqe-K1t                                                                                    (5)

Ln (qe-qt) vs t was plotted and for the pseudo second model t/qt vs t was plotted from its linear equation;

tqt=1K2  qe2+1qet                                                                                               (6)

Figure 10  shows Pseudo first order reaction for lead

Figure 10  Pseudo first order reaction for lead

Figure 11 shows Pseudo second order reaction for lead

Figure 11 Pseudo second order reaction for lead

Figure 12 shows Pseudo first order reaction for copper

Figure 12 Pseudo first order reaction for copper

Figure  13 shows Pseudo second order reaction for copper

Figure  13 Pseudo second order reaction for copper

Figure 14 shows Pseudo first order reaction for cadmium

Figure 14 Pseudo first order reaction for cadmium

Figure 15 shows Pseudo second order reaction for cadmium

Figure 15 Pseudo second order reaction for cadmium

The adsorption kinetics data for the first and second pseudo reaction model were calculated in table 4.8. Form the data and figures 10 to 15, it was observed that, all the adsorption process fitted best the pseudo second order reaction with R2 of 0.99 for all the three heavy metals, which were much closer to 1 compared to the R2 of the first order reaction (0.95, 0.91 and 0.65 respectively for lead, copper and cadmium). The pseudo second order reaction model fits best not only because of the higher R2, but also because of its experimental qe, which was much closer to the calculated qe. Therefore, the adsorption rate is proportional to the square of the concentration of the adsorbate in the solution

Table 4 Pseudo first and second order reactions constants

| PSEUDO FIRST ORDER REACTION |  |  |  |  |
| --- | --- | --- | --- | --- |
| M-Kaolinite | CONSTANTS | Lead | Copper | Cadmium |
|  | K1 | 0.161054 | 0.041648 | 0.102167 |
|  | Qe | 5.673688243 | 10.7383316 | 0.598375147 |
|  | R2 | 0.954986 | 0.910278 | 0.625525 |
| Kaolinite | K1 | 0.167182 | 0.104121 | 0.080879 |
|  | Qe | 5.807350417 | 4.804314108 | 1.290551384 |
|  | R2 | 0.940709 | 0.963888 | 0.708665 |
| PSEUDO SECOND ORDER REACTION |  |  |  |  |
|  | CONSTANTS | Lead | Copper | Cadmium |
| M-Kaolinite | H | 15.01791 | 2.918251 | 2.408782 |
|  | K2 | 0.067264 | 0.012772 | 0.110837 |
|  | Qe | 14.94216625 | 15.1157393 | 4.661833526 |
|  | R2 | 0.999795 | 0.998049 | 0.991613 |
| Kaolinite | H | 15.0468 | 18.06875 | 67.4791 |
|  | K2 | 0.067375 | 0.070427 | 0.259744 |
|  | Qe | 14.94419057 | 16.01744793 | 16.11803117 |
|  | R2 | 0.999795 | 0.99941 | 0.99998 |

CONCLUSION

In conclusion, all the adsorption isotherms had a higher R2, above 0.91; but the Freundlich isotherm model had the highest coefficient of correlation. Therefore, the adsorptions were predominantly multilayer, with some monolayer coverage and an evenly distributed binding energy. From the Langmuir isotherm model, lead had the highest adsorption capacity of 47750.2 mg.g-1 and cadmium the lowest 23.5164 mg.g-1.The pseudo-second order reaction model fitted best this adsorption study due to two factors: the high R2, and the fact that the calculated qe were much closer to the pseudo second order reaction than the pseudo first order reaction. This adsorption study was spontaneous and feasible due to the negative Gibb’s free energy, nitrate having the highest -12.36 KJ.mol-1 and cadmium the lowest -0.064 KJ.mol-1

References

- Mitra, S., Chakraborty, A. J., Tareq, A. M., Emran, T. B., Nainu, F., Khusro, A., Idris, A. M., Khandaker, M. U., Osman, H., Alhumaydhi, F. A., & Simal-Gandara, J. (2022, April). Impact of heavy metals on the environment and human health: Novel therapeutic insights to counter the toxicity. Journal of King Saud University - Science, 34(3), 101865. https://doi.org/10.1016/j.jksus.2022.101865

- Tchounwou, P. B., Yedjou, C. G., Patlolla, A. K., & Sutton, D. J. (2012). Heavy Metal Toxicity and the Environment. Experientia Supplementum, 133–164. https://doi.org/10.1007/978-3-7643-8340-4_6

- Sanders, T., Liu, Y., Buchner, V., & Tchounwou, P. (2009, January). Neurotoxic Effects and Biomarkers of Lead Exposure: A Review. Reviews on Environmental Health, 24(1). https://doi.org/10.1515/reveh.2009.24.1.15

- Cui, Z. G., Ahmed, K., Zaidi, S. F., & Muhammad, J. S. (2021). Ins and outs of cadmium-induced carcinogenesis: Mechanism and prevention. Cancer Treatment and Research Communications, 27, 100372. https://doi.org/10.1016/j.ctarc.2021.100372

- Zaynab, M., Al-Yahyai, R., Ameen, A., Sharif, Y., Ali, L., Fatima, M., Khan, K. A., & Li, S. (2022, January). Health and environmental effects of heavy metals. Journal of King Saud University - Science, 34(1), 101653. https://doi.org/10.1016/j.jksus.2021.101653

- Hu, H., & Xu, K. (2020). Physicochemical technologies for HRPs and risk control. High-Risk Pollutants in Wastewater, 169–207. https://doi.org/10.1016/b978-0-12-816448-8.00008-3

- Chen, X., Hossain, M. F., Duan, C., Lu, J., Tsang, Y. F., Islam, M. S., & Zhou, Y. (2022, November). Isotherm models for adsorption of heavy metals from water - A review. Chemosphere, 307, 135545. https://doi.org/10.1016/j.chemosphere.2022.135545

- Abin-Bazaine, A., Campos Trujillo, A., & Olmos-Marquez, M. (2022, September 28). Adsorption Isotherms: Enlightenment of the Phenomenon of Adsorption. Wastewater Treatment. https://doi.org/10.5772/intechopen.104260

- Khamwichit, A., Dechapanya, W., & Dechapanya, W. (2022, June). Adsorption kinetics and isotherms of binary metal ion aqueous solution using untreated venus shell. Heliyon, 8(6), e09610. https://doi.org/10.1016/j.heliyon.2022.e09610

- Bleam, W. F. (2016, November 30). Soil and Environmental Chemistry. Academic Press.

- Bushra, R., Ahmed, A., & Shahadat, M. (n.d.). CHAPTER 5. Mechanism of Adsorption on Nanomaterials. Detection Science, 90–111. https://doi.org/10.1039/9781782623625-00090

- Sahu, O., & Singh, N. (2019). Significance of bioadsorption process on textile industry wastewater. The Impact and Prospects of Green Chemistry for Textile Technology, 367–416. https://doi.org/10.1016/b978-0-08-102491-1.00013-7

- Proctor, & Vasquez. (2009). Chapter 10 - The Freundlich Isotherm in Studying Adsorption in Oil Processing. Bleaching and Purifying Fats and Oils (Second Edition), 209–219. https://doi.org/10.1016/B978-1-893997-91-2.50016-X

- Sparks, D. L. (2002, November 1). Environmental Soil Chemistry. Academic Press. https://doi.org/10.1604/9780126564464

- Erhayem, M., Al-Tohami, F., Mohamed, R., & Ahmida, K. (2015). Isotherm, Kinetic and Thermodynamic Studies for the Sorption of Mercury (II) onto Activated Carbon from &lt;i&gt;Rosmarinus officinalis&lt;/i&gt; Leaves. American Journal of Analytical Chemistry, 06(01), 1–10. https://doi.org/10.4236/ajac.2015.61001

- Narayanan, S. (2019, December 31). Kinetic and Equilibrium Adsorption Studies of Methylene Blue from Aqueous Solution Using Low-Cost Adsorbent. International Journal of Psychosocial Rehabilitation, 23(4), 1722–1738. https://doi.org/10.37200/ijpr/v23i4/pr190503

- Chowdhury, Dr. Papita Saha and Shamik. (2011). Insight Into Adsorption Thermodynamics. In P. M. Tadash, thermodynamics (pp. 349-364). India: Intech.

- Liu, P., Liu, J., & Wang, M. (2019, January). Adsorption of ethanol molecules on the Al (1 1 1) surface: a molecular dynamic study. Royal Society Open Science, 6(1), 181189. https://doi.org/10.1098/rsos.181189

- Erhayem, M., Al-Tohami, F., Mohamed, R., & Ahmida, K. (2015). Isotherm, Kinetic and Thermodynamic Studies for the Sorption of Mercury (II) onto Activated Carbon from &lt;i&gt;Rosmarinus officinalis&lt;/i&gt; Leaves. American Journal of Analytical Chemistry, 06(01), 1–10. https://doi.org/10.4236/ajac.2015.61001

- Khayyun, T. S., & Mseer, A. H. (2019, October 14). Comparison of the experimental results with the Langmuir and Freundlich models for copper removal on limestone adsorbent. Applied Water Science, 9(8). https://doi.org/10.1007/s13201-019-1061-2

- Piccin, J. S., Dotto, G. L., & A. Pinto, L. A. (n.d.). Adsorption isotherms and thermochemical data of FD&C Red n° 40 binding by Chitosan. SciELO - Brasil - Adsorption Isotherms and Thermochemical Data of FD&C Red N° 40 Binding by Chitosan Adsorption Isotherms and Thermochemical Data of FD&C Red N° 40 Binding by Chitosan. https://doi.org/10.1590/S0104-66322011000200014.