[image: image15.jpg]\ -
e s AT

oo






11

Synthesis of 4-Methoxyacetophenone/Cyclodextrin Covered Copper Nanomaterials and pH-dependent behavior of 4-Methoxyacetophenone–Cyclodextrin inclusion complexes
Abstract
Absorption and emission spectral maxima of 4-methoxyacetophenone (4MAP) in different -CD and -CD concentrations with pH~3 and pH~7 solutions were analysed using UV-visible, fluorescence, time resolved fluorescence measurements and molecular modeling methods. The spectral properties of the Cu:4MAP:CD nanomaterial were examined using SEM, DSC, FTIR, XRD and 1H NMR. Single emission maximum noticed in the solvents while dual emission (ICT) observed in the CD solutions. Similar absorption and fluorescence spectral shifts observed establish that 4MAP form identical type of the inclusion complexes with α-CD and β-CD. The life time of the 4MAP increased in the following order: water < α-CD < β-CD indicates that β-CD:4MAP has more stable than α-CD. SEM picture clearly shows the morphological difference between copper nano, 2AS and the Cu nano inclusion complex. SEM pictures, DSC thermogram, FTIR, 1HNMR, XRD results supported that the formation of Cu-4MAP-α-CD and Cu-4MAP-β-CD nanomaterials. 
Key words: 4-methoxyacetophenone, cyclodextrin, copper nano, inclusion complex, nanomaterials.
1.  Introduction
The most important property of CD is their ability to admit a variety of appropriately sized guest molecules into the cavity with formation of inclusion complexes [1-10]. The recognised potential of the CD-guest interaction as a model for enzyme activity sites has attracted the attention of many investigators. Further, the photophysical and photochemical properties of organic molecules included in to the CD cavity are also largely different from those of the molecules in aqueous solutions. In this paper, we report: (i) the absorption and fluorescence spectral shifts of 4MAP in α-CD, β-CD, solvents of different polarities, and various pH conditions; (ii) the proton transfer behavior of 4MAP in aqueous, α-CD, and β-CD media; (iii) the structures and geometries of the resulting inclusion complexes using PM3 molecular modeling; and (iv) the doping effects of 4MAP:CD on silver nanomaterials, characterized by FTIR, XRD and SEM analyses [1-10].
2. Materials and Methods
2.1 Preparation of CD Solution
4MAP stock solution (2 × 10⁻² mol/dm³) was prepared, and aliquots of 0.1 or 0.2 mL were transferred into 10 mL volumetric flasks. Varying concentrations of α-CD or β-CD (0.2, 0.4, 0.6, 0.8, and 1.0 × 10⁻² mol/dm³) were added, followed by dilution to 10 mL with triple-distilled water. The mixtures were shaken thoroughly, yielding a final 4MAP concentration of 4 × 10⁻⁴ mol/dm³ in all samples. Experiments were conducted at 298 K.
2.2 Preparation of Cu:4MAP:CD nanomaterials
1 × 10⁻³ M CuSO₄ solution (100 mL) in a round-bottom flask was reduced by the dropwise addition of 1% sodium borohydride while stirring vigorously on a magnetic stirrer–hot plate. As reduction progressed, the solution color changed from pale blue to reddish brown. Then, 5 mL of 1% trisodium citrate was added dropwise as a stabilizing agent.

CD (1 mmol) was dissolved in 40 mL of distilled water, and 4MAP (1 mmol) dissolved in 10 mL of ethanol was slowly added to the CD solution. The mixture was stirred at 50 °C for 2 hours. The freshly prepared copper nanoparticle solution was then added and the combined mixture was stirred for an additional 2 hours. The resulting dilute solution was gently heated to 40–50 °C until its volume was reduced by approximately 50%. The solution was then refrigerated overnight at 5 °C. The precipitated Cu–4MAP–CD nanomaterial was collected by filtration, washed with small amounts of ethanol and water to remove uncomplexed 4MAP, copper, and CD, and then dried under vacuum at room temperature. The purified powder was stored in an airtight container and used for subsequent analyses [11-16].
3. Results and Discussion
3.1. Effect of α-CD and β-CD on 4-methoxy acetophenone
Absorption and fluorescence maxima of 4-methoxy acetophenone (4MAP) in pH~3, and pH~7 phosphate buffer solutions containing various concentrations of α-CD and β-CD have given in Table 1, Fig. 1 and Fig.2. In absence of CD, the absorption and emission maxima of 4MAP in the above pH solutions appears in the following wavelength: pH~3: λabs~275, 218 nm, λflu~365, 440 nm; pH~7: λabs~275, 218 nm, λflu~359, 440 nm; The above results indicate that, neutral species present in both pH~3 and pH~7 (Table 1). In both pHs, the absorption (275, 218 nm) and emission maxima (365 nm) be similar to the spectra observed in non-aqueous solvents (cyclohexane: λabs~273, 219 nm, λflu~355 nm; acetonitrile: λabs ~275, 220 nm, λflu~360 nm; methanol: λabs~275, 220 nm, λflu~365 nm; water: λabs~275, 220 nm, λflu~365 nm), hence it can be assigned to the molecular form of 4MAP. The above values reveal that absorption and emission spectra of 4MAP is red shifted from cyclohexane to water [17-30]. 
In the ground state, with an increasing the α-CD and β-CD concentrations in pH~3 and pH~7, the absorbance is increased at the same wavelength (λabs~275, 218 nm). In the excited state, with an increasing the α-CD and β-CD concentrations, the very low emission intensities are increased at the same wavelength. Interestingly, single emission is noticed in solvents and water, while dual emission observed in the CD solutions. The effect of α-CD and β-CD on the excited state of 4MAP is more prominent than the effect on the ground state. In addition, no noteworthy changes were detected in the absorbance of these solutions when recorded after 12 hrs.
A variety of changes observed in the absorbance and emission intensities and the spectral maxima are owing to the encapsulation of 4MAP molecule into the α-CD and β-CD cavities. In both pH solutions, the presence of isosbestic point in the absorption spectra and the identical spectral shift suggests similar inclusion complex formed between 4MAP and CDs [17-30]. 
The binding constant (K) values were obtained from the slope and the intercept of the Benesi-Hildebrand plot 1/A-A0 vs 1/[CD]2 and 1/ I-I0 vs 1/[CD]2 (both absorption and fluorescence) gives a linear relationship. However, a plot of 1/A-A0 vs 1/[CD] and 1/I-I0 vs 1/[CD] reveals an upward curve. This analysis reflects the formation of 2:1 inclusion complex between 4MAP:CD. The thermodynamic parameter ΔG values are negative which suggests that the inclusion proceeded simultaneously at 303K and it is an exothermic process.
Table 1  Absorption and fluorescence maxima of 4-methoxy acetophenone (4MAP) with different α-CD and β-CD concentrations.

	Concentration of
CD x10-3 M
	pH - 3.0
	pH - 7

	
	abs
	log 
	flu
	IF
	abs
	log 
	flu
	IF

	4MAP only
(without CD)
	275
218
	3.63
	365
	0.12
	275
218
	3.61
	359
	0.12

	0.2 M α-CD
	275
218
	3.64
	365 440
	0.13
	275
218
	3.64
	359
440
	0.14

	1.0 M α-CD
	275
218
	3.63
	365 440
	0.15
	275
218
	3.61
	359
440
	0.17

	0.2 M β-CD
	275
218
	3.75
	365 440
	
	275
218
	3.81
	358
443
	0.16

	1.0 M β-CD
	275
218
	3.69
	365 440
	0.12
	275
218
	3.81
	360 443
	0.19

	Excitation wavelength (nm)
	
	
	260
	
	
	
	260
	

	K (1:1) x105 M-1  α-CD
	35
	
	170
	
	45
	
	217
	

	G (kcalmol-1)   α-CD
	-8.96
	
	-12.94
	
	-9.51
	
	-13.56
	

	K (1:1) x105 M-1  β-CD
	52
	
	185
	
	66
	
	241
	

	G (kcalmol-1)  β-CD
	-9.96
	
	-13.15
	
	-10.56
	
	-13.83
	


[image: image1.jpg]Absorbance

09

06

03

0.0

PH-3[a-CD]

225

250

275

Wavelength(nm)

300




      [image: image2.jpg]094

Absorbance
o
>

03

0.0

210

PH-7[a-CD]

240

270 300
Wavelength(nm)




[image: image3.jpg]°
@

Absorbance

0.4

PH-3[p-CD]

210

T
240

T
270
Wavelength(nm)




     [image: image4.jpg]PH-7[B-CD]

12

Absorbance
°
m

04

00

Wavelength(nm)




Fig. 1 Absorption spectra of 4MAP in different α-CD and β-CD concentrations (M): (1) 0, (2) 0.002, (3) 0.004, (4) 0.006, (5) 0.008 and (6) 0.01.
[image: image5.jpg]IF

400

350

300

250

200

150

100

50

00

o-CD [PH-3]

-

60 420

Wavelength(nm)




     [image: image6.jpg]450

300

IF

150

350 400
Wavelength(nm)

«-CD [PH-7]

450




[image: image7.jpg]p- CD [PH-3]

300 350 400 450

Wavelength(nm)



    [image: image8.jpg]B-CD [PH-7]

300 350 400 450
‘Wavelength(nm)




Fig. 2 Fluorescence spectra of 4MAP in different α-CD and β-CD concentrations (M): (1) 0, (2) 0.002, (3) 0.004, (4) 0.006, (5) 0.008 and (6) 0.01.
As mentioned earlier, the dual emission intensities significantly increased as the α-CD and β-CD concentration increases. This is due to intramolecular charge transfer (ICT) formed in 4MAP molecule.  Further, due the space restriction of the CD cavities, both the normal and ICT emission intensities are enhanced. In our earlier publications, the reason for the ICT emission is explained in detail [17-30].
To prove the ICT emission between the 4MAP and α-CD/ β-CD, we also studied the solvent provoked changes in the absorption and fluorescence spectra for this molecule in selected solvents. The spectral maxima of the 4MAP in the solvents are already given. The results shown that, the absorption and emission maxima of 4MAP is red shifted from cyclohexane to water. 4MAP gave a single broad fluorescence spectrum in the solvents. The absence of longer wavelength emission maxima in polar solvents indicates that ICT or exciplex or excimer is not formed in all the solvents. 
3.2 Excited Singlet State Lifetimes
To examine the CD induced changes in the fluorescence spectra of 4MAP the emission decays of the normal (365 nm) and ICT emission (440 nm) were measured in water and 0.01 M α-CD and β-CD (Table 1). Biexponential decay was observed in aqueous and triexponential curve were obtained in α-CD and β-CD solutions. The lifetimes of the guest: host inclusion complexes were higher than that of the isolated guest molecules. The life time of the 4MAP increased in the following order: water < α-CD < β-CD indicates that 4MAP:β-CD has more stable than 4MAP:α-CD inclusion complex. The increase in the life time value with increase in CD concentration is due to the encapsulation of the 4MAP in the CD cavity. The life time values depend on the type of CD and the nature of the process with regard to short-lived species. This may be due to the vibrational restriction of the 4MAP in the excited state. 
The decay time of the ICT increases significantly from water to CD solution. The relative fluorescence intensity of the ICT increased upon addition of CD, but this was not observed in solvents. The monomer emission decay in water and other solvents was very fast while ICT emission was not observed. This decay behaviour indicates the formation of ICT in the presence of CD. The longer lifetime is ascribed to a deep encapsulation (inside the CD cavity), while a short lifetime is due to a loosely associated form. A deeper encapsulation is expected with β-CD as compared to the α-CD, which is likely to cause a greater enhancement of fluorescence in the former than in the latter.
The decay time of the monomer emission was observed to be very short in aqueous solution and also influenced by addition of CD. Further, on addition of CD, various decay ICT emission appeared suggesting the formation of inclusion complexes. One notes that the rise time of the ICT emission (which is different from the fast decay time of the normal emission), increased as CD concentration was increased, while it was not observed in water. This indicates that the ICT of the CD:4MAP inclusion complex is quite different from that of the solvents. Thus, the above results confirm that the formation of the ICT becomes more favorable in CD solution than in the water. 
3.3. Molecular Modeling
The PM3 level optimized structures of the 4MAP, α-CD, β-CD and the inclusion complexes are shown in Fig. 3. HOMO, LUMO, thermodynamic parameters (energy, enthalpy, entropy and free energy), dipole moment, zero point vibrational energy and Mulliken charge of the 4MAP, α-CD and β-CD and inclusion complexes values are summarized in Table 2. The interior cavity size of α-CD is 4.7- 5.3 Å and β-CD is 6.0 - 6.5 Å and the exterior cavity size of α-CD is 8.8 Å and β-CD is 10.8 Å. The interior and exterior cavity size of α-CD is lower than that of β-CD. In 4MAP, the vertical and horizontal bond distance between COCH3 –OCH3 is 9.46 Å and 4.33 Å respectively (Fig. 3). In 4MAP, the vertical and horizontal bond length between the COCH3 and methoxy group is higher than α-CD and -CD cavity size whereas the horizontal bond length is lower than α-CD and -CD cavity size. Considering the shape and dimensions of 4MAP can be entrapped in the α-CD and -CD cavity. Further, the optimized structures of the inclusion complexes were also confirmed that the guest molecules included in the CD cavity. 
[image: image9.png]


[image: image10.jpg]


 

[image: image11.jpg]



HOMO



LUMO
Fig. 3. PM3 optimized structures of (a, b) 4MAP (c, d) HOMO, LUMO of 4MAP
Table 2 Binding energies and HOMO, LUMO energy of 4-methoxy acetophenone (4MAP) with α-CD and β-CD by PM6 method.

	Properties
	4MAP
	α-CD
	β-CD
	4MAP-α-CD A
	4MAP-α-CD B
	4MAP-β-CD A
	4MAP-β-CD B

	EHOMO (eV)
	-9.25
	-10.05
	-9.99
	-9.25
	-9.41
	-9.23
	-9.18

	ELUMO (eV)
	-0.39
	0.14
	0.12
	-0.52
	-0.66
	-0.36
	-0.53

	EHOMO – ELUMO (eV)
	-8.85
	-10.19
	-10.11
	-8.73
	-8.74
	-8.86
	-8.65

	µ (eV)
	-4.82
	-4.95
	-4.93
	-4.88
	-5.03
	-4.79
	-4.85

	χ (eV)
	4.82
	4.95
	4.93
	4.88
	5.03
	4.79
	4.85

	η (eV)
	4.43
	5.09
	5.05
	4.36
	4.37
	4.43
	4.32

	S (eV)
	2.21
	2.54
	2.52
	2.18
	2.18
	2.21
	2.16

	ω (eV)
	5.24
	4.81
	4.81
	5.47
	5.80
	5.19
	5.45

	Dipole (D)
	3.37
	9.92
	10.52
	6.54
	6.55
	5.51
	4.62

	E*
	-60.20
	-1353.95
	-1577.74
	-1421.52
	-1427.90
	-1648.18
	-1653.31

	ΔE*
	
	
	
	-7.35
	-13.74
	-10.23
	-15.36

	G* 
	75.03
	510.13
	606.37
	602.34
	601.97
	698.75
	700.22

	ΔG*
	
	
	
	17.17
	16.80
	17.35
	18.81

	H*
	104.80
	599.76
	704.03
	702.34
	702.88
	806.82
	806.35

	ΔH*
	
	
	
	-2.22
	-1.68
	-2.02
	-2.48

	S**
	99.86
	300.59
	327.58
	335.38
	338.43
	362.43
	355.98

	ΔS**
	
	
	
	-65.07
	-62.02
	-65.01
	-71.46


* kcal mol-1  ** kcal/mol-Kelvin
The various thermodynamic parameters of the CD:4MAP is significantly changed than the isolated guest molecule indicates inclusion complex is formed. The polarity of the CD changed after the guest entered in to the CD cavity. The negative energy, enthalpy and Gibbs free energy changes suggested that the inclusion processes were energetically and enthalpically favourable in nature and it is an exothermic. The small negative ΔS value is due to enhancement of disorder in the system. 
3.4 Inclusion Complex Nanomaterials Studies
3.4.1 Scanning Electron Microscopy
The powdered form of copper nano, 4MAP, Cu:4MAP:α-CD and nano Cu:4MAP:-CD nanomaterials were investigated by SEM (Fig. 4). This picture clearly shows the morphological difference between copper nano, 4MAP and the Cu nano. Copper present in ball shape particles, 4MAP present in nanosheet image, Cu:4PDA:α-CD and Cu:4PDA:-CD present in nano stick image. SEM EDEX data confirm 46.8% carbon, 44.06% oxygen and 9.14 % Cu present in the nanomaterials. The different structure of pure nano Cu, 4MAP and the inclusion complex supports the formation of the Cu-4MAP-CD nano materials.

   [image: image12.png]



a)  Nano Copper  




b)  4MAP
[image: image13.png]


         [image: image14.png]



       c)  Cu -4MAP-α-CD


    
d)  Cu-4MAP-β-CD
Fig 4 SEM images for a) Cu nano, b) 4MAP, c) Cu:4MAP:α-CD and d) Cu:4MAP:β-CD. 
3.4.2 Differential Scanning Colorimeter 
The DSC curves of α-CD shown three endothermic peaks at 79.2 ºC, 109.1 ºC and 137.5 °C and β-CD shows a broad endothermic peak at 128.6 ºC and, these endothermic peaks are attributed to crystal water loss from CDs. The melting point of 4MAP shows a sharp peak at 40 °C. A broader endothermic effect was recorded for α-CD, β-CD and respective inclusion complexes as a consequence of water loss from the CDs. DSC thermogram of Cu-4MAP-CD complexes did not show peaks corresponding to pure 4MAP and CD, instead new peaks appeared at 195 ºC and 214 ºC for Cu-4MAP-α-CD and Cu-4MAP-β-CD respectively.
3.4.3 Infrared spectral studies
FTIR analysis shows the 4MAP:CD inclusion complexes in comparison to those for pure α-CD, β-CD and 4MAP. In 4MAP, the C-CH3 stretching frequency appears at 2840 cm-1. The aromatic C=O, and C-O-C stretching frequency appears at 1670 cm-1 and 1023 cm-1 respectively. In the Cu:4MAP:CD nanomaterials, the C-CH3 stretching frequency appears at 3284 cm-1 and 2923 cm-1 the aromatic C=O and C-O-C stretching frequency appears at 1636 cm-1 and 1020 cm-1 respectively. In Cu:4MAP:CD stretching frequency appears at 753 cm-1 respectively. Most of the frequency was not appeared and significant decrease in intensity was noted suggest that the 4MAP molecule interact with copper nano and CD
3.4.4 Proton Magnetic Resonance Spectral Studies
In order to comprehensively examine the structures of nano copper, 4MAP and the CD complexes were investigated by proton magnetic resonance spectra. 1H-NMR spectra of 4MAP and the inclusion complexes are performed at 25 °C in DMSO-d6. The chemical shift values given below: COCH3 proton appear at 2.55, OCH3 proton appear at 3.86, ortho hydrogen respected to COCH3 proton appear at 7.93, and meta hydrogen respected to COCH3 proton appear at 6.93. Generally, the chemical shift values of the guest protons tend to show appreciable changes if the guest molecules are included in the CDs cavities. All the protons shift to up field/ down field in the Cu:4MAP:CD nanomaterials indicate that all the protons of 4MAP are interacting with CD cavity protons. 
3.4.5  X-RD Spectral Studies
In order to comprehensively examine the structures of nano copper, 4MAP and the CD complexes were investigated by powder XRD. Based on JCPDS data, the mineral name (3C) and face-centered cubic (FCC) structure were identified. The standard FCC structure corresponds to JCPDS card number 87-0717, with hkl values at 111, 200, 220, and 311. The Cu nano shows three distinct diffraction peaks at 2θ = 43.58°, 51.64°, and 74.75°. 4MAP showed the following peaks at 2θ° = 18.2, 46.2, 77.6 and 116.4°, while several peaks were observed for Cu/4MAP/β-CD at 2θ° =  12.4, 19.4, 31.6, 35.1, 38.0, 44.0, 49.1, 64.2, 77.6, 11.6 and 116.2°. The XRD patterns of Cu/4MAP/β-CD exhibited distinct diffraction features, confirming the formation of new nanomaterials. The appearance of additional peaks and variations in intensities further support the formation of novel nanomaterials.
4. Conclusion
Absorption and emission spectral maxima of 4-methoxyacetophenone (4MAP) in different -CD and -CD concentrations with pH~3 and pH~7 solutions were analysed using UV-visible, fluorescence, time resolved fluorescence measurements and molecular modeling methods. Solid inclusion complex nanomaterials were prepared and characterized by SEM, DSC, FTIR, XRD and 1H NMR. The absorption and emission maxima of 4MAP with different -CD and -CD concentrations are same at pH~3 and pH~7 medium. Single emission maximum noticed in the solvents while dual emission (ICT) observed in the CD solutions. With increasing the CD concentrations, both emission intensities are increased at the same wavelength. In α-CD and β-CD with the pHs, similar absorption and fluorescence spectral shifts observed clearly establish that 4MAP molecule form identical type of the inclusion complexes. The life time of the 4MAP increased in the following order: water < α-CD < β-CD indicates that β-CD:4MAP has more stable than α-CD. PM3 calculations further supported the formation of the inclusion complexes. The powdered form of Cu nano, 4MAP, Cu:4MAP:α-CD and Cu:4MAP:-CD inclusion complexes were investigated by SEM, DSC, FTIR and 1H NMR. SEM picture clearly shows the morphological difference between copper nano, 2AS and the Cu nano inclusion complex. SEM pictures, DSC thermogram, FTIR, 1HNMR, XRD results supported that the formation of Cu-4MAP-α-CD and Cu-4MAP-β-CD nanomaterials. 
References
1. N. Rajendiran, R.K. Sankaranarayanan, J.Saravanan, Nanochain and vesicles formed by inclusion complexation of 4, 4’-diamino benzanilide with Cyclodextrins. J. Experimental Nanoscience, 10(2015)880-899. doi.org/10.1080/17458080.2014.930523 
2. N. Rajendiran, G. Venkatesh, Inclusion complexation of 4,4'-dihydroxy benzophenone and 4-hydroxy benzophenone with α- and β-CD. Supramolecular Chemistry, 26(2014) 783-795. doi.org/10.1080/10610278.2013.873125
3. M.Shanmugam, J.Thulasidhasan, G.Venkatesh, V. Chidambaranathan, N. Rajendiran, Effect of α- and β-cyclodextrins on three S-triazine derivates: Spectral and molecular modeling studies. Physics and Chemistry of Liquids, 52(2014) 583-600. doi.org/10.1080/00319104.2014.880437
4.  Spectrochimica Acta A, 74 (2009) 469–477, A.A. Smith, K.Kannan, R.Manavalan, N. Rajendiran* Spectral characteristics of tramadol drug in different solvents and β-CD.
5.  M.Jude Jenita, G.Venkatesh, J.Thulasidasan, N. Rajendiran, Excimer formation in inclusion complexes of antihypertensive drugs with HP-α- and HP-β-CDs. Indian J. Chemistry, 52A (2013) 207-216.
6.  N. Rajendiran, R.K. Sankaranarayanan, Nanorod formation of cyclodextrin covered sudan dyes through supramolecular self assembly. J. Experimental Nanoscience, 10 (2015) 407-428, doi. 10.1080/17458080.2013.840934
7. Polycyclic Aromatic Compounds, 42 (2022) 3563-3585, N. Rajendiran, A. Antony Muthu Prabhu, T. Mohandoss, J. Thulasidhasan, R. Baskaran, Spectral and theoretical investigation of inclusion complex between cinnamic acid and hydroxycinnamic acids with native cyclodextrins. DOI: 10.1080/10406638.2020.1869794.
8. RK. Sankaranarayanan, G.Venkatesh, Jayashree Ethiraj, M.Pattabiraman, K.Saravanakumar G.Arivazhagan, R.Shanmugam, N.Rajendiran, Stepwise pesudopolyrotaxane nanostructure formation from supramolecular self-assembly by inclusion complexation of fast violet B with α- and β-cyclodextrins. J.Molecular Structure 1262(2022)133080-89, doi. 10.1016/j.molstruc.2022.133080
9. Indian J. Chemistry, 52A (2013) 207-216, M.Jude Jenita, G.Venkatesh, V.K.Subramanian, N. Rajendiran*, Excimer formation in inclusion complexes of antihypertensive drugs with HP-α- and HP-β-CDs.
10. N. Rajendiran, T. Mohandoss, J. Thulasidhasan, Dual Fluorescence of 4,4′-sulfonyldiphenol, 3,3’–dimethyl 4,4′-sulfonyldiphenol, 4,4′-sulfonyldibenzoic acid: Effects of cyclodextrin complexation. Canadian Chemical Transactions, 3(2015) 319-332. Doi. 10.13179/canchemtrans.2015.03.03.0225
11.  A. Mani, P. Ramasamy, A. Antony Muthu Prabhu, N. Rajendiran, Investigation of Ag and Ag/Co bimetallic nanoparticles with naproxen-cyclodextrin inclusion complex. J. Molecular Structure, 1284 (2023) 135301-10. doi.org/10.1016/j.molstruc.2023.135301
12.  A. Mani, P. Ramasamy, A. Antony Muthu Prabhu, P. Senthilraja, N. Rajendiran, Synthesis and Analysis of Ag/Olanzapine/Cyclodextrin and Ag/Co/Olanzapine/Cyclodextrin Inclusion Complex Nanorods. Physics and Chemistry of Liquids, 62 (2024) 196-209. doi.org/10.1080/00319104.2023.2297223
13.  A. Mani, G. Venkatesh, P. Senthilraja, N. Rajendiran, Synthesis and Characterisation of Ag-Co-Venlafaxine-Cyclodextrin Nanorods, European J Advanced Chemistry Research, 5 (2024) 9-16. doi; 10.24018/ejchem.2024.5.1.147
14.  A.Mani, P.Ramasamy, A.Antony Muthu Prabhu, P.Senthilraja, N.Rajendiran, Synthesis and Characterisation of Ag/Co/Chloroquine/Cyclodextrin Inclusion Complex Nanomaterials. J Sol-Gel Science and Technology 115 (2025) 844-856. doi.org/10.1007/s10971-024-06620-5.
15  N. Rajendiran, A. Mani, M. Venkatesan, B. Sneha, E. Nivetha, P. Senthilraja, Spectral, Microscopic, Antibacterial and Anticancer Activity of Pyrimethamine drug with Ag nano, DNA, RNA, BSA, Dendrimer, and Cyclodextrins, J Solution Chem, In press. 
16.  P Ramasamy, A Mani, B Sneha, E Nivetha, M Venkatesan, N Rajendiran, Azo-hydrazo tautomerism in Sudan Red-B and Cyclodextrin/ Sudan Red-B doped ZnO nanomaterials. J Molecular Structure 1329 (2025) 141423-32. doi.org/10.1016/j.molstruc.2025.141423
17. G.Venkatesh, T.Sivasankar, M.Karthick, N.Rajendiran, Inclusion complexes of sulphanilamide drugs and β-CD: A theoretical approach. J.Inclusion Phenomena and Macrocyclic Chemistry, 77 (2013) 309-318, doi. 10.1007/s10847-012-0248-z
18. J. Prema Kumari, A. Antony Muthu Prabhu, G. Venkatesh, V.K. Subramanian, N.Rajendiran, Effect of solvents and pH on β-CD Inclusion complexation of 2,4-dihydroxy azobenzene and 4-hydroxy azobenzene. J. Solution Chemistry, 40 (2011) 327–347. doi.org/10.1007/s10953-010-9639-1
19. T.Stalin, P. Vasantharani, B.Shanthi, A.Sekar, N.Rajendiran, Inclusion complex of 1,2,3-trihydroxybenzene with α- and β-cyclodextrins. Indian J Chemistry, 45A (2006) 1113–1120.
20. J.Prema Kumari, A. Antony Muthu Prabhu, G.Venkatesh, V.K.Subramanian, N. Rajendiran, Spectral characteristics of sulfadiazine, sulfisomidine: Effect of solvents, pH and β-CD. Physics and Chemistry of Liquids, 49(2011)108–132. doi.org/10.1080/00319104. 2010.509724
21. R.K.Sankaranarayanan, S.Siva, A. Antony Muthu Prabhu, N.Rajendiran, A study on the inclusion complexation of 3,4,5-trihydroxybenzoic acid with β-CD at different pH. J.Inclusion Phenomena and Macrocyclic Chemistry, 67 (2010) 461-470. doi.org/10.1007/s10847-009-9729-0
22.  N. Rajendiran, S. Siva, J. Saravanan, Inclusion complexation of sulfa pyridine with α- and β-CDs: Spectral and molecular modeling study. J. Molecular Structure,1054-1055 (2013) 215–222. doi.org/10.1016/j.molstruc.2013.09.035  
23. N. Rajendiran, R.K. Sankaranarayanan, Azo dye/Cyclodextrin: New findings of identical nanorods through 2:2 inclusion complexes. Carbohydrate Polymers, 106 (2014) 422-431. doi.org/10.1016/j.carbpol.2014.01.030
24.  N. Rajendiran, R.K. Sankaranarayanan, J.Saravanan, A study of supramolecular host–guest interaction of dothiepin and doxepin drugs with cyclodextrin macrocycles. J Molecular Structure, 1067(2014) 252-260. doi.org/10.1016/j.molstruc.2014.03.051
25. A. Antony Muthu Prabhu, N.Rajendiran, Encapsulation of labetalol, and pseudoephedrine in β-CD cavity: Spectral and molecular modeling studies. J. Fluorescence, 22(2012)1461-1474. doi.org/10.1007/s10895-012-1083-8
26. M.Jude Jenita, A.Antony Muthu Prabhu, N.Rajendiran, Theoretical study of inclusion complexation of tricyclic antidepressant drugs with β-CD. Indian J. Chemistry A, 51A (2012) 1686-1694.
27. N. Rajendiran, G. Venkatesh, J.Saravanan, Supramolecular aggregates formed by sulfadiazine and sulfisomidine inclusion complexes with α- and β-cyclodextrin. Spectrochimica Acta, 129A (2014) 157-162, https://doi.org/10.1016/j.saa.2014.03.028
28.  N. Rajendiran, G. Venkatesh, T.Mohandoss, Fabrication of 2D nano sheet through self assembly behavior of sulfamethoxy pyridazine inclusion complex with α- and β-cyclodextrins. Spectrochim Acta A,123A (2014) 158-166, doi.org/10.1016/j.saa.2013.12.053
29. S.Siva, R.K.Sankaranarayanan, A.Antony Muthu Prabhu, N.Rajendiran, Inclusion complexation of 3,5-dihydroxy benzoic acid with β-CD at different pH. Indian J. Chemistry, 48A (2009)1515–1521,
30.  A.Antony Muthu Prabhu, G.Venkatesh, N.Rajendiran, Azo-Hydrazo tautomerism in 1-phenyazo-2-naphthol dyes in various solvents, pH and β-CD. J. Fluorescence, 20 (2010) 961–972. Doi. 10.1007/s10895-010-0642-0

