Ag-Fe Nanoparticles Phytosynthesized by Mangifera Indica Leaf Extract:  Characterization and Biomedical Applications

### Abstract

Silver nanoparticles have demonstrated extensive biomedical applications; however, the synergistic combination of silver and iron using Mangifera indica leaf extract remains underexplored. This study focuses on the green synthesis, characterization, and biomedical evaluation (antibacterial and antioxidant activities) of silver–iron (Ag–Fe) bimetallic nanoparticles using M. indica leaf extract. The nanoparticles were synthesized via a phytosynthetic approach and characterized using UV–Visible spectroscopy, Fourier Transform Infrared (FTIR) spectroscopy, Scanning Electron Microscopy (SEM), and Energy Dispersive X-ray (EDX) analysis. Antibacterial activity was assessed using the agar well diffusion method, while antioxidant potential was evaluated using DPPH and ABTS assays. The UV–Vis spectra exhibited a distinct surface plasmon resonance peak at 445 nm, confirming nanoparticle formation. FTIR analysis revealed functional groups such as hydroxyl, carbonyl, and carboxylic groups, which played roles in reduction and stabilization. SEM images showed irregular, moderately aggregated nanoparticles, while EDX confirmed the presence of Ag and Fe. The Ag–Fe nanoparticles demonstrated significant antibacterial activity, with the highest inhibition observed against Pseudomonas aeruginosa (17.16 ± 0.76 mm), followed by Salmonella typhi, Escherichia coli, and Klebsiella pneumoniae. Antioxidant assays revealed dose-dependent radical scavenging activity. In the ABTS assay, the nanoparticles exhibited strong activity at low concentrations with an IC₅₀ of 1.42 µg/mL, while the DPPH IC₅₀ was 46.48 µg/mL compared to 26.91 µg/mL for ascorbic acid. Overall, the synthesized Ag–Fe bimetallic nanoparticles demonstrated promising antibacterial and antioxidant properties, attributable to the synergistic effects of silver and iron and the stabilizing influence of phytochemicals from M. indica. These findings suggest their potential application as antimicrobial and antioxidant agents in biomedical fields.

Key words: Green Synthesis, Bimetallic Nanoparticles, Mangifera indica, Antibacterial activity and Antioxidant activity

- Introduction

Nanotechnology has emerged as a rapidly advancing field with applications spanning medicine, agriculture, environmental remediation, electronics, renewable energy, and food safety (Bayda et al., 2019). Among nanomaterials, metal-based nanoparticles have attracted significant attention due to their unique physicochemical properties, including enhanced optical, electrical, catalytic, and magnetic characteristics (Arsenov et al., 2023).

Silver (Ag) nanoparticles are among the most extensively studied due to their potent antimicrobial, antifungal, and antiviral activities, as well as their applications in biosensing, wound healing, food preservation, and water purification systems (Shaikh et al., 2022). Conversely, iron (Fe) nanoparticles exhibit distinctive magnetic properties, redox activity, and catalytic efficiency, making them valuable in environmental remediation, magnetic resonance imaging (MRI), and wastewater treatment (El-Saadony et al., 2023).

Bimetallic nanoparticles, composed of two different metals, can exist as alloys, core–shell structures, or heterostructures. These systems often exhibit enhanced physicochemical properties, including improved stability, catalytic activity, and biological functionality, compared to monometallic nanoparticles (Padilla-Cruz et al., 2021). In particular, Ag–Fe bimetallic nanoparticles combine the broad-spectrum antimicrobial properties of silver with the magnetic and catalytic capabilities of iron, making them promising candidates for biomedical and environmental applications (Thangapushpam et al., 2024).

Plant-mediated (green) synthesis of nanoparticles has gained increasing interest due to its eco-friendliness, cost-effectiveness, and avoidance of toxic chemicals. Mangifera indica (mango) leaves, an abundant agro-waste material, are rich in bioactive compounds such as mangiferin, quercetin, gallic acid, and flavonoids. These phytochemicals serve as natural reducing and stabilizing agents and possess intrinsic antioxidant and antimicrobial properties (Al-Karagoly et al., 2023).

Despite extensive studies on monometallic nanoparticles, there is limited research on the green synthesis of Ag–Fe bimetallic nanoparticles using plant extracts. Moreover, bimetallic systems synthesized via green routes often exhibit enhanced biological activities due to synergistic interactions between the constituent metals.

Therefore, this study aims to synthesize Ag–Fe bimetallic nanoparticles using M. indica leaf extract, characterize their physicochemical properties, and evaluate their antibacterial and antioxidant potentials.

# Materials and Methodology

# 2.1	Plant Material

Fresh Mangifera indica leaves were collected from the environment of Mewar International University, Nigeria. The leaves were thoroughly washed with distilled water to remove all surface contaminants. After rinsing, the leaves were air-dried at room temperature and subsequently oven-dried at 60°C. The dried leaves were grounded into a fine powder using a mechanical grinder and stored in airtight containers.

# 2.2	Preparation of Leaf Extract

Crude extraction was prepared following the method described by Ibrahim (2015). Specifically, 10 grams of the powdered mango leaf was mixed with 90 milliliters of distilled water. The mixture was heated at 80°C for 60 minutes with continuous stirring. After cooling to room temperature, the extract was filtered using Whatman No. 1 filter paper, which was used as the reducing agent in nanoparticle synthesis.

# 2.3	Synthesis of Silver–Iron (Ag–Fe) Bimetallic Nanoparticles

The synthesis of silver–iron (Ag–Fe) bimetallic nanoparticles was carried out using the aqueous M. indica leaf extract (MLE) prepared. The green synthesis procedure was adapted from the method described by Amatya et al. (2021), with slight modifications. 10 mL of freshly prepared mango leaf extract was added to a mixture containing 10 mL of 1 mM silver nitrate (AgNO₃) solution and 10 mL of 0.1 M iron (II) sulphate (FeSO4) solution. The mixture was combined in a 1:1:1 volume ratio (v/v/v) in a conical flask. The reaction mixture was continuously stirred on a magnetic stirrer at 60°C for 30 minutes to facilitate reduction and nanoparticle formation. The formation of Ag–Fe bimetallic nanoparticles was visually confirmed by a gradual color change in the solution, indicating the successful reduction of metal ions. The synthesized nanoparticles were subsequently harvested by centrifugation at 10,000 rpm for 15 minutes. The pellet was washed three times with distilled water to remove unreacted precursors and phytochemical residues. Finally, the nanoparticles were oven-dried at 60°C and stored in airtight containers for further characterization.

### 2.4	Characterization of Synthesized Nanoparticles

To confirm the successful synthesis and to evaluate the physical and chemical properties of the silver-iron (Ag-Fe) bimetallic nanoparticles, the sample was subjected to a set of characterization techniques. These include UV–Visible Spectroscopy (UV-Vis), Fourier Transform Infrared Spectroscopy (FTIR), Scanning Electron Microscopy - Energy Dispersive X-Ray (SEM – EDX) and Dynamic Light Scattering (DLS) for particle size determination (Malvern- size distribution equipment). UV–Visible Spectroscopy was used to investigate the optical properties and surface plasmon resonance (SPR) of the synthesized nanoparticles. The analysis was carried out using a double-beam UV–Vis spectrophotometer within a wavelength range of 200–800 nm.  FTIR Spectroscopy was performed using a SHIMADZU FTIR-8400S spectrophotometer to identify the functional groups involved in the reduction of the bimetallic nanoparticles. The FTIR spectra, were recorded in the range of 4000–400 cm⁻¹, and analyzed to detect peaks that corresponds to hydroxyl, carbonyl, and other phytochemical-related functional groups (Darwich et al., 2024). Scanning Electron Microscopy (SEM) and Energy Dispersive X-Ray (EDX) was used to confirm the morphology and elemental composition of the synthesized nanoparticles (JEOL JCM-6000PLUS coupled with an EX-54450U1S61 detector, OH-USA) on various regions of the samples at 10 keV (Temesgen et al., 2024).

2.4	Antibacterial Activity

The method of Mezher et al. (2022) was adopted to assess the antibacterial activity of the synthesized Ag-Fe nanoparticles using the agar well diffusion method. Clinical isolates bacterial suspensions namely; Escherichia coli, Klebsiella pneumoniae, Salmonella typhi and Pseudomonas aeruginosa were standardized to 0.5 McFarland turbidity and swabbed uniformly on the surface of nutrient agar plates. A cork borer of 6mm diameter was used to make wells on the agar plates and 100 µL of Ag-Fe nanoparticle was added into separate wells. Gentamicin (10 µg/mL) was used as the positive control, while distilled water as the negative control. The plates were incubated at 37°C for 24 hours, after which the zones of inhibition were measured in millimeters. The tests were conducted in triplicate.

2.5	Minimum Inhibitory Concentration (MIC) and Minimum Bactericidal Concentration (MBC)

The Minimum Inhibitory Concentration (MIC) was determined using the microbroth dilution method in 96-well microtitre plates. Serial two-fold dilutions of the Ag-Fe nanoparticles was prepared in nutrient broth to obtain final concentrations of 6.25 µg/mL, 12.5 µg/mL, 25 µg/mL, 50 µg/mL, and 100 µg/mL. Each well was inoculated with 100µL of the standardized bacterial suspension. The microplates were incubated at 37°C for 24 hours, and bacteria growth was assessed visually. The MIC was recorded as the least concentration of Ag-Fe nanoparticles that inhibited visible microbial growth, indicating bacteriostatic activity (Temesgen et al., 2024). Escárcega-González et al. (2018) method was used to determine the Minimum Bactericidal Concentration (MBC), 10µL aliquots from wells showing no visible growth in the MIC assay was plated onto freshly prepared nutrient agar plates. These plates were incubated at 37°C for 24 hours.

2.6	1, 1- diphenyl-2-picryl hydrazyl (DPPH) Radical Scavenging Assay

The DPPH assay was carried out to evaluate the free radical scavenging activity of the synthesized Ag-Fe nanoparticles at different concentrations. 0.1 mM. DPPH solution was freshly prepared in methanol. In each reaction tube, 1 mL of DPPH solution was mixed with 1 mL of the nanoparticle sample at the designated concentration. The mixture was incubated in the dark at room temperature for 30 minutes. After incubation, the absorbance of the mixture was measured at 517 nm using a UV–Vis spectrophotometer. Ascorbic acid, at equivalent concentrations, was used as standard antioxidant (Donga and Chanda, 2021).

2.7	2,2′-azino-bis (3-ethylbenzothiazoline-6-sulfonic acid (ABTS) Radical Scavenging Assay

The ABTS radical scavenging activity of the Ag-Fe nanoparticles was assessed using already prepared ABTS radical cation solution. The ABTS⁺ solution was generated by mixing 7 mM ABTS stock with 2.45 mM potassium persulfate and the reaction mixture was allowed to stand in the dark at room temperature for 12–16 hours. Before use, the ABTS⁺ solution was diluted with methanol to an absorbance of 0.70 ± 0.02 at 734 nm. To test antioxidant activity, 1 mL of diluted ABTS⁺ solution was mixed with 1 mL of Ag-Fe nanoparticle samples at varying concentrations. The reaction mixtures were incubated in the dark for 10 minutes, and absorbance was measured at 734 nm. Ascorbic acid was used as a positive control. The percentage inhibition was calculated using the results from both assays were used to determine the concentration-dependent antioxidant potential of the Ag-Fe nanoparticles.

The percentage inhibition of DPPH or ABTS radicals was calculated using the formula:

Inhibition %=A0-A1A0×100

where A0​ is the absorbance of the control (DPPH or ABTS solution without sample), and A1 is the absorbance of the test sample (Donga and Chanda, 2021).

2.8	Data Analysis

The Statistical Package for Social Sciences (SPSS) version 27 software was utilized to identify differences between the groups using one-way analysis of variance (ANOVA), Tukey's test, and unpaired T-tests (p<0.05).

3.0	Results and Discussion

# 3.1 UV–Vis Spectroscopy of Synthesized Bimetallic Ag–Fe Nanoparticles

The UV–Vis absorption spectra of the synthesized Ag–Fe nanoparticles using M. indica leaf extracts revealed characteristic surface plasmon resonance (SPR) peaks within the visible region. It showed prominent absorption bands between 410 nm - 475 nm, which confirms the successful formation of silver-based nanoparticles. The SPR peak is a sigmoid optical property of metallic nanoparticles and indicates the collective oscillation of conduction electrons upon interaction with light. Ag–Fe colloid showed a distinct SPR peak around 445 nm, which is indicative of Ag0 nanoparticles and corresponds to the brownish colloid color. This collaborates with the study of Kamli et al. (2021) who synthesized Fe and Ag from Beta vulgaris and reported the usual Ag SPR at 450 nm, suggesting a strong interaction or possible core–shell structure.

Figure 1. UV–Vis Spectroscopy of Synthesized Bimetallic Ag–Fe Nanoparticles

3.2	FTIR Spectroscopy of Ag-Fe Nps

Table 1 and Figure 2 depicted the FTIR spectrum of the synthesized Ag–Fe nanoparticles which showed several absorption bands that confirm the presence of bioactive phytochemicals from mango leaf extract acting as natural reducing and stabilizing agents. Peaks around 3279.5 cm⁻¹ and 1109.9 cm⁻¹ confirm the presence of hydroxyl and ether groups, likely from polyphenols and flavonoids. The band at 1650.9 cm⁻¹ suggests carbonyl or aromatic C=C stretching, common in plant secondary metabolites. The band at 2504.2 cm⁻¹ further supports the presence of carboxylic acids, which may coordinate with Ag⁺ and Fe²⁺ ions. These spectral features indicate that M. indica leaf extract facilitated the reduction of metal ions and also provided functional groups for stabilizing the synthesized Ag–Fe nanoparticles. Kolya and Kang (2022), observed similar peaks in their study with a C–O stretch around 1016 cm−1 for green-synthesized Ag/Fe NPs, attributing it to C–O and O–H vibrations of residual phytochemicals. This suggest that these phytochemicals are strongly adsorbed on the Ag–Fe nanoparticle surface, acting as reducing agents during synthesis and as capping/stabilizing agents after formation.

Figure 2. FTIR Spectroscopy of Ag-Fe Nps

Table 1. FTIR spectroscopy of Ag-Fe NPs M. indica leaf extract

| Wave number (cm⁻¹) | Bond | Functional Group |
| --- | --- | --- |
| 3759.2 | O–H stretch (free) | Free hydroxyl groups (alcohols or phenols) |
| 3279.5 | O–H stretch (H-bonded) | H-bonded alcohols or phenols |
| 2755.2 | H–C=O stretch | Aldehydes |
| 2504.2 | O–H stretch (carboxylic acid) | Carboxylic acids |
| 2258.8 | C≡N or C≡C stretch | Nitriles or alkynes |
| 2069.2 | Weak C≡C or CO stretching | Possibly alkynes or metal-carbonyl interactions |
| 1650.9 | C=O stretch / N–H bend | Amides, carbonyls (ketones, esters), or aromatic C=C |
| 1109.9 | C–O stretch | Alcohols, ethers, esters |

### 3.3	Scanning Electron Microscopy – Energy Dispersive X-ray Spectroscopy

### Figure 3 and Table 2 showed the SEM micrograph of Ag/Fe nanoparticles synthesized using M. indica leaf extract at a magnification of x1500. The image reveals a dense distribution of star-like crystalline nanostructures, indicating uniform synthesis and dispersion across the substrate surface. These structures suggest well-formed nanoparticle agglomerates with distinct morphology, likely influenced by the phytochemical constituents of the M. indica leaf extract. The EDX Spectrum displayed a vast array of elemental composition of the synthesized Ag/Fe Nanoparticles. with an atomic concentration of Ag (0.05%), Fe (3.55%) and a weight concentration of Ag (0.09%) Fe (11.55%) respectively and average size of Z-Average: 55.92 nm. Zulfikar et al. (2021), reported similar spherical shape which was in the range of 200–400nm. Padilla-Cruz et al. (2021), also obtained ~13 nm core–shell Ag–Fe particles that showed homogeneous spherical shapes clustering together.

Figure 3. The EDX spectrum and SEM micrograph of Ag-Fe NPs (x 1500)

Table 2. Elemental composition of Ag-Fe Nanoparticles

| Element Number | Element Symbol | Element Name | Atomic Conc. | Weight Conc. |
| --- | --- | --- | --- | --- |
| 6 | C | Carbon | 66.96 | 46.91 |
| 7 | N | Nitrogen | 15.96 | 13.04 |
| 26 | Fe | Iron | 3.55 | 11.55 |
| 16 | S | Sulfur | 3.83 | 7.17 |
| 17 | Cl | Chlorine | 2.64 | 5.46 |
| 19 | K | Potassium | 2.00 | 4.57 |
| 30 | Zn | Zinc | 1.05 | 3.99 |
| 11 | Na | Sodium | 1.73 | 2.31 |
| 13 | Al | Aluminium | 0.78 | 1.23 |
| 50 | Sn | Tin | 0.14 | 0.97 |
| 29 | Cu | Copper | 0.18 | 0.66 |
| 14 | Si | Silicon | 0.37 | 0.61 |
| 20 | Ca | Calcium | 0.24 | 0.57 |
| 12 | Mg | Magnesium | 0.36 | 0.52 |
| 15 | P | Phosphorus | 0.16 | 0.28 |
| 25 | Mn | Manganese | 0.05 | 0.17 |
| 47 | Ag | Silver | 0.05 | 0.09 |
| 22 | Ti | Titanium | 0.00 | 0.00 |

Figure 4. Ag/Fe NPs – Mangifera indica Dynamic light scattering (DLS)

3.4	Antibacterial activity of Ag-Fe NPs synthesized

The biosynthesized Ag–Fe nanoparticles were evaluated for their antibacterial efficacy against four pathogenic bacteria: Escherichia coli, Salmonella typhi, Pseudomonas aeruginosa, and Klebsiella pneumoniae. These organisms are all Gram-negative bacteria associated with serious infections (including diarrheal disease, typhoid fever, nosocomial pneumonia, etc.), and notably, many strains are multidrug-resistant. The Ag–Fe BNPs demonstrated significant antibacterial activity in disk diffusion assays, as evidenced by clear inhibition zones.

In this study, the Ag–Fe NPs produced measurable zones of inhibition against all tested bacteria, indicating a broad-spectrum antibacterial effect. The result confirmed that the green-synthesized Ag–Fe NPs possess broad-spectrum antibacterial activity, with the strongest effect against P. aeruginosa as depicted in Table 3. Our findings align with zones of inhibition reported by Deljou and Goudarzi (2016), they observed biosynthesized AgNPs that yielded 22 mm zone against E. coli and 19 mm against S. typhi under similar concentrations. Lateef et al. (2016) observed complete growth inhibition of E. coli and K. pneumoniae when they used 40 µg/mL of AgNPs synthesized from cocoa pod extract, highlighting how effective biogenic Ag-containing NPs can be even against drug-resistant strains. Donga and Chanda (2021) also reported similar zones of inhibition against gram positive and negative clinical isolates. Notably, some studies reported extremely large inhibition zones with biogenic AgNPs. Hamouda and Aljohani (2024), achieved zones up to 38 mm against E. coli, P. aeruginosa, and K. pneumoniae using seaweed-derived AgNPs at high concentration outperforming even standard antibiotics in that comparison. Ag–Fe NPs showed inhibition in this range, indicating a strong antibacterial activity.

Table 3 Zones of Inhibition of Ag–Fe NPs on Bacteria Isolates

| Sample | E. coli | S. typhi | P. aeruginosa | K. pneumoniae |
| --- | --- | --- | --- | --- |
| Ag–Fe NPs | 12.93 ± 0.40 | 14.90 ± 0.31 | 17.16 ± 0.76 | 12.27 ± 0.46 |
| Positive Control (PC) (gentamycin) | 27.50 ± 0.50 | 27.17 ± 0.76 | 27.33 ± 0.58 | 29.30 ± 0.30 |
| Negative Control (NC) | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 |

Values are presented as Mean ± SD, n = 3

Figure 5 Antibacterial activity of Ag-Fe NPs

3.5	Antioxidant Activities of Ag–Fe bimetallic nanoparticles

The antioxidant potential of the Ag–Fe bimetallic nanoparticles was assessed using two complementary free radical scavenging assays: DPPH (1,1-diphenyl-2-picrylhydrazyl) and ABTS (2,2′-azino-bis(3-ethylbenzothiazoline-6-sulfonate)) radical scavenging.  The two assays both showed concentration-dependent radical scavenging effects. These assays measure the ability of the nanoparticles (and their capping phytochemicals) to quench stable free radicals by electron or hydrogen donation, thus indicating potential antioxidant activity. In our study, the Ag–Fe NPs demonstrated dose-dependent scavenging in both DPPH and ABTS assays, with a notable difference in efficacy between the two methods as shown in Table 4 and 5. The radical scavenging for DPPH increasing from 23.62% at 6.25 µg/mL to 69.17% at 100 µg/mL and ABTS radical scavenging activity reaching 82.29% inhibition at 100 µg/mL. In the DPPH assay, the IC₅₀ value of 46.48 µg/mL indicates moderate antioxidant activity compared to ascorbic acid. In contrast, the ABTS assay showed a much lower IC₅₀ value (1.42 µg/mL), indicating stronger activity in this system.

Table 4. DPPH Radical Scavenging Activity of Ag–Fe Nanoparticles and Ascorbic Acid

| Concentration (µg/mL) | % Inhibition Ag-Fe NPs | % Inhibition Ascorbic Acid |
| --- | --- | --- |
| 6.25 | 23.62 ± 1.12 | 15.58 ± 0.61 |
| 12.5 | 30.64 ± 0.13 | 39.83 ± 0.67 |
| 25 | 47.78 ± 0.09 | 59.06 ± 0.11 |
| 50 | 60.88 ± 0.05 | 69.26 ± 0.20 |
| 100 | 69.17 ± 0.17 | 78.34 ± 0.06 |

Values are presented as Mean ± SD, n = 3

Table 5. ABTS Radical Scavenging Activity of Ag–Fe Nanoparticles and Ascorbic Acid

| Concentration (µg/ml) | % Inhibition Ag-Fe NPs | % Inhibition Ascorbic acid |
| --- | --- | --- |
| 20 | 37.63 ± 0.62 | 50.46 ± 0.72 |
| 40 | 60.06 ± 0.78 | 51.74 ± 0.96 |
| 60 | 76.26 ± 0.10 | 54.08 ± 0.87 |
| 80 | 81.47 ± 0.08 | 54.97 ± 0.57 |
| 100 | 82.29 ± 0.06 | 55.21 ± 0.25 |

Values are presented as Mean ± SD, n = 3

Table 6. IC50 values of Ag–Fe Nanoparticles and Ascorbic Acid

| Antioxidants | Samples | Linear IC50 (µg/mL) |
| --- | --- | --- |
| DPPH | Ag-Fe NPs | 46.48 |
|  | Ascorbic Acid | 26.91 |
| ABTS | Ag-Fe NPs | 1.42 |
|  | Ascorbic Acid | 0.42 |

This suggested that the nanoparticles were more efficient at quenching DPPH free radicals than ABTS⁺ radicals. Das et al. (2022) reported that green-synthesized AgNPs using a Korean root extract had DPPH IC₅₀ of 56.3 µg/mL, whereas their ABTS IC₅₀ was much higher (171.4 µg/mL). Bardania et al. (2020), reported similar trend of dose dependent antioxidant activity of biogenic Ag NPs. This variation between assays may be attributed to differences in radical structure, solubility, and interaction mechanisms. The enhanced antioxidant activity is likely due to the presence of phytochemical capping agents capable of donating electrons or hydrogen atoms to neutralize free radicals. Donga and Chanda (2021), suggested green synthesized Ag NPs to serve as a good source of natural antioxidants which can be utilized to treat diseases and disorders especially those related with stress and caused by excessive production of ROS since they demonstrated it prominent antioxidant potential in various antioxidant assays.

- Conclusion

Silver–iron (Ag–Fe) bimetallic nanoparticles were successfully synthesized using Mangifera indica leaf extract via a green synthesis approach. Characterization techniques confirmed nanoparticle formation, with UV–Vis spectroscopy revealing a distinct SPR peak at 445 nm, FTIR identifying functional groups responsible for reduction and stabilization, and SEM–EDX confirming morphology and elemental composition. The synthesized nanoparticles exhibited significant antibacterial activity against E. coli, S. typhi, P. aeruginosa, and K. pneumoniae, as well as notable antioxidant activity in both DPPH and ABTS assays. These biological activities are attributed to the synergistic effects of silver and iron, along with the bioactive phytochemicals from the plant extract. The findings highlight the potential of M. indica-mediated Ag–Fe nanoparticles as multifunctional agents in biomedical applications. However, further studies, including in vivo toxicity and biocompatibility are recommended to fully establish their safety and therapeutic efficacy.

## Disclaimer (Artificial intelligence)

## Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

Al-Karagoly, H., Jaber, S., & Jawad, H. (2023). Silver nanoparticles synthesized from flaxseed extract: Antioxidant and antimicrobial evaluation. Applied Nanoscience, 13(1), 1–4.

Amatya S. P., Shrestha, S. & Aryal Y. (2021). Green Approach for Synthesis of Manganese Nanoparticle using Banana Peel (Musa paradiasca) and its Characterization. Amrit Research Journal, 2(01), 75-82.

Arsenov, D., Chaykina, D., Klimenko, S., & Savostyanov, V. (2023). Environmental impact of nanoparticle synthesis: A comparative review of chemical and green routes. Journal of Cleaner Production, 406, 137057.

Bardania H, Mahmoudi R, Bagheri H. (2020). Facile preparation of a novel biogenic silver-loaded nanofilm with intrinsic anti-bacterial and oxidant scavenging activities for wound healing. Sci Rep. 2020;10(1):1–4.

Bayda, S., Adeel, M., Tuccinardi, T., Cordani, M., & Rizzolio, F. (2019). The history of nanoscience and nanotechnology: From chemical–physical applications to nanomedicine. Molecules, 25(1), 112.

Deljou, A. & Goudarzi, S. (2016).  Green Extra cellular synthesis of AgNPs using Thermophilic Bacillus sp. AZ1 and its Antimicrobial Activity Against Several Human Pathogen Bacteria, Iran Journal of Biotechnology, 14(2): 25-32 doi: 10.15171/ijb.1259

El-Saadony, M. T., Saad, A. M., Desoky, E. S. M., & Shafi, M. E. (2023). Eco-friendly synthesis of iron nanoparticles and their application in environmental and biomedical sectors. Environmental Science and Pollution Research, 30(5), 12345–12360.

Escárcega-González Carlos Enrique, JA Garza-Cervantes, A Vázquez-Rodríguez, Liliana Zulem Montelongo-Peralta, MT Treviño-González, E Díaz Barriga Castro, EM Saucedo Salazar, RM Chávez Morales, DI Regalado Soto, FM Treviño González, JL Carrazco Rosales, Rocío Villalobos Cruz & José Rubén Morones-Ramírez (2018). In vivo antimicrobial activity of silver nanoparticles produced via a green chemistry synthesis using Acacia rigidula as a reducing and capping agent, International Journal of Nanomedicine, 13 2349–2363. https://www.dovepress.com

Hamouda, R.A. & Aljohani, E.S. (2024). Assessment of Silver Nanoparticles Derived from Brown Algae Sargassum vulgare: Insight into Antioxidants, Anticancer, Antibacterial and Hepatoprotective Effect. Mar. Drugs 2024, 22, 154. https://doi.org/ 10.3390/md22040154

Ibrahim, H. M. M. (2015). Green synthesis and characterization of silver nanoparticles using banana peel extract and their antimicrobial activity against representative microorganisms. Journal of Radiation Research and Applied Sciences, 8(3), 265–275.

Kamli, M.R., Srivastava, V., Hajrah, N.H., Sabir, J.S.M., Ali, A., Malik, M.A. & Ahmad, A. (2021). Phytogenic Fabrication of Ag–Fe Bimetallic Nanoparticles for Cell Cycle Arrest and Apoptosis Signaling Pathways in Candida auris by Generating Oxidative Stress. Antioxidants 2021, 10, 182. https://doi.org/10.3390/ antiox10020182

Kolya, H. & Kang, C.W. (2022). Biogenic Synthesis of Silver-Iron Oxide Nanoparticles Using Kulekhara Leaves Extract for Removing Crystal Violet and Malachite Green Dyes from Water. Sustainability 2022, 14, 15800. https://doi.org/10.3390/ su142315800

Lateef Agbaje, Musibau A. Azeez, Tesleem B. Asafa, Taofeek A. Yekeen, Akeem Akinboro, Iyabo C. Oladipo, Luqmon Azeez, Sunday A. Ojo, Evariste B. Gueguim-Kana and Lorika S. Beukes (2016). Cocoa pod husk extract-mediated biosynthesis of silver nanoparticles: its antimicrobial, antioxidant and larvicidal activities, Journal Nanostructure Chemistry (2016) 6:159–169 DOI 10.1007/s40097-016-0191-4

Mezher, M., Hajj, R.E. & Khalil, M. (2022). Investigating the antimicrobial activity of essential oils against pathogens isolated from sewage sludge of southern Lebanese villages. GERMS, 12, 488–506.

Padilla-Cruz, A. L., Fuentes-Maldonado, L. E., & Martínez-Castañón, G. A. (2021). Green synthesis and antibacterial activity of Ag–Fe bimetallic nanoparticles using Gardenia jasminoides extract. Materials Science and Engineering: C, 123, 112005.

Ratan Das, Prahlad Deb, Himanshu Pande, Perugu Shyam & Devendra Singh (2022). Botanical synthesis of silver nanoparticles (AgNPs) and its antifungal effect against Alternaria porri causing purple blotch of onion: An in vitro and natural epiphytic study, Journal of Agriculture and Food Research, 10 (2022) 100390.

Savan Donga & Sumitra Chanda (2021). Facile green synthesis of silver nanoparticles using Mangifera indica seed aqueous extract and its antimicrobial, antioxidant and cytotoxic potential (3-in-1 system), Artificial Cells, Nanomedicine, and Biotechnology, 49:1, 292-302, DOI: 10.1080/21691401.2021.1899193

Shaikh, A. A., Bhosale, D. M., & Pawar, K. D. (2022). Synthesis of silver nanoparticles using mango (Mangifera indica) leaf extract and evaluation of their antimicrobial potential. Journal of Drug Delivery and Therapeutics, 12(5), 210–217.

Temesgen Achamo Orshiso, Enyew Amare Zereffa, Ananda Murthy H. C., Taye B. Demissie Suresh Ghotekar, Khanderao Pagar & Onkar Pardeshi (2024). One-Pot Biopreparation of Trimetallic ZnO–MgO–CuO Nanoparticles: Enhanced Cytotoxicity, Antibacterial Activities and Molecular Docking, Chemistry Africa, 7:1963–1980 https://doi.org/10.1007/s42250-023-00830-0

Thangapushpam, R., Krishnaveni, A., & Latha, S. (2024). Antioxidant potential of biosynthesized manganese dioxide nanoparticles using Azadirachta indica. Materials Letters, 354, 79–87.

Zulfikar Mona, Nadeem Raziya, Javed Tariq, Jilani Muhammad Idrees and Javed Iram (2021). Green synthesis of Fe nanoparticles by using Mangifera Indica extract and its application in photocatalytic degradation of dyes, Water Science and Technology, doi: 10.2166/wst.2021.074