Corrosion Inhibition of Mild Steel in Acidic Media using Caladium Tricolor Starch Extract: An Eco-Friendly Approach

Abstract

Caladium tricolor tuber starch (CTS) was extracted and used as corrosion inhibitor for mild steel in 0.5M HCl and 0.5M H2SO4 acid media respectively at various concentrations using the gravimetric technique. Results obtained shows that inhibition efficiency of the CTS inhibitor varied with time and concentration. Inhibition efficiency of caladium tricolor starch obtained ranged from 60% - 95% at 0.3g – 0.9g concentration in both acidic media. Maximum efficiency was obtained at concentration of 0.9g at 48 hours in 0.5M H2SO4. The highest inhibition efficiency obtained in HCl media was 90.03% at 0.9g/L concentration after 24 hours while 95.40% was obtained in H2SO4 media at 0.9 g/L after 48 hours, indicating CTS performed better in H2SO4 than in HCl. The mode of adsorption of the caladium tricolor starch followed the Langmuir isotherm exhibiting a Gibbs free energy value of −15.246KJ/mol, which indicates strong adsorption of the caladium tricolor starch molecules on the mild steel substrate.

Key Words: Starch, Biopolymer, Corrosion, Inhibition, Caladium Tricolor

Introduction

Mild steel, a widely used construction material in industries such as manufacturing, oil and gas, and construction, faces significant corrosion risks in acidic environments. Acidic media like hydrochloric acid (HCl) and sulfuric acid (H2SO4) are commonly encountered in processes like pickling, descaling, and oil well acidization, leading to aggressive corrosion of mild steel infrastructure [Aslam et al. 2022]. Corrosion not only damages equipment and structures but also escalates maintenance costs, downtime, and safety risks. The global cost of corrosion is estimated in trillions annually, highlighting the need for effective mitigation strategies.

Synthetic corrosion inhibitors are widely used to protect metals in acidic media. These chemicals often work by adsorbing onto metal surfaces, forming protective barriers against corrosive ions [Swetha et al. 2024]. However, many synthetic inhibitors, such as chromates and heavy metal-based compounds, raise environmental and health concerns due to their toxicity and persistence. This has prompted growing interest in biodegradable, non-toxic alternatives derived from natural sources like plant extracts and biopolymers [Anyiam 2026, Raja & Sethuraman 2018, Alaneme et al. 2016, Marzorati et al 2019, Okafor et al 2018].

Starch extracts, as biodegradable polymers, have emerged as promising corrosion inhibitors for metals in acidic environments. Their effectiveness stems from the presence of hydroxyl (-OH) groups and potential glucosidic linkages that enable adsorption onto metal surfaces, forming protective barriers against corrosive ions. Starches from various plants Sweet potato [Anyiam et al 2020b], millet [Nwanonenyi et al 2016], corn [Rosliza and Siti 2022], cassava [Xianghong et al. 2022] have been explored for their inhibition properties. When dissolved in acidic media like HCl or H2SO4, starch molecules can adsorb physically or chemically on metal surfaces, form a hydrophobic film reducing contact with corrosive electrolytes, chelate metal ions, slowing anodic dissolution.

In acidic solutions, protonation of starch hydroxyls may enhance adsorption on negatively charged metal surfaces, improving inhibition efficiency [Palanisamy 2019: Zhang et al 2022]. Studies on similar starches show inhibition efficiency often increases with concentration, typically reaching optimal levels (e.g., 80-95% inhibition at 1-5 g/L [Anyiam et al 2020a]). Factors affecting performance include Starch solubility in acid, Molecular weight/distribution and temperature effects on adsorption [Xie et al. 2025].

Comparisons with synthetic inhibitors sometimes show comparable efficiency for starches, especially in mild conditions [Da Silva etal. 2025]. Limitations include potential biodegradation over long exposure and variability in plant sources. Optimization strategies of starch as a corrosion inhibitor include blending with other green inhibitors (synergism), Chemical modification to enhance solubility/adhesion, nanoparticle encapsulation for controlled release [Fidudusola et al 2025, Han et al 2005].

Caladium tricolor, a tropical plant with starch-rich tubers, presents a viable candidate for corrosion inhibition studies. In South East Nigeria, it is classed as a weed with no economic value.  Its tuber starch has been shown to possess unique structural features that may enhance its adsorption onto metal surfaces [Uwem & Ita 2019, Madison 2011, Resslar 2010, Singh et al 2010]. This study evaluates the effectiveness of Caladium tricolor starch extract as a corrosion inhibitor for mild steel in HCl and H2SO4 media. Basically, it examines inhibition efficiency via weight loss and explores adsorption isotherms. Results obtained would encourage the use of this natural biopolymer as an green alternative in acid-related industrial processes.

- MATERIALS AND METHODS

2.1	Material Collection and Preparation

Caladium Tricolor Starch Collection and Extraction

Starch extract from Caladium tricolor roots was used for this study. The roots were obtained locally, uprooted, washed, cut into pieces and dried to a constant weight under sun, and then ground to fine powder.

Preparation of Molar Acid Solutions

Stock solutions of 0.5M H2SO4, and 0.5M HCl were prepared respectively using serial dilution principle.

Preparation of the coupon

Mild steel coupons used for the study were of 0.5mm in thickness and was mechanically press cut into 3cm x 3cm. Although the coupons were used without additional polishing, they were degreased in absolute ethanol, dried with acetone, and stored in desiccators free from moisture before being used. Composition of the mild steel coupon used includes carbon 0.25	, Manganese 0.25, Phosphorus	0.045, Sulphur	0.02, Titanium 0.04, Iron 99.2, Chromium 0.05 and Copper 0.06

2.2	Experimental Method

Gravimetric Measurement Method

The prepared and weighed mild steel coupons 3cm x 3cm were subjected to time dependent gravimetric tests in 0.5 M H2SO4 and 0.5 M HCl respectively with and without the addition of CTS inhibitor (caladium tricolor starch) of concentrations ranging from 0.3g to 0.9g inhibitor concentrations, the coupons were immersed entirely in 250ml beakers containing 200ml of the test solutions with the aid of glass rods and hooks. The coupons were then retrieved at 24-hours interval progressively until 120hours and washed appropriately with fresh water to remove any corrosion product and finally with acetone. The washed coupons were dried and reweighed, the differences in weight of the coupons before and after immersion in different test solutions were taken as the weight loss, which was then used to compute the corrosion rate using the formula:

CR= (∆W x 87600)/DAt ………………………………………………………………(1)

Where CR = Corrosion Rate (mm/yr), ∆W = change in weight (g). D = Density of the coupon (g/cm³), A = area of exposed surface of the coupon (cm²)  and t = time of immersion (h).

The inhibitor efficiency was at each concentration of biomass samples calculated by comparing the corrosion rate in the absence (CRo) and presence (CR1) using the relationships;

% IE = (CRo -CRi)/CRo X 100                                                                                    (2)

where, CRo = corrosion rate of mild steel in blank corrodent, CRi = corrosion rate of mild steel in presence of the inhibitor.

The degree of surface coverage was calculated from the corrosion rate CRo using the equation

Θ  = = (CRo -CRi)/CRo                                                                                                 (3)

- RESULTS & DISCUSSIONS

3.1	Gravimetric Results:

To establish the effects of exposure time and the concentration of the CBS inhibitor on corrosion inhibition of the test coupons immersed in 0.5 M HCl and 0.5 M H2SO4 solutions, the coupons were subjected to weight loss test. The calculated data for weight loss of uninhibited and inhibited mild steel in 0.5M H2SO4 is presented in Table 1 and Figure 1. From the Table and Figures presented, weight loss reduced with increasing concentration of inhibitors except for that of 24 hours. This could be as a result of instant adsorption of inhibitor on the metal surface, however with increasing time, weight loss was seen to reduce, and hence, more inhibitor molecules were adsorbed on the metal surface thereby inhibiting corrosion which is in tandem with other works [Anyiam et al 2020b, Nwanonenyi et al 2016]. Conversely, the calculated data and graphical representation of weight loss of mild steel in blank and inhibited 0.5M HCl is presented in Table 1 and Figure 2. Results obtained shows that weight loss increased at different time intervals and followed an inconsistent trend with increasing concentration.

Table 1: Calculated values of weight loss for mild steel in 0.5 M H2SO4 in the absence and presence of caladium tricolor starch (CTS).

| Time Concentration (H2SO4) | 24h | 48h | 72h | 96h | 120h |
| --- | --- | --- | --- | --- | --- |
| Blank | 0.85 | 1.94 | 2.52 | 2.50 | 3.02 |
| 0.3 g/L | 0.08 | 0.14 | 0.20 | 0.24 | 0.28 |
| 0.5 g/L | 0.08 | 0.13 | 0.16 | 0.22 | 0.27 |
| 0.7 g/L | 0.09 | 0.12 | 0.17 | 0.22 | 0.24 |
| 0.9 g/L | 0.08 | 0.09 | 0.14 | 0.20 | 0.22 |
| Concentration (HCl) Blank | 0.10 | 0.11 | 0.33 | 0.39 | 0.53 |
| 0.3 g/L | 0.02 | 0.02 | 0.04 | 0.10 | 0.12 |
| 0.5 g/L | 0.03 | 0.04 | 0.08 | 0.09 | 0.10 |
| 0.7 g/L | 0.02 | 0.04 | 0.05 | 0.09 | 0.08 |
| 0.9 g/L | 0.01 | 0.05 | 0.08 | 0.07 | 0.10 |

Figure 1: Plot of weight loss against time for mild steel in 0.5M H2SO4 without and with caladium tricolor starch.

Figure 2: Plot of weight loss against time for mild steel in 0.5M HCL without and with caladium tricolor starch.

Corrosion rate

The calculated data for corrosion rate of mild steel in blank and inhibited 0.5M H2SO4 are presented in Table 2 and Figure 3. From the graphical representation of the corrosion rate of mild steel in blank and inhibited 0.5M H2SO4, corrosion rate increased slightly with increase in concentration under 24 hours. However, for 48 hours to 120 hours, corrosion rate followed the same trend of decreasing with increase in concentration of the inhibitor. This shows that caladium tricolor starch inhibited mild steel corrosion in 0.5M H2SO4, in a concentration-dependent manner as observed from the table and agrees with earlier studies observed by Mobin et al 2011 and Anyiam et al. 2020a.

The calculated values and graphical representation of corrosion rate of mild steel in blank and inhibited 0.5M HCl are presented in Table 2 and Figure 4. From Figure 4, corrosion rate varied slightly with increase in concentration within 24 hours to 120 hours except for that of 48 hours which increased slightly with increase in concentration.

Table 2: Calculated values of corrosion rate, inhibitor efficiency and degree of surface coverage for mild steel in 0.5M H2SO4 and 0.5 M HCl in the absence and presence of caladium tricolor starch

|  | Corrosion Inhibition |  |  |  |  | Inhibition Efficiency |  |  |  |  | Degree of Surface Coverage |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time | 24 | 48 | 72 | 96 | 120 | 24 | 48 | 72 | 96 | 120 | 24 | 48 | 72 | 96 | 120 |
| Conc. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| H2SO4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Blank | 49.96 | 55.32 | 47.69 | 34.56 | 32.43 |  |  |  |  |  |  |  |  |  |  |
| 0.3g/l | 4.36 | 8.13 | 3.59 | 3.51 | 3.33 | 91.23 | 85.30 | 92.47 | 90.39 | 89.73 | 0.9123 | 0.8530 | 0.9247 | 0.9039 | 0.8973 |
| 0.5g/l | 4.60 | 3.66 | 3.07 | 3.19 | 3.04 | 90.79 | 93.38 | 93.56 | 91.27 | 90.63 | 0.9079 | 0.9338 | 0.9356 | 0.9127 | 0.9063 |
| 0.7g/l | 4.62 | 3.60 | 3.04 | 2.99 | 2.77 | 90.75 | 94.03 | 93.62 | 91.81 | 91.46 | 0.9075 | 0.9403 | 0.9362 | 0.9181 | 0.9146 |
| 0.9g/l | 4.72 | 2.54 | 2.61 | 2.59 | 2.51 | 90.55 | 95.40 | 94.52 | 92.91 | 92.26 | 0.9055 | 0.9540 | 0.9452 | 0.9291 | 0.9226 |
| HCl |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Blank | 5.72 | 2.89 | 6.60 | 5.68 | 6.12 |  |  |  |  |  |  |  |  |  |  |
| 0.3g/l | 1.14 | 0.53 | 0.66 | 0.77 | 1.30 | 80.06 | 81.66 | 90.00 | 86.44 | 78.75 | 0.8006 | 0.8166 | 0.9000 | 0.8644 | 0.7875 |
| 0.5g/l | 1.72 | 0.99 | 1.47 | 1.12 | 1.15 | 69.93 | 65.74 | 77.72 | 80.28 | 81.20 | 0.6993 | 0.6574 | 0.7772 | 0.8028 | 0.8120 |
| 0.7g/l | 1.16 | 1.05 | 0.99 | 1.24 | 0.87 | 79.72 | 63.66 | 85.00 | 78.16 | 85.78 | 0.7972 | 0.6366 | 0.8500 | 0.7816 | 0.8578 |
| 0.9g/l | 0.57 | 1.29 | 1.49 | 0.97 | 1.12 | 90.03 | 55.36 | 77.42 | 82.92 | 81.69 | 0.9003 | 0.5536 | 0.7742 | 0.8292 | 0.8169 |

Figure 3: Plot of corrosion rate against time for mild steel in 0.5M H2SO4 without and with caladium tricolor starch.

Figure 4: Plot of corrosion rate against time for mild steel in 0.5M HCL without and with caladium tricolor starch.

Inhibition Efficiency

The data for inhibition efficiency of mild steel in blank and inhibited 0.5M H2SO4 are shown in Table 2 while Figure 5 shows the graphical illustration of inhibition efficiency of mild steel in blank and inhibited 0.5M H2SO4 acidic medium. From Figure 5, the inhibition efficiency increased with time for all concentration, after 48 hours there was gradual decline in inhibition efficiency except for 0.3g concentration that decreased first and then increased at 72 hours before decreasing. The decrease in inhibition efficiency with time depicts desorption of the CTS starch molecules adsorbed on the surface of the metal substrates. This is in tandem with other works [Anyiam et al. 2020a, Anyiam et al 2020b, Mobin et al 2011, Huang et al 2022, Othman et al 2018] on starch molecules; the maximum inhibition efficiency being 95.40% at 48 hours in the presence of starch concentration of 0.9g.

On the other hand, the inhibition efficiency data for the CTS inhibitor in 0.5M HCl, are presented in Table 2 and Figure 6. The graphical representation of inhibition efficiency of mild steel in blank and inhibited 0.5M HCl acidic medium shows that the inhibition efficiency increased with concentration and time but took a downward slide after 48 hrs with 0.9g recording the highest inhibition efficacy values.

Figure 5: Plot of Inhibition efficiency against time for mild steel in 0.5M H2SO4 without and with caladium tricolor starch.

Figure 6: Plot of Inhibition efficiency against time for mild steel in 0.5M HCl without and with caladium tricolor starch.

Adsorption considerations

Figure 7. Plot of Langmuir adsorption isotherm for Caladium Tricolor starch inhibitor on mild steel in 0.5 M H2SO4

For an adsorption /desorption process, the free energy of adsorption (∆Gads) and equilibrium constant (Kads) are related according to Equation 6 given below:

∆G =−RTIn Kads 55.5                                                                                                 (6)

where R is the universal gas constant, Kads is the adsorption-desorption equilibrium constant obtained from the intercept of plot of C /θ against C and T is the absolute temperature. The calculated ΔG (Gibbs free energy) value obtained was −15.246KJ/mol. The negative value of free energy of adsorption is an indication that CTS inhibitor is adsorbed spontaneously onto mild steel surface whereas the value of ∆Gads being lower than – 20KJ/mol means that the CTS inhibitor is physically adsorbed onto mild steel surface indicating the inhibitor molecules are electrostatically attracted to the metal surface [ Allahkarami et al. 2023].

Conclusion

The use of caladium bicolor starch as corrosion inhibitor for mild steel in acidic medium (0.5M H2SO4 and 0.5M HCl) using gravimetric method was assessed in this research work. The corrosion-inhibiting potential of Caladium tricolor starch on mild steel in 0.5 M H₂SO₄ and 0.5 M HCl solutions was evaluated using gravimetric measurements. The results demonstrated that Caladium tricolor starch is a highly effective inhibitor, achieving inhibition efficiencies of up to 95.4% in 0.5 M H₂SO₄ and 90.03% in 0.5 M HCl. The corrosion inhibition is attributed to the adsorption of glucose units from the starch molecules onto active corrosion sites on the mild steel surface. The adsorption behaviour was best described by the Langmuir adsorption isotherm, with a standard free energy of adsorption (ΔG°_ads) of –15.246 kJ mol⁻¹, indicating strong adsorption of the starch molecules. The observed trend in inhibition efficiency suggests a predominantly physisorption mechanism. Additionally, Caladium tricolor starch exhibited superior inhibitory performance in the 0.5 M H₂SO₄ medium compared to 0.5 M HCl.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

REFERENCES

Alaneme, K. K., Olusegun, S. J. & Adelowo, O. T., (2016). Corrosion inhibition and adsorption

mechanism studies of Hunteria umbellata seed husk extracts on mild steel immersed in acidic

solutions. Alexandria Engineering Journal, 55(1), p. 673–681.

Allahkarami, E., Dehghan Monfared, A., Silva, L. F. O., & Dotto, G. L. (2023). Toward a mechanistic

understanding of adsorption behavior of phenol onto a novel activated carbon composite. Scientific reports, 13(1), 167. https://doi.org/10.1038/s41598-023-27507-5

Anyiam, C. K. 2026. Comparative Studies of Caladium Tricolor Stem and Leaf Biomass Extract As

Corrosion Inhibitor for Mild Steel in Acidic Media. International Research Journal of Pure and Applied Chemistry 27 (2):119-30. https://doi.org/10.9734/irjpac/2026/v27i2994.

Anyiam, C.K., Ogbobe, O., Oguzie, E.E. et al. (2020)a. Corrosion inhibition of galvanized steel in

hydrochloric acid medium by a physically modified starch. SN Appl. Sci. 2, 520 https://doi.org/10.1007/s42452-020-2322-2

Anyiam, C.K., Ogbobe, O., Oguzie, E.E. et al. (2020)b. ynergistic Study of Modified Sweet Potato

Starch and KI for Corrosion Protection of Mild Steel in Acidic Media. J Bio Tribo Corros 6, 70 https://doi.org/10.1007/s40735-020-00362-x

Aslam, R., Mobin, M., Zehra, S. and Aslam, J. (2022) A comprehensive review of corrosion inhibitors

employed to mitigate stainless steel corrosion in different environments, Journal of Molecular Liquids, Volume 364, , 119992,ISSN 0167-7322, https://doi.org/10.1016/j.molliq.2022.119992.

Da Silva, E. M., Maravilha, T. S. L., Ortiz, R. W. P., Belati, A., Souza, A. B. O., Venancio, F., Manoel, E.

A., Gonçalves, V. O. O., Cavalcante Freitas, T., Silva, J. M., da Silva, M. T., Fontes, R. A., Kartnaller, V., & Cajaiba, J. (2025). Chemically Modified Soluble Starches as Green Scale Inhibitors in Petroleum Production. ACS omega, 11(1), 552–561. https://doi.org/10.1021/acsomega.5c05924

Fidudusola, A. F., Igbafe, S. and Igbafe, A. I. (2025) Synthesis and Application of Starch-Modified

Chitosan-Silver Nanoparticle Composite as Green Corrosion Inhibitor for Mild Steel in Acidic Media, AJERD, vol. 8, no. 3, pp. 134–147, Nov..

Han XZ, Benmoussa M, Gray JA, BeMiller JN, Hamaker BR. (2005) Detection of proteins in starch

granule channels Cereal Chemistry.. ;82(4):351-355. DOI: 10.1094/cc-82-0351.

Huang, L., Chen, WQ., Wang, SS. et al. (2022). Starch, cellulose and plant extracts as green inhibitors

of metal corrosion: a review. Environ Chem Lett 20, 3235–3264 https://doi.org/10.1007/s10311-022-01400-5

Madison, M. T., (2011). Notes on Caladium (Araceae) and its allies. Selbyana, Volume 5, pp. 342-377.

Marzorati, S., Verotta, L. & Trasatti, S., (2019). Green Corrosion Inhibitors from Natural Sources and

Biomass Wastes. Molecules, pp. 40-48.

Mobin, M., Khan, M.A. and Parveen, M. (2011), Inhibition of mild steel corrosion in acidic medium

using starch and surfactants additives. J. Appl. Polym. Sci., 121: 1558-1565. https://doi.org/10.1002/app.33714

Nwanonenyi SC, Madufor IC, Chukwujike IC, Arinze VC (2016) Experimental and theoretical studies

of the inhibitive behaviour of millet starch on the corrosion of aluminium in the sulphuric acid environment. Int J Eng Technol 8:1–13 DOI: 10.9734/IRJPAC/2016/27881`

Okafor, P. C. et al., (2018). Inhibitory action of Phyllanthus amarus extracts on the corrosion of mild

steel in acidic media. Corrosion Science, Volume 50, pp. 2310-2317.

Othman, N. K., Salleh, E. M., Dasuki, Z., & Lazim, A. M. (2018). Dimethyl Sulfoxide-Treated Starch of

Dioescorea hispida as a Green Corrosion Inhibitor for Low Carbon Steel in Sodium Chloride Medium. In Corrosion Inhibitors, Principles and Recent Applications. InTech. https://doi.org/10.5772/intechopen.73552

Palanisamy, G. (2019). Corrosion Inhibitors. In Corrosion Inhibitors. IntechOpen.

https://doi.org/10.5772/intechopen.80542

Raja, P. & Sethuraman, M., (2018) Natural products as corrosion inhibitor for metals in corrosive

media-A review. Materials Letters, Volume 62, pp. 113-116.

Rosliza R. and Siti N. Saudah (2022) Corn starch inhibitive evaluation on marine corrosion of mild

steel  J. Phys.: Conf. Ser. 2266 012010 DOI 10.1088/1742-6596/2266/1/012010

Resslar, P., (2010) Caladium bicolor naturalized on the island of Hawaii. In: Records of the Hawaii

Biological Survey for 2008. Hawaii: Bishop Museum Occasional Papers, p. 44–45.

Shwetha KM, Praveen, B.M. & Bharath K. Devendra (2024) A review on corrosion inhibitors: Types,

mechanisms, electrochemical analysis, corrosion rate and efficiency of corrosion inhibitors on mild steel in an acidic environment, Results in Surfaces and Interfaces, Volume 16, 100258, ISSN 2666-8459 https://doi.org/10.1016/j.rsurfi.2024.100258.

Singh, S., Singh, N., Isono, N. & Noda, T., (2010). Relationship of granule size distribution and

amylopectin structure with pasting, thermal, and retrogradation properties in wheat starch. Jounal of Agriculture and Food Chemistry, Volume 58, p. 1180–1188.

Uwem, I. N. & Ita, B. N. (2019) Physicochemical, Functional and Antinutritional Properties of

Starches from Caladium Bicolor and Dioscorea Dumentorum. Eur. J. Chem., 10, 228-233.

https://doi.org/10.5155/eurjchem.10.3.228-233.1833

Xianghong L, Shuduan D., Tong L. & Xiaoguang X. (2019) Cassava starch graft copolymer as a novel

inhibitor for the corrosion of aluminium in HNO3 solution, Journal of Molecular Liquids, Volume 282, 499-514, ISSN 0167-7322, https://doi.org/10.1016/j.molliq.2019.03.044.

Xie, Q., Fan, B., Tao, R., Wang, F. & Sun, Y. (2025), A Comprehensive Review of Starch: Structure,

Properties, Chemical Modification, and Application in Food Preservation. Food Frontiers., 6: 1645-1657. https://doi.org/10.1002/fft2.70040

Zhang, X., Zhang, Y., Su, Y., Wang, X., & Lv, R. (2022). Synthesis and Corrosion Inhibition Performance

of Mannich Bases on Mild Steel in Lactic Acid Media. ACS omega, 7(36), 32208–32224. https://doi.org/10.1021/acsomega.2c03545