Thermodynamic and kinetic elucidation of the biogenic capping mechanism: Evidence of ordered self-assembly in Gongronema latifolium-silver nanoparticles

​Abstract

While our previous research successfully established the exceptional in vivo safety profile (LD50 > 5000 mg/kg) and the potent antimalarial efficacy of silver nanoparticles synthesized using Gongronema latifolium, and subsequently identified both Sarsasapogenin and Cinchonidine as the primary molecular stabilizers through Density Functional Theory (DFT) modelling, the precise, intricate physical chemistry governing the formation of this protective “Safety Shield” remained largely unexplored. This current study actively bridges that critical gap by systematically investigating the underlying energetic mechanisms and complex molecular interactions involved. As the third study in this series, it experimentally elucidates the intricate energy landscape and the specific self-assembly mechanism of these biogenic caps. We meticulously monitored the reduction of silver ions under pseudo-first-order conditions across a temperature range of 303–333 K. Kinetic analysis revealed a surface-controlled process Ea≈55 kJ/mol, while Eyring analysis yielded significantly negative entropy of activation ΔS‡≈-105kJmol.K. This thermodynamic signature offers compelling physical evidence for an associative mechanism, suggesting that the critical, rate-determining step involves the assembly of a highly ordered and sterically constrained "biopolymer cage" around the silver nuclei. These experimental findings provide crucial validation for the "Safety Shield" model for biocompatible nanotherapeutics, which was originally proposed in our previous density functional theory (DFT) studies, confirming its real-world efficacy.

​Keywords: Green Synthesis; Kinetics; Thermodynamics; Activation Entropy; Gongronema latifolium; Nanoparticle Stability; Nanomedicine.

### ​

### 1. Introduction

​The paradigm of green nanotechnology has shifted from a novelty to a viable frontier in nanomedicine, offering a sustainable alternative to the toxic reagents inherent in chemical synthesis 1 – 4. Among the diverse biogenic precursors, silver nanoparticles (AgNPs) synthesized from medicinal plant extracts have garnered significant attention for their potent antimicrobial and antiparasitic properties 6 – 11. However, a persistent critique of this field remains the "black box" nature of the synthesis; while biological outcomes are frequently reported, the precise physicochemical mechanisms governing the simultaneous reduction and stabilization (capping) of the metal core remain obscured 12.

​This mechanical opacity is often rooted in the chemical complexity of the plant extracts used 5. Recent investigations into other botanical species, such as Cola hispida, have underscored the necessity of integrative analytical approaches—combining molecular and chromatographic characterization—to accurately identify the bioactive compounds that may interact with metallic precursors 13. Furthermore, the architecture of the resulting nanomaterial is heavily dictated by precursor chemistry. As demonstrated in the synthesis of zinc oxide nanoparticles, the specific choice of metallic salts and the resulting ionic environment significantly influence nucleation, growth kinetics, and final morphology 11, 14 – 15. Consequently, without a rigorous elucidation of this assembly kinetics, the correlation between engineered surface chemistry and the observed biological safety profile remains speculative rather than empirical.

​Our research group has systematically addressed this gap through a phased investigation of Gongronema latifolium-mediated AgNPs. In our initial empirical study 12, we challenged the prevailing view that the organic capping layer is merely an inert by-product. Through comprehensive multi-modal characterization, we observed a critical discrepancy between the crystallite size (XRD/TEM) and the hydrodynamic diameter (DLS), pointing to the existence of a thick, protective "biopolymer matrix" encapsulating the silver core. We hypothesized that this extensive passivation layer was the critical determinant responsible for the nanoparticle's favourable safety profile LD50>5000 mg/kg and the significant suppression of Plasmodium berghei parasitemia. We proposed that this matrix facilitated a "Trojan Horse" endocytic uptake mechanism while mitigating the direct metallic toxicity typically associated with bare silver.

​Building upon this macroscopic "Safety Shield" hypothesis, our subsequent work 16, employed a computational framework to de-convolute the molecular identity of this passivation layer. Utilizing Density Functional Theory (DFT) and MM-GBSA calculations, we interrogated the specific phytochemical constituents of the G. latifolium extract. This theoretical analysis provided a molecular resolution to our earlier experimental observations, identifying Sarsasapogenin as a rigid, chemically inert steric stabilizer—explaining the masking of metallic signals observed in our XRD data. Concurrently, Cinchonidine was identified as the bioactive lead, predicted to target Plasmodium falciparum Dihydrofolate Reductase (PfDHFR). These computational findings effectively bridged the gap between our murine safety signals and a plausible human therapeutic mechanism.

​However, a critical question remains: Does the physical formation of these nanoparticles actually follow the orderly, rigid assembly predicted by our computational models? While DFT predicts a stable, structured shell, it does not account for the chaotic kinetic environment of a boiling aqueous extract 16. If the formation process is merely a random, diffusion-controlled collision of ligands, the "ordered shell" model may be an oversimplification. Conversely, if the synthesis is thermodynamically driven toward highly ordered state, experimental evidence should exist in the form of specific activation parameters 17.

​Therefore, this present study serves as the third pillar of our investigation—the physicochemical validation. By experimentally elucidating the kinetics and thermodynamics of the G. latifolium-mediated synthesis, we seek to define the energy landscape of the capping process. Specifically, we investigated whether the formation of the capping layer is a disordered event or—as our DFT model suggests—an associative, entropically ordered self-assembly. This study thus connects the in vivo safety observed in Phase I 12 and the molecular predictions of Phase II 16 with hard physicochemical proof of the formation mechanism.

### 2. Materials and Methods

​ ​2.1 Materials

Silver nitrate (AgNO3, analytical grade) by Sigma-Aldrich (St. Louis, MO, USA) was purchased from Cobbler & Farmer Ltd. Fresh leaves of Gongronema latifolium were harvested from the School’s botanical garden and authenticated at the Department of Pharmacognosy, Faculty of Pharmaceutical Sciences, Enugu State University of Science and Technology, and processed into a crude aqueous extract following standard protocols 11.

​2.2 Experimental Design for Pseudo-First-Order Conditions

To ensure the reaction kinetics were dependent solely on the unreduced silver fraction (and not limited by extract concentration), a high ratio of extract to precursor was maintained. 10 mL of Gongronema latifolium aqueous extract was reacted with 90 mL of 1 mM AgNO3 (1:9 v/v). For thermal Control, it was ensured that spectral changes were due to SPR generation and not phytochemical degradation; hence, a "blank" control (extract + deionized water) was heated to 60°C for 60 minutes and monitored at 430 nm. For stability, the pH of the reaction mixture was monitored at 30°C and 60°C using a calibrated PH-3SC pH metre to ensure thermal variations did not induce significant protonation/deprotonation events (ΔH<0.3) 18 – 21.

​2.3 Kinetic and Morphological Monitoring

The synthesis was conducted in a temperature-controlled water bath at 30, 40, 50, and 60°C (±0.5℃). Aliquots (2 mL) were withdrawn every 5 minutes and analysed using the LABEC D-11 UV-Vis spectrophotometer (Range: 300–700 nm). To confirm that the reaction mechanism remained consistent across the temperature range, the final hydrodynamic diameter of particles synthesized at 30°C and 60°C was measured using Dynamic Light Scattering (DLS) (Malvern Zetasizer Nano ZS).

​2.4 Theoretical Models

The growth of AgNPs was modelled using pseudo-first-order kinetic equation 6 – 11. To simplify the analysis of the complex crude extract, the Ostwald Isolation Method was applied. By maintaining a large stoichiometric excess of the plant extract relative to the silver precursor (1:9 ratio), the concentration of the reducing agents remains effectively constant throughout the reaction. Consequently, the rate depends solely on the available silver ions, allowing the growth kinetics to be modelled using the pseudo-first-order equation 23 – 26:

lnA∞-At=-kobst+lnA∞-A0……1

Where kobs represents the apparent rate constant derived from the slope of the linear plot.

The energy barriers governing this rate were subsequently calculated using the Arrhenius and Eyring equations 18 – 21, 32 to determine the activation energy (Ea), enthalpy (∆H‡) and (∆S‡) of the transition state:

lnk=lnA-EaRT……(2)

lnkT=lnkBh+∆S‡R-∆H‡RT……(3)

​3. Results and Discussion

  - ​Spectral Evolution and Stability

The formation of AgNPs was tracked by the emergence of a Surface Plasmon Resonance (SPR) band. Figure 1 illustrates the spectral evolution at 50°C. A distinct peak formed at 430 nm, increasing in intensity over 60 minutes. The peak symmetry was maintained without significant red-shifting, indicating the formation of monodisperse particles protected from agglomeration 27 – 30.

Crucially, the thermal control (extract without silver) exhibited negligible absorbance changes (< 0.02 a.u.) at 430 nm upon heating to 60°C. This confirms that the observed kinetics is exclusively attributable to the reduction of Ag+ and nucleation of nanoparticles, rather than the thermal oxidation of phenolic constituents.

​

Figure 1. UV-Vis spectral evolution of AgNP synthesis at 323 K, showing the steady growth of the SPR peak at 430 nm

​3.2 Reaction Kinetics

The rate of particle formation increased significantly with temperature. Figure 2 displays the growth curves Abs430 vs. Time, showing a transition from a slow, sigmoidal growth at 30°C to a rapid exponential rise at 60°C. To quantify the rate, the data was fitted to the pseudo-first-order kinetic model  lnA∞-At vs.  Time. As shown in Figure 3, the plots exhibited high linearity (R2 > 0.98), confirming that under these conditions, the reaction rate depends linearly on the unreduced silver fraction. While the dependence on extract concentration was not explicitly modelled in this study, the high stoichiometric excess of the reducing agent (1:9 v/v) effectively isolates the silver reduction as the rate-limiting kinetic variance, consistent with established protocols 31.

​

Figure 2. Time-dependent growth of AgNPs at temperatures ranging from 303 K to 333 K

​​

Figure 3. Pseudo-first-order kinetic plots of lnA∞-At versus time. The linearity confirms the reaction order.

  - ​Thermodynamic Activation Parameters

Using the rate constants derived from Figure 3, the energy barrier of the reaction was analysed. Figure 4A (Arrhenius Plot) yielded an Activation Energy (Ea) of 55.0 kJ/mol. This value is significantly higher than the activation energy for simple diffusion-controlled processes (< 20 kJ/mol) 32. It suggests a chemically controlled surface reaction, where the rate is limited by the specific interaction between the phytochemical ligands and the silver interface, rather than simple Brownian collision. Furthermore, Figure 4B (Eyring Plot) provided the Enthalpy (ΔH‡) and Entropy (ΔS‡) of activation as 52.4 kJ/mol (Endothermic) and —104.8 J/mol⋅K respectively.

​  Figure 4. (A) Arrhenius plot for determining Activation Energy. (B) Eyring plot for determining Enthalpy and Entropy of activation

​3.4 Mechanism: The "Associative Cage" Hypothesis

The negative entropy value ΔS‡≈-105 J/mol⋅K is the defining finding of this study. In the context of the Transition State Theory, a negative entropy change indicates a loss of degrees of freedom. This strongly supports an associative mechanism, where the reactants (silver ions and phytochemicals) form a highly ordered complex in the transition state 33 – 34.

This provides direct physical evidence for an associative mechanism. Unlike simple collision theory where reactants bounce randomly, the data suggests that the bulky ligands identified in our previous computational study (Sarsasapogenin, Cinchonidine) undergo a structural reorientation to form a "supramolecular cage" around the silver nuclei (Figure 5). The negative entropy reflects the thermodynamic "cost" of organizing this bulky Sarsasapogenin lattice. However, this cost pays off in the exceptional stability and safety profile of the final particle, confirming the "Safety Shield" architecture modelled in our previous work

Figure 5. An Illustration of the schematic associative mechanism of the transition from disordered free ligands to an ordered "Sarsasapogenin Cage" corresponding to the observed negative entropy  (ΔS‡<0)

To validate that this mechanism holds true across temperatures, DLS analysis was performed on the end-products. As shown in Figure 6, the hydrodynamic diameter remained statistically consistent between 30°C (43.5 ± 2.1 nm) and 60°C (44.1 ± 3.5 nm). This confirms that thermal energy accelerated the reaction rate without altering the fundamental assembly of the biopolymer shell.

Figure 6. Comparative DLS size distribution of AgNPs synthesized at 30°C and 60°C, showing preserved morphological integrity

### ​4. Conclusion

​This study provides the thermodynamic "missing link" between our computational predictions and the observed stability of Gongronema latifolium-AgNPs. The reaction kinetics confirms a surface-controlled process, while the negative entropy of activation provides physical proof of an ordered, associative assembly. We conclude that the "Safety Shield" mechanism is not a passive outcome but an active, thermodynamically driven self-assembly of phytochemicals, validating the potential of these particles for stable biomedical applications.

Author Contributions:

Goodnews Onyedikachi Ikeh: Conceptualisation, writing – original draft, methodology, formal analysis, supervision, resources. Jasmine Kayanian: investigation, formal analysis. Rita Chiamaka Okpoto: Methodology, investigation. Charles Chinedu Diovu: formal analysis. Sunday Kaura: Investigation, editing and formal analysis. Ndidiamaka H. Okorie: Investigation, editing and formal analysis. Ibeabuchi J. Ali: Investigation, methodology.

Data availability statement

The authors confirm that the data supporting the findings of this study are available within the article and its Supplementary Appendix. Raw data files are hosted at https://drive.google.com/file/d/1ixxaHzfxCcL84MbjGz9tqedrZfDC_Tdx/view?usp=drivesdk, and can be accessed without restriction.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

[1] Mittal AK, Chisti Y, Banerjee UC. Synthesis of metallic nanoparticles using plant extracts. Biotechnol Adv. 2013;31(2):346-356. doi: 10.1016/j.biotechadv.2013.01.003

[2] Jadoun S, Arif R, Jangid NK, Meena RK. Green synthesis of nanoparticles using plant extracts: a review. Environ Chem Lett. 2021;19(1):355-374. doi: 10.1007/s10311-020-01074-x

[3] Singh J, Dutta T, Kim KH, Rawat M, Samddar P, Kumar P. ‘Green’ synthesis of metals and their oxide nanoparticles: applications for environmental remediation. J Nanobiotechnology. 2018;16(1):84. doi: 10.1186/s12951-018-0408-4

[4] Ovais M, Khalil AT, Islam NU, Ahmad I, Ayaz M, Saravanan M, et al. Role of plant phytochemicals and microbial enzymes in biosynthesis of metallic nanoparticles. Appl Microbiol Biotechnol. 2018; 102(16):6799-6814. doi: 10.1007/s00253-018-9146-7

[5] Umerie SC, Okorie NH, Dike DU, Ani NI. Phytochemical analysis and antioxidant activity of avocado pear peel (Persea americana) extract. J Pharm Res Int. 2022 Mar 29;34(28A):22-29.

[6] Zhang XF, Liu ZG, Shen W, Gurunathan S. Silver nanoparticles: synthesis, characterization, properties, applications, and therapeutic approaches. Int J Mol Sci. 2016;17(9):1534. doi: 10.3390/ijms17091534

[7] Burdușel AC, Gherasim O, Grumezescu AM, Mogoantă L, Ficai A, Andronescu E. Biomedical applications of silver nanoparticles: an up-to-date review. Nanomaterials. 2018;8(9):681. doi: 10.3390/nano8090681

[8] Tortella GR, Rubilar O, Durán N, Diez MC, Martínez M, Parada J, et al. Silver nanoparticles: toxicity in model organisms as an overview of its hazard for environmental health. J Hazard Mater. 2020;390:121974. doi: 10.1016/j.jhazmat.2019.121974

[9] Lee SH, Jun BH. Silver nanoparticles: synthesis and application for nanomedicine. Pharmaceutics. 2019;11(10):499. doi: 10.3390/pharmaceutics11100499

[10] Ikeh GO, Ugwu PE, Okpoto RC, Njoku EA, Diovu CC, Adonu CC. Biogenic Synthesis and comparative Assessment of the Antimicrobial Activities of Silver and Zinc Nanoparticles of Dialium guineense Leaf Extract against Human Pathogens. J. Compl. Altern. Med. Res. 2024:25(12):211-26. doi: 10.9734/jocamr/2024/v25i12607

[11] Okorie NH, Ikeh GO, Adonu CC, Okorie CP, Omeh RC, Nwangwu AK. Precursor Chemistry and Antimicrobial Performance: A Green Synthesis Approach to the Zinc Oxide Nanoparticles. Asian J. Apple. Chem. Res. 2025;16(2):116-40. doi: 10.9734/ajacr/2025/v16i2333

[12] Ikeh GO, Nubila NI, Nwoke CO, Nwoke CN, Okpoto RC, Igwe CC, Chukwuebuka OE. Green Synthesis of Silver Nanoparticles for Antimalarial Activity: Characterisation, Acute Toxicity, and Efficacy Studies in a Murine Model. Jabirian J. Biointerface Res. Pharmaceut. Appl. Chem. [Internet]. 2025 Jan. 10 [cited 2026 Apr. 2];2(1):15-2. Available from: https://sprinpub.com/jabirian/article/view/jjbrpac.v2i1.593

[13] Ikeh GO, Ani NI, Ude VU, Onyia JK, Diovu CC, Okpoto RC. Molecular Spectroscopic (FTIR and UV-Vis) and Hyphenated Chromatographic (GC-MS) Characterisation of Bioactive Compounds present in different solvent fraction of Extract of Leaf of Cola hispida Brenan& Keat Sterculiaceae. S. Asian Res. J. Nat. Prod. 2025;8(2):229-52. doi: 10.9734/sarjnp/2025/v8i2194

[14] Loza K, Heggen M, Epple M. Synthesis, structure, properties, and applications of silver nanoparticles. Adv Funct Mater. 2020;30(24):1904390. doi: 10.1002/adfm.201904390

[15] Finney EE, Finke RG. Nanocluster nucleation and growth kinetic and mechanistic studies: A review emphasizing stopping points. J Colloid Interface Sci. 2016;472:232-257. doi: 10.1016/j.jcis.2016.03.018

[16] Ikeh GO, Kayanian J, Nubila NI, Diovu CC, Kaura S, Okorie NH, et al. Translational Insight into Gongronema latifolium-silver Nanoparticles: Linking in vivo Safety to Molecular Antimalarial Mechanism. J. Adv. Med. Pharm. Sci. [Internet]. 2026 Mar. 26 [cited 2026 Apr. 2];28(3):22-35. Available from: https://journaljamps.com/index.php/JAMPS/article/view/850

[17] Al-Thabaiti SA, Al-Arfaj AA, Khan Z. Sol-gel synthesis of silver nanoparticles using Senegalia greggii leaf extract: Kinetics and thermodynamics. J Mol Liq. 2021;321:114749. doi: 10.1016/j.molliq.2020.114749
[18] Nayak V, Singh KR, Singh RP. Kinetics and thermodynamics of green synthesis of silver nanoparticles. J Environ Chem Eng. 2021;9(4):105574. doi: 10.1016/j.jece.2021.105574

[19] Mekky AE, Al-Hazmi GA, Al-Arfaj AA, Khan Z. Mechanistic and kinetic studies of green synthesis of silver nanoparticles using aqueous extract of Cymbopogon proximus. J Mol Liq. 2019;275:758-765. doi: 10.1016/j.molliq.2018.11.111

[20] Heidari M, Ghorbani M. Kinetic study and optimization of silver nanoparticles green synthesis using Urtica dioica extract. Sci Rep. 2022;12:12450. doi: 10.1038/s41598-022-16627-y

[21] Anandalakshmi K, Venugobal J, Ramasamy V. Characterization of silver nanoparticles by green synthesis method using Adhatoda vasica leaf extract and its antibacterial activity. Appl Nanosci. 2016;6:399-408. doi: 10.1007/s13204-015-0449-z

[22] Darroudi M, Ahmad MB, Abdullah AH, Ibrahim NA. Green synthesis and characterization of gelatin-based and sugar-reduced silver nanoparticles. Int J Nanomedicine. 2011;6:569-574. doi: 10.2147/IJN.S16867
[23] Espinoza MG, Hietala S. The effect of temperature on the nucleation and growth of silver nanoparticles mediated by a plant extract. Nanomaterials. 2020;10(9):1723. doi: 10.3390/nano10091723

[24] Prasad R, et al. Temperature-dependent synthesis of silver nanoparticles using Terminalia chebula fruit extract. Mater Lett. 2017;188:143-146. doi: 10.1016/j.matlet.2016.10.076

[25] Iravani S, Varma RS. Green synthesis, characterization and applications of silver nanoparticles. Nanomaterials. 2020;10(3):575. doi: 10.3390/nano10030575

[26] Ameen S, et al. Green synthesis of silver nanoparticles using Hibiscus rosa-sinensis: Influence of temperature and pH on growth kinetics. J Photochem Photobiol B. 2019;192:131-139. doi: 10.1016/j.jphotobiol.2019.01.014

[27] Eyley S, Thielemans W. Surface modification of cellulose nanocrystals. Nanoscale. 2014;6:7764-7779. doi: 10.1039/C4NR01756K

[28] Trache D, Tarchoun AF, Derradji M, Hamidi A, Ning N, Gandhi S, et al. Nanocellulose: From fundamentals to advanced applications. Front Chem. 2020;8:392. doi: 10.3389/fchem.2020.00392

[29] Dufresne A. Nanocellulose: From nature to high performance tailored materials. 2nd ed. Berlin: De Gruyter; 2017. ISBN: 978-3110478488.

[30] Grishkewich N, Mohammed N, Tang J, Tam KC. Recent advances in the application of cellulose nanocrystals. Curr Opin Colloid Interface Sci. 2017;29:32-45. doi: 10.1016/j.cocis.2017.01.005

[31] Laidler KJ. Chemical Kinetics. 3rd ed. New York: Harper & Row; 1987.
[32] Atkins P, de Paula J, Keeler J. Atkins' Physical Chemistry. 12th ed. Oxford: Oxford University Press; 2022. ISBN: 978-0198847816.
[33] House JE. Principles of Chemical Kinetics. 2nd ed. Burlington: Academic Press; 2007. doi: 10.1016/B978-0-12-356787-1.X5001-3

[34] Houston PL. Chemical Kinetics and Reaction Dynamics. New York: Dover Publications; 2019. ISBN: 978-0486835013.