Numerical Study of the Thermal Behavior of a Wall Built with Different Materials in a Hot and Dry Climate

.

ABSTRACT

This article presents a numerical study of the thermal behavior of walls made from different materials in a hot and dry climate, constituting a first step of thesis work. The main objective is to analyze the temperature evolution inside walls built of hollow cement blocks and local materials (CEB, CLB, and adobe), in order to identify the least performing material in terms of thermal insulation, with a view to subsequently improving its properties. The governing equations were solved using the finite element method, implemented in the COMSOL Multiphysics software (version 5.3).The study was structured around two axes: the analysis of the temperature evolution at the internal and external surfaces of the walls, and the study of the influence of the position of a cement and plaster-based coating layer on the thermal behavior of the walls. The results obtained indicate that temperature peaks are significantly higher in hollow cement block walls (38.55°C) than in those built with local materials [35.07-35.23°C]. These observations show that hollow cement block presents low thermal performance in Sahelian zones, due to its high capacity to rapidly accumulate heat. In perspective, future work will aim to propose solutions to improve the thermal performance of this material.

Keywords: Numerical study, thermal behavior, hollow cement block, local materials

1. INTRODUCTION

The building sector, alongside the transport and industrial sectors, ranks among the world’s three largest energy consumers[1].

Globally, the building sector alone accounts for   of total energy consumption [2], approximately   of greenhouse gas emissions [3], and 50% of this annual consumption is generally caused by heating, ventilation and air conditioning systems [4].

Like other African countries, Burkina Faso is a nation where the building sector is one of the major contributors to energy consumption. Until now, buildings have been designed without energy efficiency in mind, resulting in high costs for operators who have not been made aware of the need for rational energy use. Most of the time, a large proportion of this energy is used for ventilation and air conditioning in offices and homes. According to a study carried out in 1989 and made available by the Ministry of Economy and Finance, energy consumption in public sector buildings, particularly for the operation of air conditioning units, is estimated at 30,000 MWh/year, which corresponded to an estimated financial cost of 3.4 billion CFA francs per year [5].

These costs place a heavy burden on the budgets of low-income countries such as ours. To reduce this energy consumption in a context marked by climate change and the increasing scarcity of fossil fuel resources, it is necessary to consider new construction techniques in order to improve the energy efficiency of buildings.

Numerous studies [3] [6] [7] [8][9][10][11][12] have been conducted on local materials such as cut laterite bricks (CLB), compressed earth bricks (CEB) and adobe, with a view to promoting them as building materials in Burkina Faso, as these authors have demonstrated that these materials offer good thermal performance. However, it must be acknowledged that these materials have not been successful, as virtually all buildings in Burkina Faso, in particular, have until now been constructed using cement blocks. Cement blocks are a material with interesting properties in the construction sector, due to their mechanical performance, but the major drawback is that their thermal properties are unsuitable for our context. Indeed, a building constructed from cement blocks heats up quickly during hot spells and cools down quickly during cooler periods.

The aim of this study is to investigate temperature changes in a wall constructed from hollow concrete blocks and local materials, with or without render, when subjected to external and internal convective loads, in order to propose a solution for improving the thermal performance of the less insulating material.

2. METHODLOGY

Physical model description

Figure 1 presents the physical model of the rectangular wall, with a height of 3m and a thickness e=0.15m. The wall is built with hollow cement blocks or with BTC, BLT and/or adobe of dimensions 0.40 m x 0.20 m x 0.15 m. The exterior surface of the wall is subjected to convective and solar flux, while the interior surface is subjected to convective flux. Heat transfer within the wall is purely conductive because air velocity is almost zero in the block cavities. The horizontal surfaces are thermally insulated.

Figure 1 shows the two-dimensional (2D) physical model of the wall.

Figure 11: Physical model of the wall

In this study, we consider the wall to be homogeneous and isotropic.

The geometric model considered is presented in figure 2 below, where each type of material has well-defined characteristics.

Figure 2 shows the geometric model of the wall.

Figure 22: Geometric model of the wall

Table 1 presents a reminder of the thermophysical properties obtained during characterization.

Table 1: Thermo-physical properties of the materials used for the study [7] [8] (7)(8)

|  | Density | Thermal conductivity | Specific heat |
| --- | --- | --- | --- |
| Hollow cement block | 1050 | 0,785 | 1275 |
| BLT | 1075 | 0 ,556 | 1310 |
| BTC | 1700 | 0,7 | 1492 |
| Adobe | 1305 | 0,5 | 1060 |

3. Mathematical model

3.1. Heat transfer equation in the wall

Heat transfer in the wall is purely conductive. The basic equation governing heat transfer is as follows:

(1)

Where : density ; : specific heat capacity at constant pressure  and : thermal conductivity ; T: temperature (°C); : heat capacity at constant volume; : velocity field ; : heat source ; : variation of total energy; : variation of energy by conduction and : variation of energy by convection.

3.2. Simplifying assumptions

The simplifying assumptions for the physical problem are as follows:

- heat transfer is two-dimensional (2D) and transient;

- the thermo-physical properties (thermal conductivity, density, and specific heat) of the wall are constant;

- convection and radiation within the walls are negligible;

- the materials used are homogeneous and isotropic;

- the heat source is negligible in the materials.

3.3. Equation formulation

Considering the mentioned hypotheses, the equations describing the phenomenon are written as follows:

(2)

The thermophysical properties, and respectively, density, specific heat, and thermal conductivity are functions of the materials constituting the domain, namely hollow cement block, BTC, BLT, and adobe.

3.4. Initial and boundary conditions

3.4.1. Initial conditions

At time t=0s, the hollow cement block wall is at ambient temperature. The initial condition is expressed as:

and, we have: 				(3)

3.4.2. Boundary conditions

The boundary conditions for the calculation domain at are as follows:

- Exterior wall surface:

At time t>0s  , we impose on the external face a convective heat flux and a solar flux:

For  and , we have:       (4)

With:					(5)

the solar absorption coefficient of the wall and  [9] is the solar flux.

Figure 3 shows the evolution of solar flux over time.

Figure 33: Evolution of solar flux as a function of time (10)

Figure 3 represents the evolution of the solar flux density reaching the external facade of the wall as a function of solar time during the month of April in Ouagadougou. It can be seen in Figure 3 that the solar flux density in the middle of the day is visibly greater than that of the periods before noon and after noon, reaching maximum values of approximately 1100 W/m2.

- Interior wall surface:

At time t>0, we impose on the exterior face a convective heat flux:

For  and , we have: 		(6)

- Horizontal wall surfaces:

The boundary conditions for the horizontal walls are formulated as follows:

For , and , we have: 				(7)

; , we have:  					(8)

4. Resolution method

The numerical simulation was performed using the finite element method on COMSOL Multiphysics software version 5.3. The simulation duration is 24 hours with a constant time step of 5 min. The wall geometries (see figure 1), the physical properties of the materials used (see table 4), as well as the initial and boundary conditions were defined in the software. We also used constant values for the external and internal convective heat transfer coefficients from the literature. These values are respectively 16.7W/m2/K and 9W/m2/K [8]. (8)

An extremely fine quadratic mesh was adopted with 1208 triangular elements, 210 boundary elements, and four-point elements. This allowed us to obtain a convergence criterion of the order of .

5. results and discussion

In this section, we will focus, on the one hand, on the study of the temperature evolution within the wall and at the internal surface of the building wall constructed either with cement blocks or with local material (BLT, BTC, or Adobe). On the other hand, we will study the effect of a layer of cement render or plaster render on the temperature evolution of the internal wall surface.

5.1. Study of temperature evolution within different walls

We analyze the influence of temperature on construction materials on the evolution of temperature within the wall.

Figure 4 shows the evolution of temperature within the wall as a function of time.

Figure 44: Evolution of temperature within the wall as a function of time

The curves in Figure 4 show the temperature profiles within the wall constructed with hollow cement blocks or local materials and the external wall as a function of time.

The maximum temperature observed in the outdoor ambient is approximately 47.6°C, that within the wall constructed with hollow cement blocks is 38.55°C; 35.13°C for the wall constructed with BTC; it is 35.07°C for the BLT wall and for the adobe wall, it is 35.23°C. The observed temperature differences are respectively 9.05°C; 12.47°C; 12.53°C and 12.37°C.

We note that the maximum temperature values are higher in a wall constructed with hollow cement blocks than in a wall constructed with local materials.

Table 2 shows the phase shift and attenuation factor of each wall.

| Material type | Time in hours (h) |  | Phase shift (in h) | Temperature Interior (°C) |  |  | Temperature Exterior (°C) |  |  | Factor Attenuation (% ) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concrete block | 14,08 | 13,08 | 1 | 26,49 | 32,18 | 5,69 | 27,35 | 38,55 | 11,20 | 50,80 |
| BTC | 18,25 | 15,08 | 3,17 | 27,19 | 29,82 | 2,63 | 28,51 | 35,13 | 6,62 | 39,72 |
| BLT | 18,25 | 15 | 3,25 | 27,12 | 29,62 | 2,50 | 28,49 | 35,07 | 6,58 | 37,99 |
| Adobe | 18,08 | 15,00 | 3,08 | 27,00 | 29,39 | 2,39 | 28,47 | 35,23 | 6,76 | 35,35 |

We can see from Table 2 that the wall constructed from hollow cement blocks has a high damping factor (50.80%) and a low thermal time lag (1 hour), whereas the wall constructed from BTC, BLT and/or adobe have a low damping factor [35–40%] and high thermal lag [3–3.25 hours]. However, the lower the damping factor, the more temperatures are smoothed out. Like thermal lag, it also helps to characterise the thermal inertia of the building [16]. A material with low thermal lag will result in a maximum indoor temperature during the day whilst outdoor temperatures remain high [3].

The authors [3], [6], [8], [9] and [17] demonstrated in their studies that the walls of buildings constructed with local materials (BTC, BLT and/or adobe) exhibit high thermal phase shift and low damping compared to walls built with hollow cement blocks.

These results are also similar to those found by Saidi et al. [18] on the effect of stabilising compressed earth bricks (CEB) on the temperature at the inner surface of the wall. The authors found that adding paper to the CEB reduced its maximum temperature by 0.2°C and increased the time lag by one hour.

The work by Mellaikhafi et al. [19] indicates a maximum reduction of approximately 46% in heat transfer through walls containing fibres from pinnate leaves. Furthermore, the thermal phase shift and damping factor are improved, ensuring better energy efficiency. According to some authors, such good thermal performance is linked to their low thermal conductivity [20] [21] [22].

5.2. Study of the temperature evolution at the internal surface of different walls

We also study the influence of temperature on materials at the internal surface of the wall.

Figure 5 shows the temporal evolution of temperature at the internal surface of the wall.

Figure 5: Evolution of temperature at the internal surface of the wall as a function of time

The curves in Figure 5 show the 24-hour temporal evolutions of temperatures at the external and internal surfaces of the wall constructed with hollow cement blocks or local materials.

We observe in the figure that the maximum temperature values are 32.18°C; 29.82°C; 29.62°C and 29.39°C respectively for the hollow cement block wall, BTC, BLT and or adobe. The respective differences noticed are 15.42°C; 17.78°C; 17.98°C and 18.21°C.

The results obtained are similar to those obtained by Zoma et al. [6] (6)who presented a numerical study on the thermal behavior of a wall constructed with hollow cement blocks, during which they found 29°C as the maximum temperature at the internal surface of the wall. These differences could be explained by the nature of the materials or the data used during the simulation.

Table 3 shows a summary of the maximum values observed within the wall and at the internal surface.

Table 3: Maximum temperatures within the wall and at the internal surface

| Hollow block | 38,55 | 32,18 |
| --- | --- | --- |
| BTC | 35,13 | 29,82 |
| BLT | 35,07 | 29,62 |
| Adobe | 35,23 | 29,39 |

We can see from Table 3 and Figures 4 and 5 that the peak temperatures are higher in the wall built with hollow concrete blocks than in a wall built with local materials. The temperature differences observed may be due to the thermophysical properties of the materials. Indeed, the thermal conductivity of hollow cement blocks is higher than that of the other materials used (BTC, BLT and adobe).  We can therefore conclude that local building materials such as laterite blocks, BTC or adobe have higher thermal inertia than hollow cement blocks.

The authors [3], [6], [14], [23] and [24] have also shown that hollow cement blocks are a material that should be avoided in housing construction in the Sahelian region.

In light of these results, we can conclude that, although hollow concrete blocks possess mechanical strength and good water resistance compared to other construction materials, they have a major disadvantage in that their thermal properties are unsuitable for our climatic context. Indeed, a building constructed from concrete blocks heats up quickly during hot periods and cools down quickly during cooler periods.

5.3. Study of the influence of mortar on the internal wall temperature of different walls

Next, we will study the effect of a mortar layer within a wall constructed with different materials on the internal wall temperature.

Table 4 illustrates the thermophysical properties of the different types of mortar used

Table 4: Thermophysical properties of plaster and cement render [7] [8] (7)(8)

| Plaster | 1450 | 0,45 | 880 |
| --- | --- | --- | --- |
| Cement render | 1700 | 1,15 | 1000 |

We present the results obtained for a wall composed of a 25 cm layer of either cement render mortar or simple plaster mortar. The following Figure 6 shows the temporal evolution of the temperature at the internal surface of the wall.

Fig.6.a: Cement mortar

|  | Fig.6.b: Plaster mortar |
| --- | --- |

Figure 6: Evolution of temperature at the internal surface of the wall as a function of time

The curves in Figure 6 show the 24-hour temporal evolution of temperature at the external and internal surfaces of a wall constructed with hollow cement blocks, BTC, BLT, and/or adobe, composed of a layer of render mortar (Fig.6.a) and/or a layer of plaster mortar (Fig.6.b).

In Figure 6.a, we observe that the maximum temperature is 30.86°C for the hollow block wall; 29.23°C for the BTC wall; for the BLT wall, it is 29.18°C, while it is 28.86°C for the adobe wall. We notice respective differences of 16.86°C; 18.37°C; 18.42°C and 18.74°C.

Whereas in Figure 6.b, we observe 30.34°C; 28.84°C; 28.78°C and 28.52°C as maximum temperatures, respectively for the hollow cement block wall, BTC, BLT and/or Adobe, with differences of 17.26°C; 18.76°C; 18.82°C and 19.08°C.

Zoma et al. [6]  also studied the effect of mortar on the thermal behavior of a wall constructed with cement blocks, where they found 28.52°C for cement mortar and 27.963°C for plaster mortar.

Table 5 presents a summary of the maximum values observed in these two figures.

Table 5: Summary of maximum temperature values (in °C)

|  | Cement render mortar (in °C) | Plaster mortar (in °C) |
| --- | --- | --- |
| Hollow cement block | 30,86 | 30,34 |
| BTC | 29,23 | 28,84 |
| BLT | 29,18 | 28,78 |
| Adobe | 28,86 | 28,52 |

We note that, for both types of mortar, temperature peaks are still high for a hollow block wall, 30.86°C for cement render and 30.34°C for plaster render. Walls constructed with local materials have relatively low temperatures around 28°C. But comparing the two types of mortar, temperature peaks dampen a bit more for plaster mortar than for cement render mortar. This difference could be due to the thermal conductivity value, which is lower for plaster than for cement render; making the former more insulating. The maximum temperature amplitude is significantly reduced for a wall constructed with local materials compared to that of a cement block wall.

6. Conclusion

This work presents a numerical simulation of the thermal behavior of walls made from different materials in a hot and dry climate. The materials considered are hollow cement block, BLT, BTC, and adobe. The model equations were solved using the finite element method, and simulations were performed with COMSOL Multiphysics software (version 3.5).

The results show that maximum temperatures within the walls vary depending on the material: 38.55 °C for hollow cement block, 35.13 °C for BTC, 35.07 °C for BLT, and 35.23 °C for adobe. At the internal surfaces, the recorded temperatures are respectively 32.18 °C (block), 29.82 °C (BTC), 29.62 °C (BLT), and 29.39 °C (adobe).

Furthermore, the addition of a mortar layer (cement or plaster) on the internal or external faces helps to reduce the thermal amplitude, with maximum temperatures reaching 30.86 °C for the block, 29.23 °C for the BTC, 29.18 °C for the BLT, and 28.86 °C for the adobe.

Ultimately, the study highlights better thermal performance of local materials (BTC, BLT, and adobe), characterized by a significant reduction in temperature amplitudes, contrary to the hollow cement block which exhibits low thermal inertia. These results pave the way for future work aimed at improving the thermal performance of this latter material.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

[1]. Y. Camara, Etude numérique des performances thermiques d'un habitat bioclimatique, Universités UGANC et Perpignan(France), 2018

[2]. L. Yang, H. Yan and J. C. Lam, "Thermal comfort and building energy consumption implications –A review," Applied Energy, vol. 115, p. 164–173, 2014.

[3]. C. Abdoulaye, Etude des performances thermiques d’un habitat type du burkina faso. Application : contribution a la mise en place d’une reglementation thermique, Université Professeur JOSEPH KI-ZERBO, 2018.

[4]. A. Bastide, P. Lauret, F. Garde and H. Boyer, "Building energy efficiency and thermal comfort in tropical climates Presentation of a numerical approach for predicting the percentage of well-ventilated living spaces in buildings using natural ventilation," Energy and Buildings, vol. 38, p. 1093–1103, 2006.

[5]. Coulibaly, A. OUEDRAOGO, J. KOULDIATI and P. ABADIE, "Etude thermique d'un batiment bioclimatique en double paroi dénommée Newango: Inertie thermique et consommation d'énergie," 2011.

[6]. F. A. Oumarou, L. B. Abdou, O. Souleymane, S. M. K. Thierry, M. Lewamy and D. J. Bathiebo, "The Impact of Local Materials on the Improvement of the Thermal Comfort in Building," Current Journal of Applied Science and Technology, vol. 39, no. 15, pp. 22-35,, 2020.

[7]. E. Malbila, D. Y. Toguyeni, S. Bamogo, A. Lawane and J. Koulidiati, "Thermophysical and Mechanical Characterization of Local Stabilized Materials Suitable for Buildings in Dry and Hot Climate," Journal of Materials Science & Surface Engineering, vol. 6, no. 2, pp. 767-772, 2018.

[8]. Arouna Kaboré, Zoma Vincent, Palm Kalifa, Bathiebo Dieudonné Joseph, Two-Dimensional Modeling of Heat Transfers in a Ventilated Test Cell Built with Various Local Materials, Physical Science International Journal, 5(8): 14-31, 2021, ISSN: 2348-0130,

[9] Yalé Abdoul Aziz SEREBE, Zoma VINCENT, Drissa OUEDRAOGO, Salifou OUEDRAOGO, Yssa TRAORE,Ahmed Douani SERE, Numerical Study of Effect of Kenaf Fiber Content and Size on the Thermal Inertia of Adobe Walls, Volume 29, Issue 3, Page 29-41, 2025; Article no.PSIJ.134251, ISSN: 2348-0130 https://doi.org/10.9734/psij/2025/v29i3881

[10] Frédéric Nebié, Boureima Kaboré, Vincent Zoma, Emmanuel Ouedraogo, Sié Kam, Modeling and Simulation of Heat Exchanges in a Habitat F1 Built With Concrete Blocks in the City of Koudougou, Elixir Thermal Engineering 181 (2023) 57012 – 57018.

[10] KABORE Arouna, KABORE Hermann, ZOMA Vincent, SANDWIDI Sayouba, PALM Kalifa, Thermal Analysis of the Walls of a Bioclimatic Building in Earth: Measurement of Temperatures of External and Internal Surfaces, International Journal of Research and Review, Volume 12, Issue: 8, August 2025, E-ISSN: 2349-9788; P-ISSN: 2454-2237,  https://doi.org/10.52403/ijrr.20250807

[11] Arouna Kaboré, Boukaré Ouédraogo, Sayouba Sandwidi, Vincent Zoma, Hermann Kaboré, Kalifa Palm, Experimental Study of the Thermal Behavior of a Bioclimatic Building Prototype in a Sahelian Zone, Scientiifc Research Publishind, Smart Grid and Renewable Energy, 2024, 15, 187-199,  ISSN (Papier): 2151-481X, ISSN (ligne): 2151-4844

[12] Alidou Maiga, Koffi Sagna, Karim Toussakoe, Vincent Zoma, Lareba Adélaïde Ouedraogo, Sié Kam, Optimization of Thermal Comfort in Compressed Earth Block (CEB) Buildings in Burkina Faso, Science Publishing Group, Science Journal of Energy Engineering, 2024, Vol. 12, No. 4, pp. 101-112 ,  ISSN (ligne) : 2376-8126 ; ISSN (papier) : 2376-810X

[13]. Danida development advisory group., designing with nature. Guide to planning and active design in hot and dry or hot and humid climates, 1999.

[14]. B. Kaboré, Climatisation d’une habitation en zone sahélienne a l’aide du principe du puits canadien, Universite Joseph KI-ZERBO, Ouagadougou, Burkina Faso, 2017

[15]. D. J. BATHIEBO, Laboratoire d'Energie Thermique REnouvelable, Ouagadougou, 2019

[16]. L. Chahwane, Valorisation de l ’ inertie thermique pour la performance énergétique des bâtiments performance énergétique des bâtiments,” ’Université de Grenoble, 2012

[17]. Vincent Zoma, Boureima Kaboré, Germain Wende Pouiré Ouedraogo, Jean Marie Compaoré and Sié Kam, Numerical Study of the Thermal Behavior of a Hollow Block with Phase Change Materials (PCM)  in the Sahelian Zone, Asian Journal of Physical and Chemical Sciences, Volume 11, Issue 1, Page 1-12, 2023; Article no.AJOPACS.96779; ISSN: 2456-7779; DOI:10.9734/AJOPACS/2023/v11i1191

[18]. Meriem, S., Cherif, A., Ezeddine S., Zeghmati, B. R, Etude numérique du comportement thermique de brique de terre stabilisée, Conference paper on Researchgate. p.8, 2016

[19]. Mellaikhafi, A., Ouakarrouch, M., Benallel, A., Tilioua, A., Ettakni, M., Babaoui, A., & Hamdi, M. A. A, Characterization and thermal performance assessment of earthen adobes and walls additive with different date palm fibers. Case Studies in Construction Materials, 15 https://doi.org/10.1016/j.cscm.2021.e00693,2021

[20]. Jin, X., Zhang, X., Cao, Y., & Wang, G. Thermal performance evaluation of the wall using heat flux time lag and decrement factor. Energy and Buildings, 47, 369-374. https://doi.org/10.1016/j.enbuild.2011.12.010 , 2012.

[21]. Asan, H., & Sancaktar, Y. S. Effects of wall's thermophysical properties on time lag and decrement factor. energy and buildings, 28(2), 159-166, https://doi.org/10.1016/S0378-7788(98)00007-3, 1998

[22]. Ulgen, K. Experimental and theoretical investigation of effects of wall’s thermophysical properties on time lag and decrement factor. energy and buildings, 34(3), 273-278. https://doi.org/10.1016/S0378-7788(01)00087-1,2002)

[23]. Vincent Zoma, Boureima Kaboré, Germain Wende Pouiré Ouedraogo and Sié Kam, Numerical Study of the Thermal Behavior of a Wall Containing Phase Change Material (PCM) in a Hot and Dry Climate, Physical Science International Journal. Volume 28, Issue 3, ISSN: 2348-0130

[24] . Malbila E., Toguyeni D.Y. Bathiebo D. J.& Koulidiati J. (2018).Hygrothermal behavior of two buildings constructed in cement bricks and cut laterite blocks. In WEENTECH Proceedings of the International Conference on Energy, Environment and Economics (pp. 1-7)