| Journal Name: | Journal of Scientific Research and Reports |
| --- | --- |
| Manuscript Number: | Ms_JSRR_158391 |
| Title of the Manuscript: | Green Synthesis and Physicochemical characterization of NiO-ZnO nanocomposites derived from Aloe vera leaf extract |
| Type of the Article | Research Article |

PART 1 (Importance of the manuscript)

|  | ## Comments of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| Please write a few sentences regarding the importance of this manuscript for the scientific community. A minimum of 3-4 sentences may be required for this part. | This manuscript demonstrates the green synthesis of NiO-ZnO nanocomposites from Aloe vera leaf extract and investigates their structural, optical, dielectric, and antimicrobial properties. The subject is timely and aligns well with current research on green materials synthesis in sustainable nanotechnology. Combining various characterization methods with a multidisciplinary potential in biomedical and electronic sciences makes it an important approach. Nonetheless, although the potential scope outlined is promising, this manuscript currently falls short on scientific rigor, data validation, and clarity about its contribution to the field. |  |

## PART 2.1 (Objective Evaluation)

|  | ## Rating of the Reviewers | Author’s Feedback |
| --- | --- | --- |
| 1. Is the title clear and appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 4 (Good) | ## 4 (Good) |
| ## 2. Is the abstract of the article comprehensive? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| ## 3. Are the keywords appropriate and useful? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| ## 4. Is the background information of the paper sufficient and well organized? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| ## 5. Are the research objectives/hypotheses clearly stated? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| ## 6. Is the literature review relevant and up to date? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## As per the reviewer ratings, we improve the relevant literature review and add the latest references in the manuscript. |
| ## 7. Is the research methodology appropriate for the study? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## As per the reviewer ratings, we improve the research methodology in the manuscript. |
| ## 8. Were ethical issues properly addressed (if applicable)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## We add ethical issues in the manuscripts. |
| 9. Are the results presented clearly? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## As per the suggestions, we improve the results and discussion’s part. |
| 10. Are tables and figures clear, relevant, and necessary? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## Ass per the reviewers rating, we change the figures clarity. |
| 11. Does the discussion relate findings to existing literature? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| 12. Are the conclusions supported by the data? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 3 (Satisfactory) | ## 3 (Satisfactory) |
| 13. Are the limitations of the study discussed? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 1 (Poor) | ## 1 (Poor) ## As per the reviewer ratings, we add the limitations of the studies in the manuscripts. |
| 14. Are the references relevant and sufficient (in number)? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## As per the reviewer ratings, we improve the relevant literature review and add more latest references in the manuscript. |
| 15. Is the manuscript written in clear and understandable language? Rating Scale: 5 = Excellent 4 = Good 3 = Satisfactory 2 = Needs Improvement 1 = Poor N/A = Not Applicable | 2 (Need Improvement) | ## 2 (Need Improvement) ## As per the reviewer ratings, we change and improve the language in the manuscript. |

## PART 2.2 (Subjective Evaluation)

|  | ## Reviewer’s comment | Author’s Feedback (It is mandatory that authors should write his/her feedback here) |
| --- | --- | --- |
| Is the title of the article suitable? If your answer is NO, please provide a brief, clear suggestion for improvement. | Yes | ## Yes |
| ## Is the abstract of the article comprehensive? s If your answer is NO, please provide a brief, clear suggestion for improvement. | No, If the findings were quantitative, please ensure to provide (as closely as possible) actual numbers in the appropriate measure whenever used in generalized terms, for example, crystallite size, band gap values, dielectric parameters, and antimicrobial activity. It should clearly specify if the material is a composite or doped system. | ## The synthesis resulted in a material where NiO was incorporated into a ZnO system, forming a composite rather than a purely doped lattice at higher concentrations. ## Crystallite Size: X-ray diffraction (XRD) confirmed an average crystallite size ranging from 19 to 20 nm. ## Crystal Structure: The system consists of a hexagonal wurtzite structure for ZnO and a face-centered cubic (FCC) structure for NiO. ## Lattice Parameters: For ZnO, the parameter a was measured at 3.250 Å, while c ranged from 5.2030 to 5.2060 Å. The Zn-O bond length was calculated to be approximately 1.9767 Å. ## Morphology: SEM imaging identified hexagonal and spherical morphologies with larger particle clusters measuring between 250 and 350 nm. |
| ## Is the manuscript scientifically correct? If your answer is NO, please provide a brief, clear suggestion for improvement . | No, Based on the above, the structural interpretation is highly inconsistent. While the manuscript claims that this material is a “single-phase structure”, XRD results can clearly show that both ZnO (wurtzite) and NiO (FCC) phases were present in the composite system, confirming this to be a bi-phasic composite polymer. Second, the terms Ni-doped ZnO and NiO-ZnO nanocomposite are used synonymously, which does not provide a scientifically correct definition. The date here is the interpretation of this system, and, based on the presented data, it should be described as a composite in every case revealed by the independent analyses. | ## Based on the reviewer comments, It is dual crystal structures and the functional behavior of the interfaces, the material is accurately described as a bi-phasic NiO-ZnO nanocomposite |
| Are the references sufficient and recent? (YES or NO) If your answer is NO, please provide clear suggestion for improvement. | No, More recent references (2022-2025) should be included in the manuscript; citations must be more consistent for similar NiO-ZnO systems. | ## As per the reviewer ratings, we improve the relevant literature review and add more latest references in the manuscript. |
| Are there ethical issues in this manuscript? (YES or NO) (If yes, kindly please write down the ethical issues here in details) | Yes, The study does not mention any biosafety protocols, and it doesn’t replicate experiments. In addition, statistical validation (e.g., standard deviation, error bars, and significance testing) is absent, which undermines the reliability of the reported results. | ## We add ethical issues in the manuscripts |

PART 3

| Editorial Comments (This section is reserved for the comments from journal editorial office and editors): |  |
| --- | --- |
|  | Author’s Feedback |
| Overall, the manuscript addresses a topical issue in green nanotechnology, but unfortunately, it presents several critical issues. This includes misinterpretation of the structure, discordance between the classification for doping and the composite, limited validation statistics, and exaggerated antimicrobial effects. | As per the Editorial, Comments We improve and change the research manuscript. |