### RETHINKING CEMENT PRODUCTION: ENVIRONMENTAL IMPACTS AND SUSTAINABLE SOLUTIONS

### Abstract

The cement industry is a fundamental pillar of modern infrastructure development; however, it is also one of the most environmentally intensive industrial sectors. Cement production contributes significantly to greenhouse gas emissions, energy consumption, resource depletion and environmental pollution. With global cement demand continuing to rise due to urbanization and infrastructure growth, mitigating its environmental footprint has become a critical challenge. This review examines the environmental impacts of the cement industry, focusing on carbon emissions, energy use, air and water pollution and resource exploitation. Furthermore, the paper discusses potential mitigation strategies, including alternative fuels, supplementary cementitious materials, energy-efficient technologies, carbon capture and storage and sustainable construction practices. The review highlights the need for an integrated approach combining technological innovation, policy intervention and sustainable material usage to achieve a low-carbon cement industry.

Keywords: Cement industry, Environmental impact, CO₂ emissions, Sustainable construction

- Introduction

As the cornerstone of modern infrastructure, cement binds together the very fabric of contemporary civilization, from towering skyscrapers and expansive bridges to essential housing and critical transportation networks. Concrete—the composite material whose primary binder is cement—stands as the second most consumed substance on Earth after water, with global production exceeding 4.3 billion tonnes annually (Ashour et al., 2024). This colossal scale of utilization underscores cement’s indispensable role in enabling urbanization, economic development and poverty alleviation, particularly in emerging economies. The growing demand for cement is driving the increased use of aggregates, especially limestone, which is essential in producing Portland cement. However, the extraction of non-renewable resources, such as limestone, is a major concern. As energy consumption has risen rapidly in the 21st century, the extraction of these resources is causing their depletion. Yet, this vital driver of human progress carries a profound and escalating environmental burden, positioning the cement industry at the critical nexus of developmental necessity and ecological sustainability.

The environmental implications of cement production are multifaceted and severe, extending across climate systems, natural resources and local ecosystems. Most prominently, the sector is a major contributor to global anthropogenic CO₂ emissions, accounting for an estimated 8–9% of the total—a footprint that, if attributed to a nation, would rank as the world’s third-largest emitter (Yang et al., 2024). This climate impact arises from an inherent chemical process: the calcination of limestone (CaCO₃) to lime (CaO), which releases CO₂ as an unavoidable byproduct, coupled with intensive fossil fuel combustion required to achieve kiln temperatures exceeding 1400°C. Beyond greenhouse gases, the industry drives significant resource depletion, including the large-scale extraction of finite geological limestone deposits, alongside substantial consumption of water and energy. Furthermore, cement manufacturing generates considerable air pollution (particulate matter, NOₓ, SO₂) land degradation from quarrying and water contamination, collectively threatening local environmental health and biodiversity.

This review article seeks to provide a comprehensive and critical synthesis of the current state of knowledge regarding the environmental impact of cement production, with a particular focus on the interconnected challenges of climate change and resource depletion. The analysis then extends to an evaluation of emerging mitigation strategies and innovative pathways aimed at decarbonizing the industry, including material substitution, alternative fuels, carbon capture and storage (CCS) and the development of novel low-carbon binders. By integrating findings from recent scientific literature, technological assessments and policy analyses, this review highlights both the urgent constraints imposed by planetary boundaries and the transformative opportunities for transitioning toward a circular and sustainable cement economy. Ultimately, we argue that reconciling the world’s infrastructure needs with ecological limits represents one of the most pressing material challenges of the 21st century, demanding coordinated innovation across science, industry and governance.

- Materials and Methods

This review employs a systematic and interdisciplinary approach to analyze and synthesize the environmental impacts of cement production, with a focus on resource depletion and decarbonization pathways. The methodology is structured to ensure comprehensiveness, transparency and replicability.

A systematic literature search was conducted using Scopus, Web of Science and Google Scholar for peer-reviewed articles (2010-2025), complemented by key reports from the International Energy Agency (IEA), the Intergovernmental Panel on Climate Change (IPCC), and the Global Cement and Concrete Association (GCCA). Search queries combined terms like ("cement production" AND "CO2 emissions"), ("alternative binder" AND "LCA"), and ("carbon capture" AND "cement"). Initial identification yielded over 800 records. After duplicate removal and screening of titles/abstracts against inclusion criteria (focus on environmental impact or mitigation), approximately 250 full-text articles were assessed. A final corpus of 50 references was selected for in-depth synthesis.

2.1  Global Use of Concrete and Cement Production

The 21st century is being built with concrete. As the essential substrate of urbanization, industrialization and modern infrastructure, concrete is more than a construction material—it is a geological signature of the Anthropocene (Miller et al., 2024). The widespread use of concrete is driven by its strength, durability, versatility and relatively low cost. Concrete structures have long service lives and can withstand harsh environmental conditions, making them suitable for a wide range of applications.

Cement production has grown in response to this rising demand for concrete. Today, billions of tonnes of cement are produced annually worldwide, making it one of the most manufactured materials on Earth. China is the largest producer and consumer of cement, followed by countries such as India, the United States, Vietnam and Turkey (Miller and Moore, 2020). Developing economies account for a major share of cement consumption due to large-scale housing projects, transportation networks and industrial expansion, while developed countries maintain steady demand for maintenance and modernization of existing infrastructure. The pie chart (Figure 1) shows the geographical distribution of cement production, emphasizing China's dominant share and the composition of the rest of the world. China dominates cement production, contributing nearly half of the world’s total output due to its extensive construction and infrastructure activities. India is the second-largest producer, driven by rapid urbanization and infrastructure development. The rest of Asia also accounts for a significant share, reflecting growing construction demand in developing economies. Overall, the chart highlights Asia’s dominance in global cement production.

Figure 1. Geographical distribution of cement production

  - Environmental Impact of Cement Production and Resource Depletion

The scale of global cement production required to support concrete use has raised serious environmental concerns, including high energy consumption, greenhouse gas emissions and depletion of natural resources. Cement production requires significant energy and raw materials. One of the major environmental impacts of cement production is resource depletion. Large quantities of limestone, clay and sand are extracted from the earth through mining and quarrying. Quarrying for limestone involves heavy machinery and raw materials like calcium, silicon, aluminum and iron are mixed to form clinker. This clinker is then heated in cement ovens at temperatures between 1200°C and 1450°C to produce cement. These activities lead to the depletion of non-renewable natural resources, alteration of landscapes, soil erosion, deforestation and loss of biodiversity (Telschow et al., 2012). Continuous extraction also affects local ecosystems and can disrupt groundwater systems, reducing water availability in surrounding areas.

Another serious concern is high energy consumption. Cement manufacturing requires extremely high temperatures (about 1400–1450°C) to produce clinker in rotary kilns. This process depends heavily on fossil fuels such as coal, petroleum coke and natural gas, leading to excessive use of non-renewable energy resources. The burning of these fuels releases large amounts of pollutants into the atmosphere. Significant quantities of carbon dioxide (CO₂) are released both from fuel combustion and from the chemical process of calcination, where limestone decomposes into lime. The cement industry alone contributes a substantial share of global CO₂ emissions, thereby intensifying climate change (Andrew, 2019). In addition, emissions of particulate matter, nitrogen oxides (NOₓ) and sulfur oxides (SOₓ) degrade air quality and pose health risks to nearby communities. Furthermore, cement plants consume large amounts of water for cooling and processing, which can lead to water scarcity, especially in water-stressed regions. Dust generation and solid waste from production further contribute to environmental degradation.

2.2.1  Impact of Cement Production on Air Pollution

Cement production is a major source of air pollution. One of the most harmful emissions from cement manufacturing is carbon dioxide (CO2), a key greenhouse gas that contributes to global warming. During the production process, CO2 is released when limestone (CaCO3) is heated to form calcium oxide (CaO). Cement production is responsible for about 5% to 7% of global CO2 emissions and 65% of greenhouse gases. It accounts for 12% to 15% of total industrial energy use and contributes 5% to 8% of industrial CO2 emissions. Although CO₂ is not a traditional air pollutant, its accumulation in the atmosphere intensifies the greenhouse effect and leads to long-term environmental and climatic impacts.

Other most significant air pollutants released is particulate matter (PM), including fine dust generated during quarrying, crushing, grinding, clinker production and cement packaging. Dust emissions occur during various stages, such as transportation, loading and unloading of clinker. These particles can remain suspended in the air and when inhaled, cause respiratory problems, eye irritation and other health issues in nearby communities.

Another major contributor to air pollution from cement plants is the emission of nitrogen oxides (NOₓ) and sulfur oxides (SOₓ), which are produced during high-temperature fuel combustion in kilns. These gases can react in the atmosphere to form smog and acid rain, damaging crops, soil, water bodies, and infrastructure. Cement manufacturing also releases carbon monoxide (CO) and volatile organic compounds (VOCs), further degrading air quality.

Overall, emissions from cement plants can significantly reduce air quality, harm human health and contribute to environmental degradation, emphasizing the need for effective pollution control technologies and cleaner production methods.

2.2.2  Impact of Cement Production on Water and Noise Pollution

Cement production also leads to water and noise pollution. Dust generated during the process can lower air quality and visibility. When the dust settles, it can contaminate water sources, affecting both human and animal health. Wastewater runoff from cement manufacturing can pollute rivers and groundwater supplies. This pollution is a serious concern, especially in areas with growing populations and urbanization, where poor land management can cause soil erosion and water runoff.

Noise pollution is another major issue in cement production. Noise comes from various stages such as raw material preparation, clinker burning, and heavy machinery used in the process. Cement plants produce different types of noise, including gas noise from blowers, mechanical noise from crushers and milling machines, and electromagnetic noise from electric motors. Continuous exposure to high noise levels can harm human health, leading to problems such as hearing loss, memory loss, hypertension, insomnia and fatigue. Long-term exposure to noise can also increase the risk of cardiovascular disease. Additionally, workers in cement plants may struggle to detect hazards due to the loud noise, affecting safety in the workplace (Canfeng et al., 2012).

2.2.3  Use of Chemical Additives in Cement Production:

Cement production is a complex process that involves several steps to produce high-quality cement. In this process, cement plants often use chemical additives to improve efficiency, control emissions and enhance the quality of the cement produced. Some of these chemical additives may contain oil-based components, which can end up in wastewater.

This wastewater generation during cement production, especially when it contains oil-based chemical additives, can have significant negative effects on the environment. These effects can range from contamination of water bodies to harming ecosystems, human health, and even the broader environmental balance. The incorporation of zinc oxide nanoparticles in cement grinding significantly reduces energy consumption while enhancing early hydration and maintaining mechanical performance (Osman et al. 2020).

The figure 2 illustrates the cement manufacturing process and shows how different stages contribute to air, water, and noise pollution. the diagram highlights that cement production not only consumes natural resources and energy but also creates significant environmental impacts through dust, emissions, noise, and pollution at every major production stage.

Quarry limestone,

clay, and other

materials

Crush

material

Pre-heat

mixture

Heat mixture to 1500°C to

calcinate limestone and

produce clinker

Ship, bag and

distribute dry

cement

Grind and cool

mixture

Heavy particle and dust and

noise emission from machine

Hazard gas, dust and

noise emission from

machine

Greenhouse gas emission

from limestone

decomposition and fuel

Vehicle, equipment

emission

Dusts from

atmosphere gather

on the water

surface

Dusts from

atmosphere gather

on the water

surface

Heavy particle and dust from

atmosphere gather on the water surface

Figure 2 Summarization diagram on the impact of cement production

- Sustainable Alternatives and Solutions in Cement Manufacturing

One important solution is the use of blended cements such as Portland Pozzolana Cement (PPC) and Portland Slag Cement (PSC), which partially replace clinker with industrial by-products like fly ash and blast furnace slag. This reduces carbon emissions, energy consumption and waste disposal problems. Another sustainable approach is the development of geopolymer cement, which uses industrial wastes such as fly ash and slag instead of limestone, significantly lowering CO₂ emissions.

Another promising approach is the use of recycled materials in cement production to reduce the consumption of natural resources and minimize environmental pollution. Industrial by-products and construction waste such as fly ash, blast furnace slag (Prosek et al., 2019), silica fume, recycled concrete powder, waste glass and demolished construction debris can be partially used as raw materials or clinker substitutes in cement manufacturing (Imbabi et al., 2012). This approach not only reduces landfill waste but also lowers energy consumption and carbon dioxide emissions associated with limestone extraction and clinker production. In addition, recycling materials helps conserve natural resources and promotes a circular economy in the construction industry. However, the quality, consistency and proper processing of recycled materials are critical to ensuring the strength and durability of the final cement product.

Sousa & Bogas, (2021) investigated the comparison of energy consumption and carbon emissions between traditional clinker production and recycled cement production to evaluate their environmental sustainability. The findings showed that, under conservative conditions, recycled cement production generates only about 58–74% of the carbon emissions produced during clinker manufacturing. Sensitivity analysis revealed that the major factors affecting emissions in recycled cement production are the moisture content of waste cement, the proportion of cement paste present in the waste material, and the energy required for the drying process. A major limitation of the recycling process is the pretreatment stage, particularly the washing and drying of waste materials, which increases energy demand and emissions. However, the study suggests that if these pretreatment stages are eliminated through the development of an efficient dry recycling process, carbon dioxide emissions could potentially be reduced to as low as 13% of those associated with traditional clinker production.

The production of ordinary Portland cement (OPC) contributes significantly to global carbon dioxide emissions due to the use of raw materials and the extremely high kiln temperature of about 1500°C required during manufacturing. To reduce these emissions, He et al., (2019) developed two types of recycled cement, namely RC-450°C and RC-800°C, produced by heating waste OPC paste at 450°C and 800°C respectively, followed by grinding in a ball mill. The use of recycled cement not only lowers CO₂ emissions but also helps reduce environmental problems associated with landfill disposal of demolished concrete waste. The study compared the carbon emissions generated during the production of OPC, RC-450°C, and RC-800°C by considering emissions from both fuel combustion and clinker materials. The results showed that RC-450°C production could reduce CO₂ emissions by about 94% compared to conventional OPC production. In addition, when mixed with water, RC-450°C was capable of capturing an extra 4% CO₂ by weight through the formation of calcium carboaluminate and calcite compounds. RC-450°C also demonstrated higher paste strength and lower carbon emissions than RC-800°C. Furthermore, the strength of RC-450°C paste was found to be comparable to that of OPC paste, indicating its potential to completely replace ordinary Portland cement in construction applications.

In addition to improving energy use, researchers have also explored using waste materials as partial substitutes for cement in concrete. Emphasize the potential for using waste products to replace a portion of the cement used in concrete (Ekincioglu et al., 2013). This not only reduces the need for limestone, a key raw material, but also helps decrease the environmental impact of cement production.

The use of agricultural waste materials as supplementary cementitious materials can significantly reduce cement consumption, save energy, and lower carbon dioxide (CO₂) emissions, thereby contributing to environmental sustainability. The use of paddy straw ash (rice straw ash) in cement production is an emerging sustainable approach for reducing environmental pollution and improving waste utilization. Paddy straw, an agricultural residue produced after harvesting rice, is often burned openly in fields, causing severe air pollution and greenhouse gas emissions. When this straw is burned under controlled conditions, the resulting ash contains a high amount of silica, which has pozzolanic properties similar to fly ash. This ash can be partially used as a substitute for cement or clinker in concrete and cement manufacturing. The use of paddy straw ash helps reduce cement consumption, lower carbon dioxide emissions, conserve natural resources, and manage agricultural waste effectively. It can also improve certain properties of concrete such as durability and resistance to chemical attack. In this study, rice husk ash (RHA) and wheat straw ash (WSA) were used together as ternary cementitious materials (TCM) to partially replace Portland cement in concrete mixtures. Concrete mixes containing 0%, 5%, 10%, 15%, and 20% replacement levels of RHA and WSA were investigated to evaluate their effects on fresh, physical, and hardened properties of concrete. A total of 240 specimens, including cubes, cylinders, and beams, were prepared using a 1:2:4 mix proportion with a water-cement ratio of 0.50 and cured for 7 and 28 days. The results indicated that the workability of fresh concrete decreased as the amount of TCM increased. However, at an optimum replacement level of 10% TCM (5% RHA and 5% WSA), the compressive strength, splitting tensile strength, and flexural strength improved by 12.65%, 9.40%, and 9.46% respectively after 28 days of curing. Additionally, the density and water absorption of concrete decreased with increasing TCM content, while drying shrinkage was also reduced. These findings demonstrate that the combined use of RHA and WSA can improve concrete performance while reducing the environmental impact associated with Portland cement production.

Several waste materials are being investigated for their ability to replace cement, including oyster shells, cockle shells, and eggshells (Olivia & Oktaviani, 2017). These materials, often discarded as waste, can provide an eco-friendly alternative. Additionally, industrial by-products such as fly ash, slag, rice husk ash, palm oil fuel ash, and waste ceramic powder have been used as supplementary cementitious materials (Diliberto et al., 2017). These materials have pozzolanic properties, meaning they can react with lime to form compounds that help strengthen concrete, making them valuable in reducing cement usage.

Chen et al., (2002) proposed an innovative method for utilizing waste glass in cement production through both laboratory experiments and industrial-scale testing in a cement plant. Laboratory analysis of 32 different glass samples indicated that the chemical composition of glass is influenced more by its application than by its color or source. The alkali content, which is a key concern in cement manufacturing, was found to range between 0 and 22%. For waste glass bottles commonly generated in Hong Kong, the sodium oxide (Na₂O) content varied from 10% to 19%, with an average value of approximately 15%. During plant trials, around 1.8 t/h of waste glass bottles were introduced into the rotary kiln along with 280–290 t/h of raw materials. The results showed no significant increase in sulfur dioxide (SO₂) emissions, while nitrogen oxide (NOx) emissions also remained stable since they mainly depend on kiln temperature. The sulfur trioxide (SO₃) content of the produced clinker was similar to that obtained without glass addition. Although the alkali content of the clinker increased slightly, it remained within acceptable statistical limits. Detailed quality assessment of the final cement demonstrated that the tested level of waste glass addition did not significantly affect cement performance or quality.

Incorporation of industrial by-products such as fly ash, ground granulated blast-furnace slag (GGBS), silica fume and limestone powder significantly improves the sustainability of cement pastes. Low-carbon cement pastes incorporating industrial by-products exhibit improved workability and controlled setting behavior when properly proportioned (Balestra et al., 2025)

Thermally converted sawdust acts as a reactive, porous additive, improving CO₂ uptake and refining the microstructure of cement-based materials. CO₂ curing synergizes with the sawdust-derived material to enhance early strength and durability while achieving significant carbon sequestration and overall CO₂ reduction (Song et al., 2025). Replacing high volumes of cement with limestone powder is an effective and practical strategy to reduce the carbon footprint of concrete while maintaining performance at optimized replacement levels. Cement replacement with limestone powder can reduce CO₂ emissions by 15–25%, depending on replacement level and mix design (Zydek & Tanner, 2025)

3.1  Solutions for Air & Noise pollution:

The cement industry’s harmful effects on the environment and human health have led to continuous efforts to reduce pollution caused by industrial activities. Various strategies are being applied to minimize these impacts. One effective method to reduce dust emissions is by frequently spraying water, oil, or other materials that help stabilize the soil, as suggested by (Jadoon et al 2016). This reduces the dust in the air. Additionally, dust emissions can be controlled by maintaining bag house filters properly (Zainudeen et al 2004), which trap dust particles. Electrostatic Precipitators, when designed and operated correctly, can also help minimize dust emissions from cement plants.

Noise pollution is another significant issue in cement manufacturing. To address this, technologies like noise attenuation, absorption, and insulation are used to reduce noise levels (Zhang et al 2012). Administrative measures, such as rotating workers from noisy to quieter areas, can also help reduce their exposure to harmful noise. In addition, workers can use ear protection such as earplugs and earmuffs. Earplugs can reduce noise by around 30 dBA, while earmuffs can reduce it by 40-50 dBA, helping to protect workers' hearing. Many cement companies already offer ear protection devices to workers and have standard operating procedures (SOPs) in place to manage noise levels in the workplace (Anwar et al 2013).

Another challenge is the impact of oily wastewater on water systems. To address this, superhydrophobic materials are being used to separate oil from water in cement plants (Gou et al 2020). Several methods are available for producing these materials, such as electrostatic assembly, condensation, anodization, hydrothermal treatment, and plasma treatment, among others. These techniques help in creating materials that can efficiently separate oil and water, improving water quality. However, more work is needed to develop these solutions in a cost-effective, environmentally friendly way.

The carbon footprint of concrete can be reduced by using Portland-Limestone Cement, as it lowers clinker content and thereby reduces CO₂ emissions from calcination and fuel consumption. Zydek, C. J., & Tanner, J. E. (2025)

- Conclusion

Cement production stands at a critical juncture. While its environmental impacts are severe, the breadth and depth of emerging sustainable solutions presented in this review offer a credible pathway for transformation. The journey from a linear, high-emission model to a circular, low-carbon industry will be complex and capital-intensive, demanding unprecedented collaboration between industry, academia, policymakers, and the construction sector. The imperative is clear: rethinking cement is not merely a technical challenge but a prerequisite for sustainable development. By aggressively pursuing the integrated hierarchy of solutions—from using less, to using better, to capturing the rest—the cement industry can transform itself from a climate problem into a vital part of a net-zero future. The time for incremental improvement has passed; the era of systemic re-invention must begin.

References

Andrew, R. M. (2019). Global CO 2 emissions from cement production, 1928–2018. Earth System Science Data, 11(4), 1675-1710.

Ashour A., Wang X. & Han B. (Eds.). (2024). Sustainable Concrete Materials and Structures. Elsevier

Balestra, C. E. T., Dragunski, D. C., Neckel, R. M., Silvestro, L., Savaris, G., & Schneider, R. (2025). Fresh Properties of Low-Carbon Cement Pastes Incorporating Industrial By-Products. Journal of Materials in Civil Engineering, 37(1), 04024443.

Canfeng, Z., Shujie, Y., & Dong, L. (2012). Comprehensive control of the noise occupational hazard in cement plant. Procedia Engineering, 43, 186-190.

Chen, G., Lee, H., Young, K. L., Yue, P. L., Wong, A., Tao, T., & Choi, K. K. (2002). Glass recycling in cement production—an innovative approach. Waste Management, 22(7), 747-753.

Diliberto, C., Lecomte, A., Mechling, J. M., Izoret, L., & Smith, A. (2017). Valorisation of recycled concrete sands in cement raw meal for cement production. Materials and structures, 50(2), 127.

Ekincioglu, O., Gurgun, A. P., Engin, Y., Tarhan, M., & Kumbaracibasi, S. (2013). Approaches for sustainable cement production–A case study from Turkey. Energy and Buildings, 66, 136-142.

Gou, X., Zhang, Y., Long, L., Liu, Y., Tian, D., Shen, F., ... & Deng, S. (2020). Superhydrophilic and underwater superoleophobic cement-coated mesh for oil/water separation by gravity. Colloids and Surfaces A: Physicochemical and Engineering Aspects, 605, 125338.

He, Z., Zhu, X., Wang, J., Mu, M., & Wang, Y. (2019). Comparison of CO2 emissions from OPC and recycled cement production. Construction and Building Materials, 211, 965-973.

Imbabi, M. S., Carrigan, C., & McKenna, S. (2012). Trends and developments in green cement and concrete technology. International Journal of Sustainable Built Environment, 1(2), 194-216.

Miller S. A., Juenger M., Kurtis K. E., & Weiss J. (2024). Cement and Alternatives in the Anthropocene. Annual Review of Environment and Resources, 49.

Miller, S. A., & Moore, F. C. (2020). Climate and health damages from global concrete production. Nature Climate Change, 10(5), 439-443.

Miller, S. A., Horvath, A., & Monteiro, P. J. (2018). Impacts of booming concrete production on water resources worldwide. Nature Sustainability, 1(1), 69-76.

Mohamad, N., Muthusamy, K., Embong, R., Kusbiantoro, A., & Hashim, M. H. (2022). Environmental impact of cement production and Solutions: A review. Materials Today: Proceedings, 48, 741-746.

Oh, D. Y., Noguchi, T., Kitagaki, R., & Park, W. J. (2014). CO2 emission reduction by reuse of building material waste in the Japanese cement industry. Renewable and Sustainable Energy Reviews, 38, 796-810.

Olivia, M., & Oktaviani, R. (2017). Properties of concrete containing ground waste cockle and clam seashells. Procedia engineering, 171, 658-663.

Osman, D. A. M., Nur, O., & Mustafa, M. A. (2020). Reduction of energy consumption in cement industry using zinc oxide nanoparticles. Journal of Materials in Civil Engineering, 32(6), 04020124.

Prošek, Z., Nežerka, V., Hlůžek, R., Trejbal, J., Tesárek, P., & Karra’a, G. (2019). Role of lime, fly ash, and slag in cement pastes containing recycled concrete fines. Construction and Building Materials, 201, 702-714.

Song, S., Liu, G., Liu, Z., Liu, J., Teng, J., & Shi, H. (2025). Synergistic Effects of Thermally Converted Sawdust and CO 2 Curing on Cement-Based Materials. Journal of Materials in Civil Engineering, 37(8), 04025251.

Sousa, V., & Bogas, J. A. (2021). Comparison of energy consumption and carbon emissions from clinker and recycled cement production. Journal of cleaner production, 306, 127277.

Telschow, S., Frandsen, F., Theisen, K., & Dam-Johansen, K. (2012). Cement Formation A Success Story in a Black Box: High Temperature Phase Formation of Portland Cement Clinker. Industrial & engineering chemistry research, 51(34), 10983-11004.

Yang Y., Liu Y., Liu L., Liu Z., & Wu H. (2024). Monitoring global cement plants from space. Remote Sensing of Environment, 302, 113954.

Zainudeen, N., & Jeyamathan, J. (2008, February). Cement and its effect to the environment: A case study in SriLanka. In Proc. from Int. Conf. Build. Educ. Res (pp. 1408-1416).

Zydek, C. J., & Tanner, J. E. (2025). Reducing the Carbon Footprint of Concrete by Replacing High Volumes of Cement with Limestone Powder. Journal of Materials in Civil Engineering, 37(4), 06025002.