Assessment of the Physical Properties of Reclaimed Fine Aggregate as a Viable Concrete Material for Recycling and Sustainable Use

Abstract

As a result of rapid urbanization especially in the developing nations, there is increasing demand for sustainable construction materials. This coupled with increasing cost of the materials and environmental degradation as a result of mining of aggregates, there has been growing interest in the reuse of construction and demolition waste(CDW). Reclaimed fine aggregate (RFA), refers to fine aggregate derived from crushed concrete waste. It is being considered as a possible alternative to natural river sand in concrete production. This study assesses the integrity of RFA as a viable material for concrete by focusing on its physical characteristics. Study is light for comparison with require limits from standards. It is therefore concluded that RFA is unsuitable for complete substitution of natural aggregate in concrete production. However, it is recommended as partial replacement for natural aggregate in concrete production.

Key Words: Integrity, Reclaimed Fine Aggregate, Viable, Concrete, Demolition Waste, Sustainable.

1. INTRODUCTION

Significant volumes of C&D waste are generated annually in the construction industry as a result of rapid urbanization. This has resulted in increased rate of environmental degradation and resource depletion. In the opinions of Kumar et al., (2020), it is projected that construction waste could exceed 3.4 billion tonnes by 2050 globally. This is alarming and poses a lot of challenge to the environmental condition of the surrounding localities. Hence, there is the need for recycling strategies being emphasized. One means of providing sustainable solution is the reuse of waste concrete as reclaimed fine aggregate in new concrete production.

Natural fine aggregates, particularly river sand, are becoming scarce due to over-extraction and rising cost of transportation (United Nations Environment Programme (2019), In view of this the use of alternative materials such as RFA are gaining attention as substitutes. However, there is also a growing concern about their structural integrity and durability which is posing a great challenge to its widespread adoption.

Concrete and Demolition waste disposal can result into surface water contamination. In the words of Amoatey and Baawain (2019), the effect of contaminants on surface water like ponds and rivers on aquatic flora and fauna can be very harmful. Aside this, CDW can cause air pollution it can increase the presence of harmful and various poisonous gases, such as carbon monoxide (CO), carbon dioxide (CO2), hydrogen fluoride (HF), sulphur dioxide (SO2), oxides of nitrogen (NOx), particulate matter, such as PM10, asbestos, and volatile organic compounds (Silva et al., 2014).

According to (Kantová, 2017), a lot of noise is being generated by concrete mixers, earthmoving machinery, pile drivers, pneumatic devices, and various other operating machineries at the CDW sites in the cause of CDW disposal. The effect of the noise pollution can bring about a lot of stress, irritability, sleep disturbances, high blood pressure, irregular heartbeats heart diseases, and noise induced hearing loss. Since most of the waste generated by the CDW is inert and non-degradable it can also affect agricultural land. The effect of CDW disposal affects virtually every facet of human activities including schools, colleges, old age home, nursing homes, offices, clinics, and hospitals.

Going through available literatures, research efforts on the use of construction and demolition waste as a viable material of construction in Nigeria only predominantly focused on the recycling of coarse aggregate without due consideration for fine aggregate. The existing studies also lay emphasis on the mechanical performance of recycled materials, particularly compressive strength of concrete produced from recycled coarse aggregate. The impact of the essential physical properties that dictate the behavior of fine aggregates in concrete is not taken into account. Consequently, this study aims to address the identified deficiencies by delivering a thorough evaluation of the physical properties of reclaimed fine aggregate sourced from local demolition waste and assessing its viability as a sustainable alternative to natural fine aggregate for concrete production in Nigeria.

1.1 Characteristics of Reclaimed Fine Aggregate

Bu et al. (2022) posited that RFA are obtained by crushing used concrete from CDW and as such it may contain residual mortar attached to original aggregates. Consequently, it is expected that the adhered mortar will affect the physical properties of RFA significantly. According to the authors, the effects include increased porosity and water absorption. Kim et al (2019) further opined that RFA can contain certain impurities that can cause variability in the quality of concrete and consequently influence concrete performance and durability.

1.2 Physical and Micro – structural Characteristics of Recycled Aggregates

The differentiating elements between RCA natural aggregates River Sand are the combination of materials and the history of its use. According to Abbas et al., (2009) RFA contains layers of adhered old and porous mortar on the surface of the original natural aggregate after crushing. The quantity of adhered mortar makes up for up to 25-65% of the RCA particle volume. As a result of this hifh percentage of adhered mortar, there is a previously exerted external pressure and environmental conditions extreme porosity causing micro-cracked condition. This can further lead to increase in water absorption up to 10 times natural aggregate with considerable changes in the major properties of RFA. Additionally, Katz, (2003) opined that bulk specific gravity can decreases by about 5 to 20 percent when compared to natural aggregates. RFA particles become more angular with rougher surfaces because the crushing process creates particles that differ from the natural gravel and crushed stone which typically has smooth and rounded surfaces. The concrete mix's particle packing and inter-particle friction get affected by this altered material structure. The total RCA grading shows differences because the brittle fracture of adhering mortar during processing creates higher amounts of fine particles which get released into the final product (Silva et al., 2017). The engineering behavior of RAC systems develops from their physical properties which include high absorption and low density and angularity and varying grading patterns because these properties determine all aspects of fresh mix rheology and long-term durability

1.3 Sources and Composition of CDW

The diverse materials in Construction and Demolition Waste create an unpredictable waste stream, which primarily consists of hardened concrete. The source material known as "concrete demolition waste" originates from planned building demolitions and structural failures and natural disasters and armed conflicts. The processed recycled concrete aggregate (RCA) consists of natural aggregates which combine with hydrated cement paste (HCP) and mortar and various contaminants. The contaminants of this material include ceramic materials which consist of bricks and tiles and gypsum products and wood and plastics and residual metals from reinforcement. The various qualities of source material create a main obstacle which prevents recycling facilities from achieving consistent RCA quality testing results (Silva et. al., 2014).

1.4 RFA Conversion Process

Several mechanical processes are required in converting large amounts of CDW into reusable RFA. These procedures can be broken down into primary and secondary stages. The primary stage involves crushing or breaking down large pieces before secondary and tertiary crushing processes where the required particle size distributions are created. This is followed by the screening process where materials are divided into multiple size categories. The last stage is the cleaning procedures where water washing and air sifting and manual picking aim to eliminate light contaminants and fine particles take place Verian et. al., 2018. Advanced facilities use magnetic separation methods to extract ferrous metals and advanced sorting systems to process materials. According to Oikonomou (2005), the final quality of the RCA depends on processing methods and the inherited properties which the parent concrete structure possesses through its original strength and porosity and exposure history. According to Dimitriou et. al.(2018.) production of consistent results in quality control testing requires processing functions and source identification to be evaluated.

1.5 Durability Considerations

Durability is a major consideration in concrete production and it remains a key concern in RFA concrete. However, durability of concrete is dependent on the properties of its constituent materials. Hence, there is the need for assessment of the properties of RFA so as to ascertain its suitability for use in concrete production. However, durability can be improved using supplementary cementitious materials such as fly ash and silica fume, which reduce porosity and enhance bonding (Bu et al., 2022).

1.6 Environmental and Economic Benefits

In the opinions of Li et al., (2018), the use of RFA as substitute for river sand has lots of environmental and economic benefits. Some of these benefits include waste reduction, natural resources conservation, and lower construction costs. It can also result in minimization of landfill usage and environmental pollution and make it an essential component of sustainable construction practices.

1.7 Objectives of the Study

The objectives the study is to assess the physical properties of sourced RCA and to compare the results obtained conventional natural Rivers Sand and relevant standards.

2. Methodology

The need to understand the characteristic properties of RFA and natural river sand is necessary and it involves both theoretical understanding and experimental evaluation. Theoretically, the study tries to explain the behavior of aggregates based on the principles from materials science and geotechnical engineering, which relate aggregate properties. On the other hand experimental and standardized laboratory tests are conducted in accordance with specifications such as ASTM C33 and BS 882. Common tests include sieve analysis to determine grading, specific gravity and water absorption tests, bulk density measurement, and moisture content determination. For RFA, special attention was given to its higher water absorption capacity, lower density, and potential impurities compared to river sand. These differences are experimentally quantified and then interpreted using theoretical models to evaluate their influence on workability, strength development, and long-term performance. By integrating theoretical predictions with empirical results, a comprehensive understanding of the suitability of RFA as a partial or full replacement for river sand in construction applications is advocated.

. The key parameters evaluated include:

- Shape and Texture

- Particle size distribution

- Specific gravity

- Water absorption capacity

- Moisture Content

- Percentage silt content

- Bulking

Comparative analysis was conducted between natural fine aggregate (river sand) and RFA

2.1 Material Acquisition

The sample of RFA used in the study was collected from demolition waste (CDW) from a designated site in Ilaro, Ogun State.  The used concrete materials consist of demolished concrete materials like beams, columns, and slabs. The material was procured and transported to the laboratory for the purpose of this research.

2.2 Processing of Recycled Fine Aggregate (RCA)

The procured CDW were subjected to two stages of crushing. The first stage involves the manual breaking of concrete lumps by a mechanical breaker (jackhammer) to achieve the desired size. The second stage is the breaking of the resulting debris by passing them through a machine. The process of separation was done through a series of crushing and mechanically sieved to separate the coarse recycled concrete aggregate (RCA) and RFA. The target grading for coarse RCA was 4.75mm to 19mm, while that of RFA passed the 4.75mm sieve.

2.3 Integrity Test of Recycled Fine Aggregate

The integrity test on the recycled fine aggregate and river sand was carried out in the laboratory. The properties examined are the parameters stated in section 2.0. They were carried out in line with specifications in BS EN, 933 – 1:2012, BS 812-103.1:1985, BS 812-109:1990, BS 812 – 124:1989 respectively.

2.3.1 Sieve Analysis

Sieve analysis was used to find the particle size distributions of the two types of aggregates. In carrying out the test, 500gram of the samples were passed through a series of standard sieves with mesh sizes positioned on one another in descending orders of their sizes. The percentage of materials that stayed on and passed through each sieve were used that to make grading curves. The Fineness Moduli (FM) of the samples were determined from the Sieve Analysis Table by dividing the sum of the cumulative percentage passing by 100. In the same vein, the Coefficient of uniformity and the Coefficient of Curvature were calculated using equation 1 and 2 respectively.

Cu= D60 D30                                                                                                                                     (1)

CC= D302D60 × D10                                                                                                                            (2)

Cu is Coefficient of Uniformity, Cc is the Coefficient of Curvature, D10 is the size of the particles at which 10% of the samples pass through the sieves, D30 is D30 is the size of the particles at which 10% of the samples pass through the sieves and D60 is D60 is the size of the particles at which 10% of the samples pass through the sieves.

2.3.2 Test for Specific Gravity 
Specific gravity of aggregates gives the information about the density and strength of aggregates. While the Water Absorption refer to the amount of water that a dry aggregate can absorb when it comes in contact with water. The two properties were determined using the pycnometer method in accordance with specifications In BS in carrying out the test, the mass of oven-dried aggregate was determined alongside its corresponding displaced water volume. Equations 3 and 4 were used in calculating the Specific Gravity and Water absorption respectively.

The apparent specific gravity is lw M4M4-M2-M3                                                                                                        (3)

M1 = mass of saturated surface dry sample in air, M2 = apparent mass in water of the basket containing the saturated sample in grams, M3 = apparent mass in water of the empty basket in grams, and M4 = ass of oven dried test portion in air in grams. ℓw = density of water at the temperature recorded when M2 was calculated in mega grams per meter.
The test was repeated to check specific gravity to within 0.02 and water absorption 0.05%

The percentage of absorption M1-M2M4×100%                                                                                                    (4)

2.3.4 Determination of Moisture Content of Fine and Coarse Aggregate.

The moisture content of the samples were determined by oven dreying them in a ventilated oven at a temperature of about 100 ± 50C as stated in BS 812-109:1990. The calculation was carried out by the use of the formulae:

Moisture Content (% dry mass) = M2-M3M3-M1×100                                                                                                    (5)

2.3.5 Percentage Silt Content.

The test was conducted in compliance with standard test method stated in B.S. EN 1097 – 6:2022. Percentage silt content is calculated using equation 3.10
V=V1V2×100											          (6)

Where: V1 is the volume of the silt layer and V2 is the sand level below the silt,

2.3.6 Bulking

Bulking is determined using procedures of BS 812-2: 1995.The following procedures was taken: after allowing the 500g oven-dried fine aggregate sample to cool to room temperature at 100 degrees Celsius, it was weighed and measured as W1. After the sample was weighed and stored in an airtight container, the weight was noted as W2. 
The water content was calculated using Equation 7.

WC=W1-W2W1X 100                                                                                                                                                     (7)

## 2.3 7 Reliability and Validity

All tests were carried out in triplicate and average values were reported to ensure reliability, additionally, standard procedures were strictly followed in accordance relevant codes and standards so as to minimize experimental errors. The use of internationally recognized testing standards and properly calibrated equipment helps to ensure the validity of the experimental work.

3.0 Results and Discussions

As stated earlier, the performance of concrete in service and its durability depends on the characteristic properties of its constituent materials. The results obtained from the integrity test carried out on both materials are discussed extensively in this section. Furthermore, comparisons were drawn to ascertain the possibility of substituting RFA for river sand in the manufacture of concrete.

3.1 Texture

The result of the test carried out to determine the surface texture of both materials indicates that both materials have rough surface textures. This is very advantageous for concrete performance because a rough surface enhances the mechanical interlocking and bond strength between the aggregate and cement paste (Neville, 2011). The implication of this is that the use of RFA is unlikely to negatively affect the interfacial transition zone (ITZ) but rather contribute to improved bonding characteristics in concrete.

3.2 Gradation

3.2.1 Sieve Analysis

From the sieve analysis results shown in Figure 1, the Fineness Modulus (FM), Coefficient of Uniformity (Cu), and Coefficient of Curvature (Cc) were determined. The fineness moduli of the two materials are 2.82 and 2.92 respectively. According to Neville (2011`), fine aggregates with FM between 2.3 and 3.1 are generally considered as suitable for concrete production. These results shows that both materials are medium sand with FM ranging between 2.6 t0 2.9. This range is the ideal range recommended for structural concrete because it balances workability with strength characteristics (ASTM C33). The result thus indicates that both materials have similar grading characteristics.

Figure 1: Sieve Analysis Curve of River Sand and RFA

Figure 2: Chart of Gradation Parameters

3.2.2 Coefficient of Uniformity and Coefficient of Curvature.

According to Das (2015), fine aggregates with Cu values of less than 4 is considered to be poorly graded while values greater than 4 are said to be well graded. From the results presented in Figure 2, River Sand and RFA has Cu of 4.5 and 4 respectively, hence both materials are well graded. This is an indication that both materials the range of particle sizes aregood implying that the voids between larger particles are filled by smaller particles. The effect of this is that the concrete produced from the samples will have better packing and higher density, high compaction efficiency, greater strength and stability and Moderate permeability.

3.3 Physical Properties of RFA and River Sand

The results of the physical properties of RFA and River Sand are discussed under this section. The properties considered are specific gravity, water absorption, moisture content, percentage silt content and bulking

3.3.1 Specific Gravity

The results of the specific gravity of both materials (river sand and RFA) are 2.62 and 2.50 respectively. This Mean that the specific gravity of River Sand is higher than that of RFA. The lower specific gravity of RFA can be attributed to the presence of adhered mortar and higher porosity, which reduces its density. The effect of this reduction can lead to slightly lower concrete density and increased paste demand. However, the values fall within acceptable limit of 2.5 -2.7 ((Neville, 2011; Shetty, 2005), thus confirming that RFA can be used in structural concrete with proper mix adjustments.

Figure 3: Specific Gravity of River Sand and RFA

3.3.2 Water Absorption

The result of the Water Absorption test as presented in Figure 3 reveals that there is a significant difference between the value of River Sand (0.5%) and Recycled aggregate (3.4%). The high water absorption of RFA can be attributed to its porous structure and residual cement paste. The likely effect of this is that there may be an increased water demand in concrete mix this can lead to risk of altering the water-cement ratio, which directly affects strength and durability and if not done it will result in potential reduction in workability. In order to maintain mix consistency and performance, there is the need to pre-soak the RFA or adjust water cement ratio.

Figure 4: Physical Properties of River Sand and RFA

3.3.3 Moisture Content

From the results of the moisture content of both samples presented in Figure 4, the value for River Sand is (2%) while that of RFA is (6%). The value for River Sand is considerably higher than that of RFA. Although BS EN 1097 – 2:2020 does not specify any limit, it requires accurate measurement for mix design adjustments. The effect of the higher value of moisture content in RFA is that it can contribute to increase in bulking of the sample (Portland Cement Association (2016) Neville, 2011; Shetty, 2005;).  It can also affect the workability of fresh concrete and as well alter the effective waster cement ratio of the concrete mix. In order to avoid inconsistencies in concrete quality, it is needful to ensure proper moisture correction.

From Figure 4, River sand has a bulking value of 17% while RFA has a value of 30%. This implies that the volume of River sand is 17% more than its dry volume, consequently necessary adjustment must be made to cater for the difference if volume batching is to be adopted. Alternatively the mix must be batch by weight. The result of River sand indicates a sample with moderate moisture content which is typical of slightly damp sand. On the other hand, RFA with bulking value of 30% indicates a sample with high moisture content which is at about the optimum bulking condition. This can be as result of the adherence of mortar and dry cement paste to the particles of the sample. The inference on this is that it has a tendency to significantly expand in volume. This has a negative influence that can lead to low sand content mix causing harsh concrete and reduced strength.

3.3.4 Percentage Silt Content

The silt content of sand is the amount of very fine particles usually the percentage of the particles that passes through the 75 µm sieve present in the aggregate. It is an important quality parameter in Concrete Technology due to the effect bonding and strength of concrete materials as a result of the presence of excess fines in the material. River Sand with silt content of 3% falls within the acceptable range for most codes of practice for concrete materials. The range according to ASTM C33:2016 and BS 882:2004 is < 5%. It implies that the sand is clean and suitable for concrete works with minimal effect on strength and durability of concrete. Conversely, RFA with silt content value of 6% possess fines of slightly higher content than the specified limit of 5%. The effect of this is that it will produce weak bond between cement paste and aggregate, increase the water demand and reduced strength and durability (Neville, 2011; Shetty, 2005; ASTM C33, 2020). To avoid these negative effects it will be necessary to ash the sand before use or to blend with cleaner sand.

3.3.5 Bulking

From Figure 4, River sand has a bulking value of 17% while RFA has a value of 30%. This implies that the volume of River sand is 17% more than its dry volume, consequently necessary adjustment must be made to cater for the difference if volume batching is to be adopted. Alternatively the mix must be batch by weight. The result of River sand indicates a sample with moderate moisture content which is typical of slightly damp sand. On the other hand, RFA with bulking value of 30% indicates a sample with high moisture content which is at about the optimum bulking condition. This can be as result of the adherence of mortar and dry cement paste to the particles of the sample and the relatively high moisture content. The inference on this is that it has a tendency to significantly expand in volume. This has a negative influence that can lead to low sand content mix causing harsh concrete and reduced strength. Additionally, the risk of volumetric errors during batching and inaccurate proportioning of materials can not be ruled out.

4.0 Conclusion

Based on the results obtained in the study, it can be concluded that properties of RFA differ significantly from that of River Sand possibly due to its higher water absorption, moisture content, and fines content.

Further conclusions are that the specific gravity and grading are comparable thus supporting its possible suitability. Although, the RFA has higher water absorption and moisture content this can be taken care of by adjusting the mix design parameters. The excessive bulking tendencies can also be limited by carefully controlling the batching or better still by adopting the method of batching by weight. In addition proper processing, grading, and quality control of reclaimed fine aggregates can improve the quality of the properties of the material which can in turn improve the performance when used in concrete production.

ACKNOWLEDGEMENT

The authors wish to acknowledge the contributions of TETFUND in providing financial support for the research by funding the research.

COMPETING INTERESTS DISCLAIMER:

Authors have declared that they have no known competing financial interests OR non-financial interests OR personal relationships that could have appeared to influence the work reported in this paper.

Disclaimer (Artificial intelligence)

Author(s) hereby declare that NO generative AI technologies such as Large Language Models (ChatGPT, COPILOT, etc.) and text-to-image generators have been used during the writing or editing of this manuscript.

References

Abbas, A., Fathifazi, G., Isgor, O. B., Razaqpur, A. G., Fournier, B., & Foo, S. (2009). Durability of recycled aggregate concrete designed with equivalent mortar volume method. Cement and Concrete Composites, 31(8), 555–563.

Amoatey, P., and  Baawain, M. S. (2019). Effects of pollution on freshwater aquatic organisms. Water Environment Research, 91(10), 1272–1287.

ASTM C 33: Standard Specification for Concrete Aggregates, (2016)., American Society for Testing and Materials (ASTM), West Conshohocken, PA, ASTM C 33,

ASTM International (2020). ASTM C33/C33M: Standard Specification for Concrete Aggregates.

BS 812: Part 103, (1985). “Methods for Determination of Particle Size Distribution”, British Standard Institution London.

BS 812: Part 109: 1990 Methods for Determination of Moisture Content, BSI British Standards Institution London, BSI British Standards Institution London

BS 812-124:2009, Testing aggregates - Method for determination of frost heave, British Standards Institution London.

BS EN 882: (2004) Specification for Aggregates from Natural Sources for Concrete,British Standards Institution London.

BS EN 933 – 1:2012, Tests for geometrical properties of aggregates.Methods for Determination of Particle Size Distribution”, British Standard Institution London.

BS EN 1097 – 2:2020 - Tests for mechanical and physical properties of aggregates. Determination of loose bulk density and voids – BSI British StandardsInstitution London.

Bu, C., Liu, L., Lu, X., Zhu, D., Sun, Y., Yu, L., & Wei, Q. (2022). The durability of recycled fine aggregate concrete: A review. Materials, 15(3), 1110. https://doi.org/10.3390/ma15031110

Das, B. M. (2010/2015). Principles of Geotechnical Engineering.

Dimitriou, G., Savva, P., & Petrou, M. F. (2018). Enhancing mechanical and durability properties of recycled aggregate concrete. Construction and Building Materials, 158, 228–235.

Katz, A. (2003). Properties of concrete made with recycled aggregate from partially hydrated old concrete. Cement and Concrete Research, 33(5), 703–711.

Kim, H., Lee, S., & Park, J. (2019). A study on the properties of recycled aggregate concrete and its production facilities. Applied Sciences, 9(9), 1935.

Kumar, R., Singh, S., & Sharma, P. (2020). Durability studies on recycled fine aggregate concrete. Construction and Building Materials, 250, 118850.

Li, X., Ling, T. C., & Mo, K. H. (2018). Study on waste concrete as reclaimed fine aggregate. Applied Mechanics and Materials, 121–126, 2942–2945.

Neville A. M. Properties of Concrete, 5th edition. Pearson Education Limited 2011

Oikonomou, N. D. (2005). Recycled concrete aggregates. Cement and Concrete Composites, 27(2), 315–318.

Poon, C. S., & Chan, D. (2006). Feasible use of recycled aggregates in concrete. Resources, Conservation and Recycling, 47(3), 234–250.

Portland Cement Association (2016). Design and Control of Concrete Mixtures (16th ed.). PCA.

Shetty, M. S. (2005). Concrete Technology: Theory and Practice. S. Chand.

Silva, R. V., de Brito, J., & Dhir, R. K. (2014). Properties and composition of recycled aggregates from construction and demolition waste. Construction and Building Materials, 65, 201–217

Silva, R. V., de Brito, J., & Dhir, R. K. (2017). Availability and processing of recycled aggregates within the construction and demolition supply chain: A review. Journal of Cleaner Production, 143, 598–614.

United Nations Environment Programme (2019), Sand and sustainability: Finding new solutions for environmental governance of global sand resources. UNEP.

Verian, K. P., Ashraf, W., & Cao, Y. (2018). Properties of recycled concrete aggregate and their influence in new concrete production. Resources, Conservation and Recycling, 133, 30–49.